SUPPLEMENTARY
18 Jan 2000
03390sup
UPDATES  -

18 Jan 00
-
Added Euclid Chemical products



SECTION  03390


CONCRETE CURING
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and apply curing compounds to Portland cement concrete paving as described in Contract Documents.

2.
Furnish and apply curing compounds to concrete slabs and exterior flatwork as described in Contract Documents, if approved by Architect in writing prior to use.

B.
Related Sections

1.
Division 02  -

a.
Cast-in-place concrete site elements
02776
b.
Portland cement concrete paving
02753sup
2.
Section 03313  -  Normal weight structural concrete
03313
 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing & Materials
ASTM
1.
ASTM C 309-98a, 'Standard Specification for Liquid Membrane-Forming Compounds for Curing Concrete'

 1.3
SUBMITTALS
A.
Product Data  -  Manufacturer's product data.
Product Data
B.
Quality Control  -  Manufacturer's printed installation instructions.
Quality
PART 2 PRODUCTS
 2.1
MATERIALS
A.
Interior

1.
Low VOC (less than 300 grams per liter), water-borne, membrane forming curing compound meeting requirements of ASTM C 309, Type 1D, Class B.

2.
Acceptable Products And Manufacturers  -
Approved Products
a.
Day Chem Rez Cure (J-11-W) by Dayton/Richmond Concrete Accessories, Miamisburg, IL  (800) 745-3700  www.daytonrichmond.com
b.
Kurez W VOX by Euclid Chemical Co, Cleveland, OH  (800) 321-7628 www.euclidchemical.com
c.
Horncure 100 by TAMMS Industries, Mentor, OH  (800) 218-2667 www.tamms.com
d.
L & M Cure R by L & M Construction Chemicals, Omaha, NE  (800) 362-3331  www.lmcc.com
e.
1100-WD by W. R. Meadows, Elgin, IL  (847) 683-4500 www.wrmeadows.com
f.
Equal as approved by Architect before use.  See Section 01600.

B.
Exterior

1.
Low VOC (less than 300 grams per liter), water-borne, membrane forming curing compound meeting requirements of ASTM C 309, Type 2.

2.
Acceptable Products And Manufacturers  -
Approved Products
a.
Day Chem White Pigmented (J-10-W) by Dayton/Richmond Concrete Accessories, Miamisburg, IL  (800) 745-3700 www.daytonrichmond.com
b.
Aqua-Cure VOX by Euclid Chemical Co, Cleveland, OH  (800) 321-7628  www.euclidchemical.com
c.
Horncure 200-W by TAMMS Industries, Mentor, OH  (800) 218-2667 www.tamms.com
d.
L & M Cure R-2 by L & M Construction Chemicals, Omaha, NE  (800) 362-3331  www.lmcc.com
e.
1200 White by W. R. Meadows, Elgin, IL  (847) 683-4500 www.wrmeadows.com
f.
Equal as approved by Architect before use.  See Section 01600.

PART 3 EXECUTION  -  Not Used
Installation

END OF SECTION

557-1804
1
Section 03390

Welfare Services Center
October 11, 2000
Concrete Curing


