STANDARD
7 Mar 2000
06110
UPDATES  -

31 Jan 00
-
Modified requirements for multiple member beams and columns.

16 Dec 98
-
Modified lumber grade requirements for treated sill plates.

6 May 98
-
Added requirements for sill sealers.



SECTION  06110


WOOD FRAMING
PART 1 GENERAL
Edit Article ‘1.1' as necessary to give an accurate, but brief description of the work of this Section, especially if the scope of the work is not shown graphically on the Drawings.

 1.1
SUMMARY
A.
Includes But Not Limited To

1. Furnish and install wood framing and blocking as described in Contract Documents including following:  

a. Wood blocking and nailers for roof coping and fascia.  

b. Wood blocking for supporting wall mounted equipment.

B.
Related Sections

1. Section 07631 – Roof Flashing 

2. Section 10811 – Commercial Toilet Accessories 

 1.2
DELIVERY, STORAGE, AND HANDLING
Delivery
A.
Protect lumber and plywood and keep under cover in transit and at job site.

B.
Do not deliver material unduly long before it is required.

C.
Store lumber and plywood on level racks and keep free of ground to avoid warping.  Stack to insure proper ventilation and drainage.

Delete Paragraph ‘D’ if no trusses used on Project.

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Dimension Lumber

1.
Meet requirements of PS 20-70 and National Grading Rules for softwood dimension lumber.

2.
Bear grade stamp of WWPA, SPIB, or other association recognized by American Lumber Standards Committee identifying species of lumber by grade mark or by Certificate of Inspection.

3.
Lumber 2 inches or less in nominal thickness shall not exceed 19 % in moisture content at time of fabrication and installation and be stamped 'S-DRY', 'K-D', or 'MC15'.

4.
Lumber shall be S4S. 

B.
Lumber Ledgers  -  No. 1 Douglas Fir, Larch, or Southern Pine.

Backblocking for gypsum wallboard is only required where single layer Type ‘C’ gypsum wallboard is installed on trusses or plywood web joists to meet specific fire assembly requirements.  Delete reference to gypsum board back blocking if no Type ‘C’ gypsum board used.

C. Pressure Treating of Wood 


1.
Tread lumber to be in contact with concrete or masonry, or specified above for pressure treatment, in accordance with LP 2-80 and dry after treatment.  

a. Lumber grade and species shall be as specified for he particular use.  

b. Identity treated lumber as to name of treated, preservative used, and retention in lbs/cu ft.  

c. Season after treatment to moisture content required for nontreated material.  

D. Fasteners and Adhesives

1.
Wood screws, expansion bolts – standard type and make for job requirements  

2. Bolts – as specified in Section 05051.  

3. Construction Mastics – meet requirements of American Plywood Association Specification AFG-01 September 1974.  Use Phenol Resorcinol type for use on pressure treated wood products.  

4. Nails – 16d common, unless specifically specified otherwise in contract documents.  

5. Power Actuated Fasteners – Hilti or ITW Ramset 

PART 3 EXECUTION 

3.1 ERECTION 

A. General 

1. Wood in contact with concrete or masonry – 

a. Use pressure treated wood.

b. Set true and level to provide full bearing.  Use mortar as specified in Division 04 for leveling if leveling is required.  

2. Secure one manufacturer approved fastener in each hole of framing anchor that bears on framing member.  

3. Installation of bolts – 

a.
Provide bolt heads and nuts bearing on wood with washers.  


END OF SECTION

ADVANCE \d252
B L A N K   P A G E

557-1804 (20020)
3
Section 06110

Orlando Welfare Complex
October 11, 2000
Wood Framing


