STANDARD
1 Aug 1998
07111

UPDATES  -

It is preferred that a dampproofing system be used on all Projects, unless site conditions are such that a more sophisticated system is required.



SECTION  07111


BITUMINOUS DAMPPROOFING
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and apply to exterior foundation walls and top of footings as described in Contract Documents.

 1.2
DELIVERY, STORAGE, AND HANDLING
Delivery
A.
Store dampproofing at 40 deg F or above prior to application.

 1.3
PROJECT CONDITIONS
A.
Project Environmental Requirements  -  Do not apply when ambient temperature is below 40 deg F, surface temperature is below 33 deg F,  or when rain is expected before applied dampproofing will dry.

  1.4
SCHEDULING
A.
Do not backfill against bituminous dampproofing for 24 hours after application.

PART 2 PRODUCTS
 2.1
MATERIALS
Edit the list of approved manufacturers to include only those with whom you are familiar and whose products are available in the Project area.  You may add any manufacturers whose products you determine meet the specification and Project requirements.

A.
Acceptable Products And Manufacturers
Approved Products
1.
Hydrocide 700B by Sonneborn Building Products, Shakopee, MN  (800) 496-6067  www.chemrex.com
2.
Karnak 100 by Karnak Chemical Corp, Clark, NJ  (800) 526-4236 www.karnakcorp.com
3.
Sealmastic Asphalt Emulsion Dampproofing Type I by W R Meadows, Elgin, IL  (847) 683-4500  www.wrmeadows.com
4.
Ecomul-11 by Epro Inc, Westerville, OH  (800) 8821896  

5.
Mulseal by Koch Materials Co, Heath, OH  (800) 443-2244  www.tuff-n-dri.com
6.
Equal as approved by Architect before bidding.  See Section 01600.

PART 3 EXECUTION

 3.1
APPLICATION
Installation
A.
Spray Application  -  Spray to a thickness of 10 mils minimum.

B.
Brush / Roller Application  -  Apply two coats of dampproofing at rate recommended by Manufacturer.  Apply coats in cross hatch method so coats are applied perpendicular to each other.  Before applying second coat allow first coat to dry in accordance with Manufacturer’s recommendations.

C.
Apply dampproofing to cover area from finish grade line down to and including top of footings.


END OF SECTION

557-1804 (20020)
1
Section 07111

Orlando Welfare Complex
October 11, 2000
Bituminous Dampproofing


