SUPPLEMENTARY
7 Mar 2000
07190sup

UPDATES  -

14 Jul 98
-
Added Dayton Superior siloxane product.



SECTION  07190


WATER REPELLANTS
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and apply water repellent system to exposed exterior masonry as described in Contract Documents.

B.
Related Sections

1.
Division 04  -  Masonry
04813 04814 04815 04930
 1.2
SUBMITTALS
A.
Product Data  -  Manufacturer's product data including data substantiating that materials specified are recommended by Manufacturer for applications shown.
Product Data
B.
Quality Assurance / Control  -  Manufacturer's printed installation instructions.
Quality
 1.3
QUALITY ASSURANCE
A.
Qualifications  -  Installer shall be acceptable to Manufacturer as applicator of its product.

B.
Regulatory Requirements  -  Comply with applicable VOC standards and other local requirements.

C.
Pre-Installation Conference  -  Schedule pre-installation conference for same time as application of test application.
Pre-installation
 1.4
PROJECT CONDITIONS
A.
Project Environmental Requirements

1.
Temperatures at time of application  -

a.
Silane  -   Between 40 and 75 deg F.

b.
Siloxane  -   Between 40 and 100 deg F.

2.
No precipitation shall have occurred within 24 hours of application nor expected for 3 hours minimum after completion of application.

PART 2 PRODUCTS
 2.1
MATERIALS
Edit the list of approved manufacturers to include only those with whom you are familiar and whose products are available in the Project area.  Do not add any manufacturers or change the systems specified without written prior approval of A & E Services.

A.
Approved Products And Manufacturers
Approved Products
Although both types of repellant can be bid together and perform equally well over most surfaces, silane requires moderate installation temperatures and must be applied on materials which are alkaline, generally mortar, CMU, or concrete.  Silane penetrates deeper and protects somewhat longer.  Siloxane keeps the water beaded up on the surface better but does not penetrate into the substrate as well.

1.
Silane  -

a.
Weather Worker S-20 (J-28) by Dayton Superior Corp, Oregon, IL  (800) 745-3707  www.daytonrichmond.com
b.
Hydrozo Enviroseal 20 by Hydrozo - Harris Specialty Chemicals, Jacksonville, FL  (800) 322-7825 www.hsc-ss.com
c.
Rainstopper 120 by TexCote - Textured Coatings of America, Fort Lauderdale, FL  (305) 581-0771  www.texcote.com
2.
Siloxane  -

a.
Weather Worker WB (J-26-WB) by Dayton Superior Corp, Oregon, IL  (800) 745-3707  www.daytonrichmond.com
b.
Sure Klean Weather Seal Siloxane WB Concentrate by ProSoCo, Kansas City, KS  (800) 255-4255  www.prosoco.com
c.
Thorosiloxane 85 System by Thoro - Harris Specialty Chemicals, Jacksonville, FL  (800) 322-7825  www.hsc-ss.com
d.
Rainstopper 600 by TexCote - Textured Coatings of America, Fort Lauderdale, FL  (305) 581-0771  www.texcote.com
PART 3 EXECUTION
 3.1
EXAMINATION
A.
Test substate for moisture content.  Do not apply if moisture contents of wall not within limits acceptable to Manufacturer.

B.
Apply 10 foot by 10 foot test application for review of substrate preparation procedures and application methods.

 3.2
PREPARATION
A.
Do not apply water repellent until after installation of sealants in areas to receive water repellants and adjoining areas.

B.
Clean substrate of substances which will interfere with penetration and adhesion of water repellent.

C.
Protect adjoining work from spillage or blow-over as recommended by Manufacturer.

 3.3
APPLICATION
Installation
A.
Apply two heavy saturation spray coats beginning at bottom of walls and following Manufacturer's written application instructions.

 3.4
CLEANING
A.
Immediately clean adjoining surfaces of spillage and overspray as recommended by Manufacturer.


END OF SECTION

557-1804 (20020)
2
Section 07190

Orlando Welfare Complex
October 11, 2000
Water Repellents


