OPTIONAL
28 Jul 1999    
07242opt
UPDATES  -

This system is standard with the Heritage 98 SOUTHWEST Style Option

If this system is used and gypsum board sheathing, as specified in Section 09251, is required for fire rating purposes, show the gypsum board sheathing installed over the panel product structural sheathing.  The panel product sheathing is not to be deleted from a standard plan under any circumstances.



SECTION  07242


POLYMER BASED EIFS
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and install PB EIFS as described in Contract Documents including sealants.

B.
Related Sections

1.
Division 09  -  Gypsum Sheathing
09251
 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM C 578-95, 'Standard Specification for Rigid, Cellular Polystyrene Thermal Insulation'

 1.3
SUBMITTALS
A.
Product Data
Product Data
1.
Manufacturer's literature

2.
Maintenance, cleaning, and repair instructions

3.
Color selection

B.
Shop Drawings  -  Show EIFS Manufacturer's details and recommended sealant application.
Shop Drawings
C.
Samples  -  Field created sample of each color and texture to be used.  Make sample with same tools and techniques to be used on Project.
Samples
D.
Quality Assurance / Control  -  Letter from EIFS Manufacturer certifying level of training and experience of Installer.
Quality
 1.4
QUALITY ASSURANCE
A.
Qualifications  -  Installer shall have performed at least three installations of similar size, scope, and complexity in each of the past two years and be approved by EIFS Manufacturer.

B.
Regulatory Requirements  -  System shall be recognized for intended use by applicable building codes.

 1.5
DELIVERY, STORAGE, AND HANDLING
Delivery
A.
Materials shall be delivered in original, unopened packages with labels intact.

B.
Store in cool, dry location, out of direct sunlight and weather, and at temperatures above 40 deg F.

 1.6
PROJECT CONDITIONS
A.
Project Environmental Requirements  -  Ambient air temperature shall be 40 deg F minimum and rising at time of installation and remain at 40 deg F or above for 24 hours minimum after application.

 1.7
WARRANTY
Warranty
A.
Manufacturer's five year guarantee that system shall be free from defects which will affect its weather resistance.

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Insulation Board Adhesive  -  Standard of EIFS Manufacturer.

B.
Insulation Board  -  Meet requirements of ASTM C 578, nominal 1 pcf aged expanded polystyrene by EIFS Manufacturer.

C.
Mechanical Fasteners

1.
Masonry  -  Type M expansion fastener with 1-1/2 inch diameter washer and one inch minimum penetration into masonry.

2.
Steel Framing, 20 ga And Thinner  -  Type S self-tapping bugle head screws with 1-1/2 inch diameter washer and 5/8 inch minimum penetration into framing.

3.
Steel Framing, Thicker Than 20 Ga  -  Type S-12 self-tapping bugle head screws with 1-1/2 inch diameter washer and 5/8 inch minimum penetration into framing.

4.
Wood Framing  -  Type W bugle head screws with 1-1/2 inch diameter washer and 5/8 inch minimum penetration into framing.

D.
Standard Reinforcing Mesh  -  A balanced, open weave treated glass fiber mesh by EIFS Manufacturer, 4 oz per sq yd minimum weight.

E.
High Strength Reinforcing Mesh  -  Same as standard mesh except made for high impact areas, 20 oz per sq yd minimum.

F.
Base Coat  -  Manufacturer’s standard.

G.
Finish Coat  - 100 percent acrylic, factory-mixed, elastomeric, flexible coating with integral color and texture.

H.
Sealants  -  As recommended by EIFS Manufacturer.

I.
Water  -  Clean, drinkable.

 2.2
APPROVED MANUFACTURERS
Approved Products
Edit the list of approved manufacturers to include only those with whom you are familiar and whose products are available in the Project area.  Do not add or approve any other manufacturers or systems without approval of Architectural & Engineering Services.

A.
Dryvit, West Warwick, RI  (800) 556-7752  www.dryvit.com
B.
Finestone Division of Simplex Products, Adrian, MI  (800) 545-6555  www.simplex-products.com
C.
Parex, Redan, GA  (800) 537-2739  www.parex.com
D.
Pleko, Tacoma, WA  (206) 473-5138  www.pleko.com
E.
Retro Wall - Soft Coat PB by RETRO TEK, Madison, WI  (800) 225-9001  

F.
Senergy Inc, Cranston, RI  (800) 221-9255  www.senergyeifs.com
G.
Sto Finish Systems Div, Atlanta, GA  (800) 221-2397  www.stocorp.com
PART 3 EXECUTION
 3.1
INSPECTION
A.
Prior to application, inspect substrate for compliance with Contract Documents and with EIFS Manufacturer's printed requirements.

 3.2
INSTALLATION
Installation
A.
Insulation Board

1.
Apply insulation board in running bond pattern with joints staggered in relation to substrate joints and staggered and interlocked at corners.

2.
Attach board to substrate with mechanical fasteners in addition to adhesive required by EIFS Manufacturer.

3.
Sand high spots to create smooth surface.

B.
Base Coat And Reinforcing

1.
Apply base coat to insulation board on fascia, soffits, and wall areas below level of lower eaves.  Embed one layer of high strength mesh with edges abutted and material smoothed out until completely embedded in adhesive.  Allow to cure for 24 hours.

2.
Apply base coat over cured, reinforced base coat and remaining exposed insulation board.  Embed one layer of standard reinforcing mesh overlapping edges 2-1/2 inches minimum.  Smooth out material until completely embedded and allow to cure for 24 hours.

C.
Finish Coat

1.
Correct surface irregularities, such as trowel marks and board lines.

2.
Apply finish coat with stainless steel trowel using sufficient manpower and equipment to insure continuous wet edge to prevent cold joint, scaffolding lines, etc.  Same type of equipment and techniques shall be used by all applicators.  Finish shall closely match samples prepared for Architect.

D.
Apply sealants as required by EIFS Manufacturer.

 3.3
CLEANING
A.
Remove debris resulting from work of this Section and clean adjacent surfaces.


END OF SECTION

ADVANCE \d252
B L A N K   P A G E

20020
1
Section 07242

MeetingHouse
May 22, 2000
Polymer Based EIFS

