STANDARD
1 Aug 1998
07621

UPDATES  -

This Section specifies miscellaneous steel flashing.  Generally, this type of flashing is preferred, but the Architect may specify either steel or aluminum at his option.  If both steel and aluminum flashings are used, the SUMMARY Articles of Sections 07621 and 07622 should be carefully edited to indicate where each type of flashing is to be used.



SECTION  07621


GALVANIZED STEEL FLASHING AND COUNTERFLASHING
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and install flashing, counterflashing, and hold-down clips as described in Contract Documents and not specified to be of other material.

Delete paragraph ‘2' if refrigerant lines enter directly through building wall.

 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM A 361-94, 'Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) by the Hot-Dip Process for Roofing and Siding'

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Sheet Metal

1.
Galvanized iron or steel meeting requirements of ASTM A 361, G 90.

Edit paragraph ‘a’ to fit Project requirements.

a. 22 ga for hold-down clips.

b.
24 ga for all other.

2.
Finish  -

a.
Metal exposed to view shall have face coating of polyvinyledene Fluoride (PVF2) Resin-base finish (Kynar 500 or Hylar 5000) containing 70 percent minimum PVF2 in resin portion of formula.  Thermo-cured two coat system consisting of corrosion inhibiting epoxy or acrylic latex primer and top coat factory applied over properly pre-treated metal.  Reverse side coating shall be thermo-cured system consisting of corrosion inhibiting epoxy or acrylic latex primer applied over properly pre-treated metal.

b.
Color as selected by Architect from Manufacturer's standard colors.

B.
Screws, Bolts, Nails, And Accessory Fasteners  -  Of strength and type consistent with function.

 2.2
FABRICATION
A.
Form accurately to details.

B.
Profiles, bends, and intersections shall be even and true to line.

C.
Fold exposed edges 1/2 inch to provide stiffness

PART 3 EXECUTION
 3.1
INSTALLATION
Installation
A.
Install with small, watertight seams.

B.
Slope to provide positive drainage.

C.
Provide sufficient hold down clips to insure true alignment and security against wind.

D.
Provide 4 inch minimum overlap.

E.
Allow sufficient tolerance for expansion and contraction.

F.
Insulate work to prevent electrolytic action.

 3.2
CLEANING
A.
Leave metals clean and free of defects, stains, and damaged finish.


END OF SECTION

557-1804 (20020)
1
Section 07621

Orlando Welfare Complex
October 11, 2000
Galv. Steel Flashing And Counterflashing


