OPTIONAL
1 Aug 1998
07631opt
 UPDATES  -

This Section is intended for use with Section 07322opt concrete roof tile used with the SOUTHWEST Style Option.



SECTION  07631


ROOF FLASHING
PART 1 GENERAL
 1.1
SUMMARY
A.
Products Supplied But Not Installed Under This Section

1.
Roof flashing

B.
Related Sections

1.
Section 07322  -  Installation
07322opt 07322sup
 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM A 361-94, 'Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) by the Hot-Dip Process for Roofing and Siding'

2.
ASTM B 101-96, 'Standard Specification for Lead-Coated Copper Sheet and Strips for Building Construction'

PART 2 PRODUCTS
 2.1
MATERIALS
A.
2 lb Per Sq Ft Sheet Lead

1.
Pipe jacks

2.
Flashing and counterflashing which contours to tile profile.

3.
Trim terminations, trim junctions, and eave offsets.

B.
16 oz Lead-Coated Copper meeting requirements of ASTM B 101, Grade I or II, or 26 ga AISI Type 304 Stainless Steel with No. 1 or 2D finish

1.
Metal Valleys  -  10 foot maximum length, with 8 inch overlap.

C.
24 Ga Hot-Dipped, Galvanized Steel or 0.053 Inch Hard Anodized Aluminum -

(Base metal to match that used for fascias)

1
Trough metal on flared gables.

2.
Hold-down clips and miscellaneous (aluminum need not be anodized where concealed).

D.
28 ga Minimum Hot-Dipped, Galvanized Steel meeting requirements of ASTM A 361.

1.
Valley Flashing  -  8 inch wide, 6 inch end lapped.

E.
Metallic Coated Bitumen

1.
At Hips And Ridges  -  Over field tile and under hip and ridge tiles, 9 inches wide minimum.

2.
At Wall To Roof Transition  -  Under counterflashing and over ends of field tile.

3.
Ridge vent to roof transition.

4.
Approved Manufacturers -
Approved Products
a.
Tile Flash by Protecto Wrap, Denver, CO  (800) 759-9727 www.protectowrap.com
b.
Flashband by 3E Corporation, Moorestown, NJ  (609) 866-7600

c.
Hardcast AFT-701 by Carlisle Coatings & Waterproofing Inc, Wylie, TX  (800) 527-7092  www.carlisle-ccw.com
F.
Pipe Flashing For Plumbing Vent Lines

1.
Flash pipes passing through roof with 16 oz sheet copper flashing fitted snugly around pipes or with 4 lb per sq ft lead flashing fitted around pipes and turned down into pipe 1/2 inch with turned edge hammered against pipe wall.  Calk between copper flashing and pipe with flexible waterproof compound.

2.
Flashing base shall be at least 24 inches square.

G.
Roof Jacks For Flues And Furnace Piping  -  Factory-made galvanized steel.

H.
Nails  -  10d Hot-Dipped galvanized unless shown differently.  Use nails of aluminum or copper with aluminum or copper sheet metal, respectively.

 2.2
FABRICATION
A.
Form accurately to details.

B.
Profiles, bends, and intersections shall be even and true to line.

PART 3 EXECUTION  -  Not Used
Installation

END OF SECTION

Project Number
1
Section 07631

Project Name
Project Date
Roof Flashing


