
SUPPLEMENTARY
1 Aug 1998
07631sup
UPDATES  -

This Section is intended for use with membrane roofing systems.  Any other metal flashing required for such roofing systems should be included in this Section.  Coordinate with roofing system manufacturer’s warranty requirements.



SECTION  07631


ROOF FLASHING

PART 1 GENERAL
Edit Article ‘1.1' as necessary to give an accurate, but brief description of the work of this Section and accurate listing of related work, especially if the scope of the work is not shown graphically on the Drawings.

 1.1
SUMMARY
A.
Products Supplied But Not Installed Under This Section

1.
Gravel stops, roof edge strips, and scuppers not specified to be of other materials.

B.
Related Sections

Edit to indicate the Section number of the exact roofing system to be used.

1.
Section 075??  -  Installation

 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM A 361-94, 'Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) by the Hot-Dip Process for Roofing and Siding'

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Sheet Metal

1.
24 ga galvanized steel.  Meet requirements of ASTM A 361, for 1.25 oz commercial.

2.
Finish  -

a.
Metal exposed to view shall have face coating of polyvinyledene Fluoride (PVF2) Resin-base finish (Kynar 500 or Hylar 5000) containing 70 percent  minimum PVF2 in resin portion of formula.  Thermo-cured two coat system consisting of corrosion inhibiting epoxy or acrylic latex primer and top coat factory applied over properly pre-treated metal.  Reverse side coating shall be thermo-cured system consisting of corrosion inhibiting epoxy or acrylic latex primer applied over properly pre-treated metal.

b.
Color as selected by Architect from Manufacturer's standard colors.

B.
Sealants  -  Rubber base type conforming to Fed Spec TC‑S‑00230.

C.
Nails And Other Fasteners  -  Hot-dipped galvanized of strength and type consistent with function.

 2.2
FABRICATION
A.
Form accurately to details.

B.
Profiles, bends, and intersections shall be even and true to line.

PART 3 EXECUTION  -  Not Used
Installation

END OF SECTION

557-1804 (20020)
2
Section 07631

Welfare Services Center

Roof Flashing


