
STANDARD
19 Nov 1999
07631
UPDATES  -

19 Nov
-
Added Metal Sales Mfg Corp.

3 Mar 99
-
Moved drip edges from 07634 to this Section.  Deleted requirement for valley flashing.  Changed metal to kynar coated aluminum or steel.

This Section is intended for use with asphalt shingles specified in Section 07312.  Flashing for metal shingles specified in Section 07313 is included with the shingle system, and flashing for concrete roof tile is specified in Section 07634opt.



SECTION  07632


ROOF SCUPPERS
PART 1 GENERAL
Edit Article ‘1.1' as necessary to give an accurate, but brief description of the work of this Section and accurate listing of related work, especially if the scope of the work is not shown graphically on the Drawings.

 1.1
SUMMARY
A.
Products Supplied But Not Installed Under This Section

1.
scuppers not specified to be of other materials.  

 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM A 361-94, 'Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) by the Hot-Dip Process for Roofing and Siding'

 1.3
SUBMITTALS
A.
Sample  -  12 inch square sample of valley metal with product data.
Samples
PART 2 PRODUCTS
 2.1 MATERIALS
A.
Formed Valley Metal And Drip Edge

Select one of the following metal options

1.
Metal  -

a.
Aluminum  -  0.032 inch thick minimum

a.
Steel  -  Minimum 24 ga, hot-dipped galvanized to meet requirements of ASTM A 361, 1.25 oz/sq ft.

2.
Finishes  -

a.
Face coating polyvinyledene Fluoride (PVF2) Resin-base finish (Kynar 500 or Hylar 5000) for coil coating components containing 70 percent minimum PVF2 in resin portion of formula.  Thermo-cured two coat system consisting of corrosion inhibiting epoxy or acrylic latex primer and top coat factory applied over properly pre-treated metal.

b.
Reverse side coating of steel flashings to be thermo-cured system consisting of corrosion inhibiting epoxy or acrylic latex primer applied over properly pre-treated metal.

c.
Color as selected by Architect from Manufacturer's standard colors.

Edit the list of acceptable manufacturers to include only those with whom you are familiar and whose products are available in the Project area.  You may use any manufacturers whose products meet the specification requirements.

3.
Acceptable Manufacturers  -
Approved Products
a.
Copper Sales Inc, Minneapolis, MN  (800) 426-7737  www.unaclad.com
b.
Englert Inc, Perth Amboy, NJ  (800) 610-1975  www.englertinc.com
c.
Metal Sales Manufacturing Corp, Sellersburg, IN  (800) 999-7777 www.mtlsales.com
d.
Peterson Aluminum Corp, Elk Grove, IL  (800) 323-1960   ww.pac‑clad.com
 


e.
Reynolds Metals Company, Richmond, VA  (800) 841-7774  www.rmc.com
f.
Vincent Metals, Minneapolis, MN  (800) 328-7800  www.vincentmetalgoods.com
g.
Equal as approved by Architect before installation.  See Section 01600.

B.
Pipe Flashing For Plumbing Vent Lines

1.
16 oz sheet copper or 4 lb per sq ft lead flashing.

2.
Flashing base shall be at least 24 inches square.

C.
Roof Jacks For Flues And Furnace Piping  -  Factory-made galvanized steel.

 2.2
FABRICATION
A.
Form accurately to details.  Provide formed valley metal in 10 foot lengths with one inch ‘V’ crimp and break in center to match roof slopes.

B.
Profiles, bends, and intersections shall be even and true to line.

PART 3 EXECUTION
 3.1
INSTALLATION
Installation
A.
Interface With Other Work  -  Coordinate with pipe installers for proper size of roof jacks and pipe flashing.

B.
Pipe Flashing For Plumbing Vent Lines

1.
Copper  -  Fit snugly around pipes.  Calk between copper flashing and pipe with specified sealant.

2.
Lead  -   Fit around pipes and turn down into pipe 1/2 inch with turned edge hammered against pipe wall.


END OF SECTION

557-1804 (20020)
1
Section 07631

Orlando Welfare Complex

Roof Scuppers

