OPTIONAL
25 Jan 2000
07634opt.b
UPDATES  -

25 Aug 98
-
Added Englert Inc.

This Section specifies non-perforated soffits with the panels generally running parallel with the building.  It is generally used where a strip soffit vent is detailed.  If this system is used, check the soffit details on the Storage Building for the type of soffit to be used there.



SECTION  07634


METAL SOFFITS
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and install metal soffit as described in Contract Documents.

 1.2
SUBMITTALS
A.
Quality Assurance / Control  -  Manufacturer's published installation instructions.
Quality
 1.3
WARRANTY
Warranty
A.
Manufacturer's written 20 year guarantee for finish.

PART 2 PRODUCTS
 2.1
COMPONENTS
A.
Soffits

1.
Panels  -

a.
0.032 inch thick minimum aluminum, flush panel design, width of panels as selected by Architect from Manufacturer’s standard panels.

b.
Panels shall be interlocked full length of panel.

2.
Finish  -

a.
Polyvinyledene Fluoride (PVF2) Resin-base (Kynar 500 or Hylar 5000) finish for coil coating components containing 70 percent minimum PVF2 in resin portion of formula.  Thermo cured two coat system consisting of corrosion inhibiting epoxy or acrylic latex primer and top coat factory applied over properly pretreated metal.

b.
Color as selected by Architect from Manufacturer's standard colors.

Edit list of acceptable manufacturers to include only those with whom you are familiar and whose products are available in Project area.  You may add any manufacturers whose products you determine meet specification and Project requirements.

3.
Acceptable Manufacturers  -
Approved Products
a.
AEP / Span, Dallas, TX  (800) 527-2503  www.aep-span.com
b.
ATAS Aluminum Products, Allentown, PA  (800) 468-1441 www.atas.com
c.
Copper Sales Inc, Anoka, MN  (800) 426-7737  www.unaclad.com
d.
Englert Inc, Perth Amboy, NJ  (800) 610-1975  www.englertinc.com
e.
Fashion Inc, Ottawa, KS  (800) 255-1009  www.fashioninc.com
f.
Peterson Aluminum Corp, Elk Grove, IL  (800) 323-1960   ww.pac‑clad.com
g.
Reynolds Metals Company, Richmond, VA  (800) 841-7774  www.rmc.com
h.
Vincent Metals, Minneapolis, MN  (800) 328-7800  www.vincentmetalgoods.com
i.
Equal as approved by Architect prior to bidding.  See Section 01600.

B.
Continuous Soffit Vent

Edit list of acceptable manufacturers to include only those with whom you are familiar and whose products are available in Project area.  You may add any manufacturers whose products you determine meet specification and Project requirements.

1.
Acceptable Manufacturers  -

a.
Vent-A-Strip by Alcoa Building Products, Sydney, OH  (800) 962-6973 www.alcoahome.com
b.
Soffit Louver Strips by The Solar Group, Taylorsville, MS  (800) 647-7063  www.thesolargroup.com
c.
Equal as approved by Architect before installation.  See Section 01600.

C.
Fastening Devices  -  1-1/2 inch cadmium or zinc plated ring shanked nails.

PART 3 EXECUTION
 3.1
INSTALLATION
Installation
A.
Conceal fasteners where possible.  Paint heads of exposed fasteners to match background.

B.
Isolate from dissimilar metals to prevent electrolytic action.

C.
Repair buckling or bowing due to improper installation at no additional cost to Owner.


END OF SECTION

20020
1
Section 07634

MeetingHouse
May 22, 2000
Metal Soffits


