OPTIONAL
19 Jul 1999
08211opt
UPDATES  -

19 Jul 99
-
Deleted Total Openings Systems as a VMR partner

12 Oct 98
-
Updated VMR contact information

It is generally preferred that factory-finished doors be used.  This Section would be used for addition / remodel Projects where existing doors are to be matched.

This Section should be also be used for opaque finished doors, such as in the attic of the Legacy 96.



SECTION  08211


FIELD-FINISHED FLUSH WOOD DOORS
PART 1 GENERAL
 1.1
SUMMARY
A.
Products Supplied But Not Installed Under This Section

1.
Flush wood doors

Door lites are not recommended or generally authorized, except in doors to nursery rooms.  However, if lites are required, it is preferred that they come installed from the door manufacturer.  The appropriate requirements and modifications to the Section should be made.

Edit Paragraph ‘B’ to fit the Project requirements.

B.
Related Sections

1.
Division 06  -

a.
Installation
06202
2.
Division 09  -  Finishing of doors
09925 09936ar.a 09936ar.b
 1.2
SUBMITTALS
A.
Product Data
Product Data
1.
Manufacturer's product literature.

2.
Maintenance and repair instructions.

B.
Shop Drawings  -  Schedule showing type of door at each location.  Included shall be size, veneer, core type, fire rating, hardware prep, openings, blocking, etc.
Shop Drawings
Delete Paragraph ‘C’ if no mineral core, double doors specified.

 1.3
DELIVERY, STORAGE, AND HANDLING
Delivery
A.
Deliver in clean truck and, in wet weather, under cover.  Deliver to building site after plaster, cement, and taping compound are dry.  At time of delivery of unfinished doors, seal top and bottom rails of doors that are to remain on site in storage longer than seven days before they are installed.

B.
Store doors in a space having controlled temperature and humidity range between 25 and 55 percent.  Store flat on level surface in dry, well ventilated space.  Cover to keep clean but allow air circulation.  Do not subject doors to direct sunlight, abnormal heat, dryness, or humidity.

C.
Handle with clean gloves and do not drag doors across one another or across other surfaces.

 1.4
WARRANTY
Warranty
A.
Manufacturer's standard full door warranty for lifetime of original installation

1.
Warranty shall include finishing, hanging, and installing hardware if manufacturing defect was discovered after door was finished and installed.

2.
Warranty to include defects in materials including following  -

a.
Delamination in any degree.

b.
Warp or twist of 1/4 inch or more in door panel at time of one year warranty inspection.

c.
Telegraphing of core assembly  -  Variation of 1/100 inch or more in a 3 inch span.

PART 2 PRODUCTS
 2.1
MANUFACTURED UNITS
A.
Wood Doors

1.
For Transparent Finish  -

a.
Type  -  AWI PC-5ME or FD-5ME

b.
Grade  -  AWI Premium, except face veneer.

c.
Face Veneer  -

1)
Plain sliced Red Oak meeting requirements of AWI Grade A, 1/50 inch thick minimum immediately prior to finishing.

If other species of veneer are specified to match existing doors or if darker stains are to be used, another type of matching may be necessary.  Darker woods and stains, such as LDS Mahagony, should be slip matched to lessen ‘barber-poling’.

2)
Face veneers shall be running book matched.

d. Fully Type I  -  Adhere all glue lines with Type I adhesive, including veneer lay-up.

Delete paragraph ‘2' if no painted wood doors required.

2
2.
Core  -

a.
Fully bonded to stiles and rails and sanded as a unit prior to applying veneers.

Edit paragraphs 'b' and 'c' to correspond with Project requirements for fire rated doors.

b.
Non‑Rated 

1)
32 lb density meeting requirements of ANSI A 208.1 Mat Formed Wood Particle Board, Grade 1‑L‑1 minimum.

2)
Stiles  -

a)
1-3/8 inches deep minimum before fitting.

b)
3/8 inch minimum of stile face to be hardwood matching face veneer material.

3)
Rails  -

a)
1-1/8 inches

b)
Mill option.

 2.2
APPROVED MANUFACTURERS
Approved Products
No other door manufacturers are acceptable

A.
Buell Door Co, Dallas, TX

B.
Oshkosh Architectural Door Co - Fenestra, Oshkosh, WI

C.
VT Industries, Holstein, IA

D.
Weyerhaeuser, Marshfield, WI

Article ‘2.3' is required for fire-rated doors, optional on other doors.  If any of the doors on a Project are fire-rated, all the doors should be factory-machined.

 2.3
FABRICATION
A.
Doors shall be factory-machined.  Coordinate with Section 08115 and Sections under 08700.

 2.4
SOURCE QUALITY CONTROL
A.
Verification of Performance

1.
Doors shall have following information permanently affixed on top of door  -

a.
Manufacturer

b.
Door designation or model

c.
Veneer species

Paragraph ‘2' applies only if fire-rated doors are used.

PART 3 EXECUTION
 3.1
VMR SUPPLIERS
Approved Products
These are the only suppliers authorized to provide hollow metal, wood doors, and hardware for all LDS Projects including work by FM Groups.  They are available for consultation and document preparation during design.  If the documents are not made available on Dodge / Scan or CMD due to Project size (FM Group work, for example), the VMR Suppliers must be contacted so they can be sent the appropriate documents and information.

A.
Architectural Building Supply, Salt Lake City, UT Russ Farley

Phone (800) 574-4369
FAX 801-484-6817

B.
Beacon Metals Inc, Salt Lake City, UT  Chad Riches

Phone (888) 823-2206
FAX 801-485-7647

C.
Girtman & Associates, Nashville, TN  Lisa Ehrie

Phone (615) 350-6000
FAX 615-350-6686
E-Mail info@girtman.com


END OF SECTION

557-1804 (20020)
2
08211

Orlando Welfare Complex
October 11, 2000
Field-Finished Flush Wood Doors


