SUPPLEMENTARY
1 Aug 1998
09207sup.a
UPDATES  -



SECTION  09207


WOVEN WIRE METAL LATH
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and install woven wire metal lath on exterior surfaces to be plastered as described in Contract Documents.

 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM A 641-98, 'Standard Specifications For Zinc Coated (Galvanized) Carbon Steel Wire'

2.
ASTM C 841-98, 'Standard Specification for Installation of Interior Lathing and Furring'

3.
ASTM C 847-95, 'Standard Specification for Metal Lath'

PART 2 PRODUCTS
 2.1
MATERIAL
A.
Metal Lath

1.
Acceptable Products  -
Approved Products
a.
Galvanized Woven Wire Fabric Lath (Stucco Netting) of 17 gauge wire with 1‑1/2 inch openings meeting requirements of ASTM C 847.

b.
Stucco-Rite by K-Lath, Fonatana, CA  (800) 669-5284  

c.
Equal as approved by Architect before installation.  See Section 01600.

 2.2
ACCESSORIES
A.
Lathing Accessories

1.
Meet requirements of SPR R3-60 and be galvanized after fabrication unless specified differently.

2.
Includes -

a.
Exterior Corner Reinforcement  -  18 gauge.

b.
Casing Beads And Drip Screed  -  24 gauge.

c.
Corner Beads And Base or Parting Screeds  -  26 gauge

d.
Control Joints  -  28 gauge.

e.
Cornerite And Strip Reinforcements  -  2.5 lb metal lath coated with rust-inhibitive paint

f.
Attachment Clips  -  As approved by Lath Manufacturer.

B.
Attaching Devices

1.
Hanger Wire And Tie Wire  -  Meet requirements of ASTM A 641.

2.
Power-driven Staples  -  Formed from galvanized (Type I Coating) steel wire with tensile strength from 80,000 to 110,000 psi and meeting governing codes.

3.
Attachment Clips  -  As approved by Lath Manufacturer.

C.
Building Paper  -  Kraft waterproofed meeting requirements of Fed Spec UU-B-790, Grade D.

 2.3
ACCEPTABLE MANUFACTURERS
Approved Products
A.
Any Manufacturer meeting specification requirements and building codes is approved.

PART 3 EXECUTION
 3.1
INSTALLATION
Installation
A.
Install in accordance with requirements of ASTM C 841.

B.
Secure lath to supports at intervals not to exceed 6 inches on center.  Furr lath out 1/4 inch from substrate.

C.
Laps  -  1/2 inch minimum at sides and one inch minimum at ends.


END OF SECTION

20020
1
Section 09207

MeetingHouse
May 22, 2000
Woven Wire Metal Lath


