SUPPLEMENTARY
1 Aug 1998
09207sup.b
UPDATES  -



SECTION  09207


EXPANDED METAL LATH
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

1.
Furnish and install expanded metal lath on exterior surfaces to be plastered as described in Contract Documents.

 1.2
REFERENCES
Delete or add references based on editing of other parts of this Section.

A.
American Society For Testing And Materials
ASTM
1.
ASTM A 641-98, 'Standard Specification For Zinc Coated (Galvanized) Carbon Steel Wire'

2.
ASTM C 841-98, 'Standard Specification for Installation of Interior Lathing and Furring'

3.
ASTM C 847-95, 'Standard Specification for Metal Lath'

PART 2 PRODUCTS
 2.1
MATERIAL
A.
Metal Lath

1.
Meet requirements of ASTM C 847.

2.
Use 3.4 lb diamond mesh on framing spaced 16 inches on centers.

3.
Use 3/8 inch, 3.5 lb rib lath on framing spaced 24 inches on centers.

4.
Galvanized.

 2.2
ACCESSORIES
A.
Lathing Accessories

1.
Meet requirements of SPR R3-60 and be galvanized after fabrication unless specified differently.

2.
Includes  -

a.
Exterior Corner Reinforcement  -  18 gauge.

b.
Casing Beads and Drip Screed  -  24 gauge.

c.
Corner Beads and Base or Parting Screeds  -  26 gauge

d.
Control Joints  -  28 gauge.

e.
Cornerite and Strip Reinforcements  -  2.5 lb metal lath coated with rust-inhibitive paint

f.
Attachment Clips  -  As approved by Manufacturer.

B.
Attaching Devices

1.
Hanger Wire And Tie Wire  -  Meet requirements of ASTM A 641.

2.
Power-Driven Staples  -  Formed from galvanized (Type I Coating) steel wire with tensile strength from 80,000 to 110,000 psi and meeting governing codes.

3.
Attachment Clips  -  As approved by Manufacturer.

C.
Building Paper  -  Kraft waterproofed meeting requirements of Fed Spec UU-B-790, Grade B.

 2.3
ACCEPTABLE MANUFACTURERS
Approved Products
A.
Any Manufacturer meeting Contract Document requirements and building codes is approved.

PART 3 EXECUTION
 3.1
INSTALLATION
Installation
A.
Install in accordance with requirements of ASTM C 841.

B.
Secure lath to supports at intervals not to exceed 6 inches on center.

1.
Wire  -  Place where sides of sheets lap at supports and at side laps of sheets between supports.

2.
Nails  -  Engage at least two strands of diamond mesh.  Where common nails are used, bend across three strands minimum.

C.
Laps  -  1/2 inch minimum at sides and one inch minimum at ends.  Ends shall occur over supports and be staggered.

D.
Corners

1.
Diamond Mesh  -  Start at least one stud away from corner.  Bend into corner and carry on to abutting wall at least 3 inches.  Otherwise use corner lath.

2.
Rib or Sheet Lath  -  Butt into corner and use corner lath.


END OF SECTION

20020
2
Section 09207

MeetingHouse
May 22, 2000
Expanded Metal Lath


