STANDARD
7 Mar 2000
09250

UPDATES  -

20 Jul 99
-
Changed pre-installation conference requirements.

1 Jun 99
-
Added skim coat and skim coat alternate for smooth and lightly textured walls.

10 May 99
-
Deleted requirement for skim coating.  Changed method of attaching metal corner bead.  Added requirement to rout out gypsum board in some cases.



SECTION  09250


GYPSUM WALLBOARD

PART 1 GENERAL

 1.1
SUMMARY

A.
Includes But Not Limited To

1.
Furnish and install gypsum wallboard as described in Contract Documents, except behind ceramic tile.

2.
Furnish and install acoustical sealants as described in Contract Documents.

Edit Paragraph ‘B’ to fit Project requirements.

B.
Related Sections

1.
Division 06  -  Backblocking of gypsum wallboard joints
06110
2.
Section 09305  -  Backerboard and gypsum board behind ceramic tile
09305
3.
Section 09822  -  Quality of acoustical sealants
09822
 1.2
REFERENCES

Delete or add references based on editing of other parts of this Section.

A.
Gypsum Association

1.
GA-214-90  -  'Recommended Specification: Levels of Gypsum Board Finish'

B.
American Society For Testing And Materials
ASTM
1.
ASTM C 36-97, 'Standard Specification for Gypsum Wallboard'

2.
ASTM C 475-94, 'Standard Specification for Joint Compound and Joint Tape for Finishing Gypsum Board'

3.
ASTM C 840-98, ‘Standard Specification for Application and Finishing of Gypsum Board’

4.
ASTM C 1002-98, 'Standard Specification for Steel Drill Screws for Application of Gypsum Board or Metal Plaster Bases'

 1.3
SUBMITTALS

A.
Quality Control  -  Fire test results or assembly diagrams and numbers confirming products used will provide required fire ratings with installation configurations used.


Quality
  1.4
QUALITY ASSURANCE

A.
Pre-Installation Conference  -  Schedule pre-installation conference immediately prior to installation of gypsum wallboard.  In addition to agenda items specified in Section 01300, review finish requirements necessary for installation of finish materials over gypsum wallboard.
Pre-installation
 1.5
DELIVERY, STORAGE, AND HANDLING
Delivery
A.
Deliver materials in original packages, containers, or bundles bearing brand name, applicable standard designation, and Manufacturer's name.

B.
Store material under roof and keep dry.  Stack gypsum board flat and protect from damage.

 1.6
PROJECT CONDITIONS

A.
Environmental Requirements

1.
Temperature shall be 50 deg F minimum and 95 deg F maximum day and night during entire joint operation and until execution of Certificate of Substantial Completion.

2.
Provide ventilation to eliminate excessive moisture.

3.
Avoid hot air drafts which will cause too rapid drying.

PART 2 PRODUCTS

 2.1
MATERIALS

A.
Gypsum Board

The acceptability of the assembly consisting of one layer of the specified gypsum board attached directly to the specified trusses is covered in ICBO Evaluation Report No. 4431, dated June 1989.  The acceptability of the assembly consisting of one layer of the specified gypsum board attached directly to the specified plywood web joists is covered in SWRI No. 01-4873-003 by Southwest Research Institute, dated Aug 1992.  The acceptability of the assembly consisting of one layer of the specified gypsum board on a Corridor ceiling is covered in SWRI No. 01-4873-005 by Southwest Research Institute, dated Aug 1993.

Type 'C' board should only be specified if at least one of these assemblies is included on the Project and should only be used on those assemblies.

1

1.
For all applications  -  Any manufacturer's product meeting requirements of ASTM C 36, Type X, UL one-hour rated, tapered edge, face paper suitable for painting.

 2.2
ACCESSORIES

A.
Gypsum Wallboard Mounting Accessories

1.
Acceptable Products  -
Approved Products
a.
Furring Channels  -

1)
Walls  -  Galvanized USG DWC-25

2)
Ceilings  -  Galvanized USG DWC-20

b.
Resilient Channels  -  RC-1 by USG

c.
Equal as approved by Architect before installation.  See Section 01600.

B.
Corner And Edge Trim

Use of plastic trim or bull-nosed trim is generally not acceptable.  With approval of the Project Manager, it may be used for decorative applications on ceilings or higher wall areas not subject to damage.

1.
Acceptable Types And Manufacturers  -
Approved Products
a.
Metal  -  24 ga minimum steel, electrolytic galvanized zinc-coated, treated for maximum cement and paint adhesion.  Surfaces to receive bedding cement shall be knurled for maximum bonding.

b.
Paper-Faced Metal  -

1)
Beadex Drywall Accessories, Auburn, WA  (800) 726-2397

2)
Chicago Metallic, Chicago, IL  (800) 323-7164  www.chicago‑metallic.com
3)
Goldline Drywall Trim by Unimast Inc, Schiller Park, IL  (847) 928-3400  www.unimast.com
4)
United States Gypsum Co, Chicago, IL  (800) 874-4968 www.usg.com
5)
Equal as approved by Architect before installation.  See Section 01600.

C.
Joint Compound

1.
Best grade or type recommended by Wallboard Manufacturer and meeting requirements of ASTM C 475.

a.
Use Taping Compound for first coat to embed tape and accessories.

b.
Use Taping Compound or All-Purpose Compound for subsequent coats except final coat.

c.
Use Finishing Compound for final coat and for skim coat.

Do not use fiber-glass mesh reinforcing tape or no-tape reinforcing systems.

D.
Joint Reinforcing  -  Paper reinforcing tape acceptable to Wallboard Manufacturer.

E.
Skim Coat Alternate

1.
Acceptable Products And Manufacturers  -

a.
Sheetrock First Coat by United States Gypsum Company  (800) 874-4968  www.usg.com
b.
Prep Coat Plus by Hamilton Materials Inc, Orange, CA  (714) 637-2770

F.
Fasteners

1.
Bugle head screws meeting requirements of ASTM C 1002.

Edit paragraphs 'a' and 'b' to fit Project circumstances.

a.
Types  -

1)
Type S  -  For fastening gypsum board to steel framing and ceiling suspension members, truss members, and plywood web joists.

b.
Lengths  -

1)
Of length to penetrate steel framing 3/8 inch minimum.

PART 3 EXECUTION

 3.1
INSTALLATION
Installation
Blocking of ends and edges is only necessary for Type 'C' board.

A.
Interface With Other Work  -  Coordinate with Division 06 for location of backblocking for edges and ends of gypsum board and for blocking required for installation of equipment and building specialties.  Do not install gypsum board until required blocking is in place.

B.
General  -  Install and finish as recommended in ASTM C 840 unless specified otherwise in this Section.

C.
Mounting Accessories

1.
Furring Channels  -  Apply with screws through flanges into each framing member.

D.
Gypsum Wallboard

1.
General  -

a.
Install so trim and reinforcing tape are fully backed by gypsum wallboard.  No hollow spaces between pieces of gypsum board over 1/8 inch wide before taping are acceptable.

b.
Rout out backside of gypsum board to accommodate items which extend beyond face of framing, but do not penetrate face of gypsum board, such as metal door frame mounting brackets, etc.

2.
Single Layer Application  -

a.
Apply ceilings first using minimum of two men.

b.
Use board of length to give minimum number of joints.

c.
On walls over 9 feet high and on ceilings, apply board perpendicular to support.

d.
Stagger end joints.  End and edge joints of board applied on ceilings shall occur over framing members or be back blocked with 2x4 blocking.  End joints of board horizontally applied on walls shall occur over framing members.  Edge joints of board vertically applied on walls shall occur over framing members.

e.
Butt edges in moderate contact.  Do not force in place.  Shim to level.

f.
Leave facings true with joint, finishing flush.  Vertical work shall be plumb and ceiling surfaces level.

g.
Scribe work closely.  Keep joints as far from openings as possible.  if joints occur near an opening, apply wallboard so vertical joints are centered over openings.  No vertical joints shall occur within 8 inches of external corners or openings.

h.
Install board tight against support with joints even and true.  Tighten loose screws.

i.
Calk perimeter joints in sound insulated rooms with specified acoustical sealant.

3.
Double Layer Application  -

a.
Apply base layer as specified for single layer application, except edge joints need not occur over framing members or be back blocked.

b.
Apply face layer with joints staggered in relationship to base and occurring over supports.  Use combination of adhesive and screws to meet Manufacturer's specifications for fire-rated assembly.  Apply screws attaching face layer through base layer into support for specified penetration.

4.
Fastening  -

a.
Apply from center of wallboard towards ends and edges.

b.
Apply screws 3/8 inch minimum from ends and edges, one inch maximum from edges, and 1/2 inch maximum from ends.

c.
Spacing  -

1)
Ends  -  Screws not over 7 inches on center at edges where blocking or framing occurs.

2)
Metal Framed Walls  -  Screws 12 inches on center in panel field.

d.
Set screw heads 1/32 inch below plane of board, but do not break face paper.  If face is accidentally broken, apply additional screw 2 inches away.

f.
Screws on adjacent ends or edges shall be opposite each other.

g.
Drive screws with shank perpendicular to face of board.

E.
Trim

1.
Corner Beads  -

a.
Attach metal or paper faced metal corner beads to outside corners.

1)
Attach metal corner bead with staples spaced 4 inches on center maximum and flat taped over edges of corner bead.  Also, apply screw through edge of corner bead where wood trim will overlay corner bead.

2)
Set paper-faced trim in solid bed of taping compound.

Edit paragraph ‘2' to fit Project circumstances. 

2.
Edge Trim  -  Apply where gypsum board abuts dissimilar material in accordance with Manufacturer's instructions.  Hold channel and 'L' trim back from exterior metal window and door frames 1/8 inch to allow for calking.

F.
Finishing

1.
General  -

a.
Tape and finish joints and corners as specified below to correspond with final finish material to be applied to gypsum board.   When sanding, do not raise nap of gypsum board face paper or paper-faced trim.

b.
First Coat  -

1)
Apply tape over center of joint in complete, uniform bed of specified taping compound.  If metal corner bead is used, apply reinforcing tape over flange of metal corner bead and trim so half of tape width is on flange and half is on gypsum wallboard.

2)
Completely fill gouges, dents, and fastener dimples.

3)
Allow to dry and sand lightly if necessary to eliminate high spots or excessive compound.

c.
Second Coat  -

1)
Apply coat of specified joint compound over embedded tape extending 3-1/2 inches on both sides of joint center.  Use finishing compound only if applied coat is intended as final coat.

2)
Re-coat gouges, dents, and fastener dimples.

3)
Allow to dry and sand lightly to eliminate high spots or excessive compound.

d.
Third Coat  -  Apply same as second coat except extend application 6 inches on both sides of joint center.  Allow to dry and sand with fine sandpaper or wipe with damp sponge.

e.
Fourth Coat  -  Apply same as second coat except extend application 9 inches on both sides of joint center.  Allow to dry and sand with fine sandpaper or wipe with damp sponge.

2.
Finishing Levels  -

In all ceilings, but on Addition / Renovation Projects particularly, it is critical that the ceiling be smooth before applying ceiling tile.  The joints in the drywall must be taped as specified in Section 09250.  On existing ceilings where existing tile has been removed or other damage to the existing ceiling has occured, it may be necessary to specify a layer of drywall over the existing ceiling or to specify floating out the ceiling so it will be smooth enough to accept ceiling tile.

a.
Unfinished Gypsum Board Surfaces And Under Acoustical Tile  -

1)
GA-214-90 Level Two  -  'All joints and interior angles shall have tape embedded in joint compound and one separate coat of joint compound applied over all joints, angles, fastener heads, and accessories.  Surface shall be free of excess joint compound.  Tool marks and ridges are acceptable,' except under acoustic tile.

b.
Gypsum Board Surfaces in Mechanical, Storage, And Utility Areas to Receive Paint, and Surfaces to Receive Sisal Wall Covering  -

1)
GA-214-90 Level Three  -  'All joints and interior angles shall have tape embedded in joint compound and two separate coats of joint compound applied over all joints, angles, fastener heads, and accessories.  All joint compound shall be smooth and free of tool marks and ridges.'

c.
Gypsum Board Surfaces to Receive Vinyl Wall Covering, Multi-Color Coating System, and Painted Heavy Texturing, Except in Mechanical, Storage, And Utility Areas  -

1)
GA-214-90 Level Four  -  'All joints and interior angles shall have tape embedded in joint compound and three separate coats of joint compound applied over all joints, angles, fastener heads, and accessories.  All joint compound shall be smooth and free of tool marks and ridges.'

d.
Painted Smooth and Lightly Textured Gypsum Board Surfaces, Except in Mechanical, Storage, And Utility Areas  -

1)
GA-214-90 Level Five  -  ‘All joints and interior angles shall have tape embedded in joint compound and three separate coats of joint compound applied over all joints, angles, fastener heads, and accessories.  A thin skim coat of finishing compound, or a specified skim coat alternate, shall be applied to the entire surface.  Surface shall be smooth and free of tool marks and ridges.’

 3.2
CLEANING

A.
Remove from site debris resulting from work of this Section including taping compound spills.


END OF SECTION

557-1804 (20020)
5
Section 09250

Orlando Welfare Complex
October 11, 2000
Gypsum Wallboard


