STANDARD
13 Jan 1999
09652
UPDATES  -

13 Jan 99
-
Updated manufacturer’s phone numbers and deleted color choices.



SECTION  09652


 RESILIENT SHEET FLOORING
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

Edit paragraph 1' as necessary if no integral sheet vinyl base required.

1.
Furnish and install flooring, with integral coved sheet vinyl base where indicated on Drawings, as described in Contract Documents.

 1.2
SUBMITTALS
A.
Product Data
Product Data
1.
Manufacturer's literature or cut sheet for each component of system

2.
Maintenance instructions

3.
Color and style selection

 1.3
PROJECT CONDITIONS
A.
Project Environmental Requirements

1.
Store materials at not less than 70 deg F for at least 24 hours before using.

2.
Do not apply in temperatures below 70 deg F.

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Flooring

1.
0.050 inch minimum vinyl wear layer bonded to filled fibrous composition backing.  Total thickness 0.080 inch minimum.  Color and pattern to extend entirely through wear layer.

2.
Approved Patterns And Manufacturers  -
Approved Products
a.
Commercial Corlon by Armstrong World Industries  (800) 292-6308 www.armstrongfloors.com
b.
Series 8000 by Azrock Industries, San Antonio, TX  (205) 766-0234 www.domco.com
c.
Foundations by Congoleum Corp, Lawrenceville, NJ  (609) 584-3000 www.concoleum.com
d.
ArchiTextures - Terrain by Mannington Commercial, Salem, NJ  (609) 935-3000  www.mannington.com
B.
Adhesive  -  Water-resistant type.  Best grade in accordance with Manufacturer's recommendations.

Delete Paragraphs ‘C’ and ‘D’ if no integral sheet vinyl base.

C.
Metal Corner And Cap Trim  -  As recommended by Sheet Vinyl Manufacturer.

D.
Cove Stick  -  As recommended by Sheet Vinyl Manufacturer.

PART 3 EXECUTION
 3.1
EXAMINATION
A.
Inspect surfaces for conditions not suitable for first class installation.  Remedy cracks and minor irregularities in accordance with Manufacturer's recommendations.  Do not start work until defects are corrected.

 3.2
INSTALLATION
Installation
A.
Install flooring in manner to produce smooth, even finished surfaces tightly jointed and accurately aligned in accordance with Manufacturer's recommendations.

1.
Fit neatly against projections, piping, electrical service outlets, etc.

Delete paragraph ‘2' if no integral sheet vinyl base to be provided.

2.
Form 4 inch high integral cove base supported by cove stick.

3.
Leave flooring level, free from buckles, cracks, and projecting edges.

B.
Install in accordance with Manufacturer's recommendations.

 3.3
ADJUSTING
A.
Inspect floors and make necessary adjustments within one month after mechanical heat or other heat has been supplied continuously in finished areas.


END OF SECTION

20020
1
Section 09652

MeetingHouse
May 22, 2000
Resilient Sheet Flooring

