SECTION 09654

RUBBER FLOOR MAT

PART 1 – GENERAL 

1.1 SUMMARY 

A. Includes but not limited to 

1. Furnishing and installing rubber floor mat as described in contract documents.  

1.2 SUBMITTALS

A. Product Data – manufacturer’s product literature 

1.3 PROJECT CONDITIONS 

A. Project environmental requirements 

1. Store materials at not less than 70 deg F for at least 24 hours before using.  

2. Do not apply in temperatures below 70 deg F.  

PART 2 – PRODUCTS 

2.1 MATERIAL 

A. Entry tile – recessed 

1. Specifications – No TT-12:  Furnish and install Musson No. TT‑12 Fluff-Cord Strip Tile in alternating parquet pattern, either perpendicular or diagonally as shown on drawings.  Tile shall be 3/8” thick x 12” x 12” tile size (or longitudinal rolls 12” wide x 25’ long) with a close-nap nylon carpet-like surface in Natural Earthtone gray color; manufactured of rubber-fabric, heavy duty truck or bus tire strips bonded to a flexible backing with a “dry back” adhesive back.  Tile must be installed using manufacturer’s specific installation instructions and Musson No. TT-390, Non-flammable Environmentally Safe Adhesive.  

2. Meets OSHA specifications and flammability requirements of DOC-FF-1-170.  

3. Approved manufacturers – 

a. Musson Rubber Co., Akron, OH  (800) 321-2381.  

B. Adhesive – Best grade as recommended by rubber manufacturer.  

PART 3 – EXECUTION 

3.1 PREPARATION 

A. Surface to receive rubber shall be sound, clean, free from foreign matter, tightly nailed, and dry.  Remedy cracks and minor irregularities in accordance  with Manufacturer’s recommendations.  Do not start work until defects are corrected.  

3.2 INSTALLATION 

A. Install in manner to produce smooth, even-finished surfaces tightly jointed and accurately aligned.  

B. Fit rubber tightly.  

C. Secure rubber with dry-back adhesive back.  

D. Line up to  and bottom lines or rubber at joints throughout.  

E. Roll rubber until firm bond has been established.  

F. Leave level, free from buckles, cracks, and projecting edges.  

3.3 ADJUSTING 

A. Inspect and make necessary adjustments within one month after mechanical heat or other heat has been supplied continuously in finished areas.  

END OF SECTION

557-1804 (20020)
1
Section 09654

Orlando Welfare Complex
October 11, 2000
Rubber Floor Mat
557-1804 (20020)
2
Section 09654

Orlando Welfare Complex
October 11, 2000
Rubber Floor Mat 


