STANDARD
29 Jun 1999
09723

UPDATES  -

29 Jun 99
-
Updated Bolta phone number.

11 Feb 99
-
Changed method of selecting and specifying colors.

Vinyl wall covering is authorized for use only where shown on current, standard plans, without exception.



SECTION  09723


VINYL-COATED FABRIC WALL COVERING

PART 1 GENERAL

 1.1
SUMMARY

A.
Includes But Not Limited To

Refer to vinyl-coated fabric wall covering as ‘Type B Wall Covering’ on the Drawings and in the Finish Schedule.

1.
Furnish and install wall covering as described in Contract Documents.

B.
Related Sections

1.
Section 09923  -  Priming of gypsum board surfaces.
09923
 1.2
SUBMITTALS

A.
Product Data
Product Data
1.
Manufacturer's literature or cut sheet

2.
Cleaning and maintenance instructions

3.
Color and pattern selection

B.
Quality Assurance / Control  -  Manufacturer's published installation instructions.
Quality
 1.3
QUALITY ASSURANCE

A.
Qualifications  -  Installer shall have satisfactorily completed at least one project of comparable quality and scope within two years before bidding and be approved by Architect.

B.
Regulatory Requirements

1.
Meet or exceed Fed Spec CCC-W-408A Type II, Class A.  Requirements of this standard restrict approvals to flame spread no higher than 25.

2.
Manufacturer shall meet governing codes requiring higher than specified standards.

PART 2 PRODUCTS

 2.1
MATERIALS

A.
Wall Covering

1.
Supporting Materials  -  Cotton cloth, osnaburg, or other suitable materials that will meet above standards.

2.
Coating Compound  -  Formulate from Virgin Polymerized or Copolymerized Vinylchloride resin, plasticized with phosphate or phthalate-ester plasticizers exclusively and be integrally pigmented.

3.
Top Coating  -  Meet requirements of Table 1 Fed Spec CCC-W-408a clear virgin polymerized vinyl-chloride resin or a modified vinyl chloride resin.  Use phosphate or phthalate-ester plasticized exclusively.

4.
Width  -  54 inches minimum.

5.
Minimum Weight  -  20 oz per lin yard for 54 inch width.

Select the pattern to be used as the Pattern Quality Standard from one of the patterns recommended below, unless another is approved by Project Manager after submission of required color board.  Select a color available in the selected pattern from neutral or pastel colors.

6.
Quality Standards  -

a.
Pattern  -  Alcazar or Lyon by Bolta

b.
Color  -  

7.
Approved Manufacturers  -
Approved Products
a.
Bolta Wallcoverings Div of GenCorp, Hackensack, NJ  (800) 621-4006 www.cw.gencorp.com/bolta.htm
b.
Genon Wallcovering Div of GenCorp, Hackensack, NJ  (201) 489-0100 www.gencorp.com
c.
R J F Koroseal Wall Covering, Fairlawn, OH  (800) 828-4556  

d.
Laminating Services, Louisville, KY  (800) 453-9132  www.vinlfab.com
B.
Adhesives

1.
Use only fungus resistant adhesives.

2.
Acceptable Manufacturers  -
Approved Products
a.
Romans Professional extra strength.

b.
Equal as recommended by Wall Covering Manufacturer and approved by Architect before installation.  See Section 01600.

PART 3 EXECUTION
Installation
 3.1
PREPARATION

A.
Prime or size surfaces other than gypsum board with material recommended by Wall Covering Manufacturer.


END OF SECTION

557-1804 (20020)
2
09723

Orlando Welfare Complex
October 11, 2000
Vinyl-Coated Fabric Wall Covering


