SECTION 09800

ELASTOMERIC COATING SYSTEM

1.1
GENERAL


A.
Submittals:  Submit the following according to Conditions of the Contract and Division 1 Specification Sections:

1.
Product data for each coating system specified, including block fillers and primers.

a.

Provide the manufacturer's technical information including label analysis and instructions for handling, storing, and applying each material proposed for use.


2.
Samples for initial color selection in the form of manufacturer's color charts.  After color selection, the Architect will furnish color chips for surfaces to be coated.


B.
Applicator Qualifications:  Engage an experienced applicator who has successfully completed coating system applications similar in material and extent to those indicated for the Project.


C.
Single-Source Responsibility:  Provide primers and undercoat material produced by the same manufacturer as the finish coats.


D.
Deliver materials to the job site in the manufacturer's original, unopened packages and containers bearing manufacturer's name and label.


E.
Store materials not in use in tightly covered containers in a well-ventilated area at a minimum ambient temperature of 45 deg F.  Maintain containers used in storage in a clean condition, free of foreign materials, and residue.


F.
Project Conditions:  Apply coatings only when the temperature of surfaces to be coated and surrounding air temperatures are between 45 deg F  and 95 deg F.  Do not apply coatings in snow, rain, fog, or mist; when the relative humidity exceeds 85 percent; at temperatures less than 5 deg F above the dew point; or to damp or wet surfaces.

G. Warranty:  

Special Project Warranty:  Submit a written warranty on labor and material executed by the manufacturer, covering failure of elastomeric coatings within the warranty periord.  This warranty shall be in addition to, and not a limitation of, other rights the Owner may have against the Contractor under the Contract Documents.

Warranty period for elastomeric coatings is 5 years after the date of substantial completion.

1.2 PRODUCTS


A.
Manufacturers:  Subject to compliance with requirements, provide products of one of the following:

1.

Rainguard Products, Inc. – Tec Top 

2.

Textured Coatings of America – Texcote STRETCH

3.

Tamms Industries, Co. - Tamolastic


B.
Special Coating Materials, General:  Provide block fillers, primers, finish coat material, and related materials that are compatible with one another and the substrates indicated under conditions of service and application, as demonstrated by the manufacturer based on testing and field experience.


C.
Material Quality:  Provide the highest quality grade of the various coatings as regularly manufactured by acceptable coating manufacturers.  Materials not displaying manufacturer's identification as a best-grade product will not be acceptable.


D.
Colors:  Provide color selections made by the Architect from the manufacturer's full range of colors, both standard and premium colors.

1.3
EXECUTION


A.
Examination:  Examine substrates and conditions under which coatings will be applied for compliance with requirements on applying coatings.  Surfaces to receive coatings must be thoroughly dry before coatings are applied.


1.
Do not proceed with coating application until unsatisfactory conditions have been corrected.


2.
Start of application will be construed as the Applicator's acceptance of surfaces within that particular area.


B.
Coordinating Work:  Review Sections in which other coatings are provided to ensure compatibility of the total systems for various substrates.  On request, furnish information on the characteristics of specified finish materials, to ensure use of compatible primers.


1.
Notify the Architect of problems anticipated using the coatings specified over substrates primed by others.


C.
Surface Preparation:  Clean and prepare surfaces to be coated according to the manufacturer's instructions for each particular substrate condition and as specified.


1.

Provide barrier coats over incompatible primers or remove and reprime.


D.
Material Preparation:  Carefully mix and prepare materials according to the coating manufacturer's directions.


1.
Stir materials before application to produce a mixture of uniform density, as required during application.  Do not stir surface film into the material.  Remove film and, if necessary, strain the coating material before using.


2.
Use only thinners approved by the manufacturer, and only within recommended limits.


E.
Application:  Apply special coatings by brush, roller, spray, squeegee, or other applicators according to the manufacturer's directions.  Use brushes best suited for the material being applied.  Use rollers of carpet, velvet back, or high-pile sheep's wool as recommended by the manufacturer for the material and texture required.


1.
Do not apply coatings over dirt, rust, scale, grease, moisture, scuffed surfaces, or conditions detrimental to the formation of a durable coating film.


2.

Provide finish coats compatible with the primers used.


3.
The number of coats and the film thicknesses required are the same regardless of the application method.  Do not apply succeeding coats until previous coat has cured.  Sand between applications where sanding is required to produce a smooth, even surface.


4.
Where undercoats or other conditions show through the final coat, apply additional coats until the cured film has a uniform coating finish, color, and appearance.


F.
Scheduling Coating:  Apply first coat to surfaces that have been cleaned, pretreated, or otherwise prepared for coating as soon as practicable and before subsequent surface deterioration.  Allow sufficient drying time between successive coats.  Do not recoat until the coating has dried.


G.
Application Procedures:  Apply coatings by brush, roller, spray, or other applicators according to the manufacturer's directions.


H.
Minimum Coating Thickness:  Apply materials at the manufacturer's recommended spreading rate.  Provide 20 mils total dry film thickness of the final finish coat.  


I.
Prime Coats:  Before applying finish coats, apply a prime coat of material, as recommended by the manufacturer, to material required to be coated or finished that has not been prime-coated by others.  Recoat primed and sealed substrates where there is evidence of suction spots or unsealed areas in the first coat to ensure a finish coat with no burn-through or other defects due to insufficient sealing.


J.
Completed Work:  Match approved samples for color, texture, and coverage.  Remove, refinish, or recoat work not complying with specified requirements.


K.
Cleaning:  At the end of each work day, remove rubbish, empty cans, rags, and other discarded materials from the site.


1.
Upon completion of work, clean glass and spattered surfaces.  Remove spattered coatings by washing, scraping, or other methods.  Do not scratch or damage adjacent finished surfaces.


L.
Protection:  Protect work of other trades, whether to be coated or not, against damage from coating.  Correct damage by cleaning, repairing, replacing, and recoating as acceptable to the Architect.  Leave in an undamaged condition.


M.
Signs:  Provide "Wet Paint" signs to protect newly coated finishes.  Remove temporary protective wrappings provided by others for protection of their work, after completing coating operations.


1.
At completion of construction activities of other trades, touch up and restore damaged or defaced coated surfaces.

END OF SECTION 09800

557-1804 (20020)
3
Section 09800

Orlando Welfare Complex
October 11, 2000
Elastomeric Coating System 


