STANDARD
2 Aug 1999
09914
UPDATES  -

2 Aug 99
-
Added PPG Porter

11 Jan 99
-
Updated Benjamin Moore Products.  Added ICI Devoe and ICI Fuller O’Brien.

Edit title and other references in this Section to include only type of surfaces to be painted.



SECTION  09914


EXTERIOR PAINTED CMU, CONCRETE, STUCCO
PART 1 GENERAL
 1.1
SUMMARY
A.
Includes But Not Limited To

Delete paragraph ‘1' is no new exterior cementitious surfaces are to be painted.

1.
Preparing and painting new exterior masonry, concrete, and stucco surfaces as described in Contract Documents.

On addition / remodel Projects requiring painting of existing surfaces, list or describe the existing exterior cementitious surfaces to be painted under this Section, show them graphically on the Drawings, or include them on a schedule in the Drawings.  If one of the latter two options is used, delete paragraph ‘2.’

2.
Preparing and painting following existing exterior CMU, concrete, and stucco surfaces as described in Contract Documents  -

a.


b.


c.


B.
Related Sections

1.
Section 09901  -  General Painting Requirements
09901
Edit the list of approved manufacturers and their systems to include only those with whom you are familiar and whose products are available in the Project area.  Do not add or approve any other manufacturers or systems without approval of Architectural & Engineering Services.

PART 2 PRODUCTS
 2.1
MATERIALS
A.
Sealer

1.
Benjamin Moore  -  Moore’s Acrylic Sealer 066

2.
ICI Paints  -

a.
ICI Dulux  -  2000-XXXX Decrashield Primer

b.
ICI Devoe  -  DR2002 Wonder Guard Exterior Acrylic Latex HP Primer

c.
ICI Fuller O’Brien  -  668-50 Weather King Exterior Acrylic Latex Primer

3.
PPG Paints  -

a.
PPG Pittsburgh Paints  -  

b.
PPG Porter  - 898 Porterlock Pigmented Bonding Coat

4.
Pratt & Lambert  -  Weatherflex Pigmented Surface Conditioner 380-6508

5.
Sherwin-Williams  -  LOXON Clear Masonry Sealer

6.
Wm. Zinsser  -  Bulls Eye 1-2-3 Primer / Sealer Stain-Killer

B.
Primer Coat

1.
Benjamin Moore  -  023 Fresh Start

2.
ICI Paints  -

a.
ICI Dulux  -  2000-XXXX Decrashield Primer

b.
ICI Devoe  -  DR2002 Wonder Guard Exterior Acrylic Latex HP Primer

c.
ICI Fuller O’Brien  -  668-50 Weather King Exterior Acrylic Latex Primer

3.
PPG Paints  -

a.
PPG Pittsburgh Paints  -  6-603 SpeedHide Alkali Resistant Primer

b.
PPG Porter  -  335 Acri-Pro 100 Acrylic Primer

4.
Pratt & Lambert  -  Vapex House Paint

5.
Sherwin-Williams  -  LOXON Masonry Primer

6.
Wm. Zinsser  -  Bulls Eye 1-2-3 Primer / Sealer Stain-Killer

C.
Finish Coat

1.
Benjamin Moore  -  171 Moorcraft SuperSpec Flat Latex Paint

2.
ICI Paints  -

a.
ICI Dulux  -  2200-XXXX Decrashield Flat Finish

b.
ICI Devoe  -  DR15XX Wonder Shield Flat Finish

c.
ICI Fuller O’Brien  -  FOB663-XX Weather King II Exterior Latex Flat

3.
PPG Paints  -

a.
PPG Pittsburgh Paints  -  72-Line Sunproof Flat

b.
PPG Porter  -  519 Acri-Shield Flat Exterior Acrylic

4.
Pratt & Lambert  -  Vapex House Paint

5.
Sherwin-Williams  -  A-100 Exterior Latex Flat

Edit the list of approved manufacturers to include only those with whom you are familiar and whose products are available in the Project area.  Edit the product listing in each paint Section to correspond with this list as edited for this Project.  DO NOT ADD OR APPROVE ANY OTHER MANUFACTURERS OR SYSTEMS.  NO OTHER MANUFACTURERS OR PRODUCTS ARE ACCEPTABLE FOR THIS PAINT.

 2.2
APPROVED MANUFACTURERS
Approved Products
A.
Benjamin Moore, Montvale, NJ  (888) 236-6667  www.benjaminmoore.com
B.
ICI Paints

1.
ICI Dulux Paints, Cleveland, OH  (800) 984-5444  www.icidulux.com
2.
ICI Devoe,  www.devoepaint.com
3.
ICI Fuller O’Brien,  www.fullerpaint.com
C.
PPG Paints

1.
PPG Pittsburgh Paints, Pittsburgh, PA  (800) 441-9695 www.ppgaf.com
2.
PPG Porter, Louisville, KY  (800) 322-6370  www.porterpaints.com
D.
Pratt & Lambert, Cleveland, OH  (800) 289-7728  

E.
Sherwin-Williams, Cleveland, OH  (800) 321-8194  www.sherwin-williams.com
F.
Wm. Zinsser & Co, Somerset, NJ  (908) 469-8100  www.zinsser.com
PART 3 EXECUTION
 3.1
PREPARATION
A.
Except for steam cured products, cure cement type surfaces from 60 to 90 days in accordance with Paint Manufacturer's recommendations before painting.

 3.2
APPLICATION
Installation
A.
General  -  See appropriate paragraphs of Section 09901.
09901
B.
New Surfaces

1.
On highly porous surfaces when weather is exceptionally hot and dry, it may be desirable to dampen surface before applying first coat of an emulsion paint.

2.
Completely cover voids in masonry block but do not fill.

3.
Roll after spraying if necessary to eliminate pinholing.

After examination of the existing surfaces to be repainted, edit the procedure to be followed in preparing those surfaces for repainting, if necessary.

Delete Paragraphs ‘C’ and ‘D’ if no existing exterior CMU, concrete, or stucco work is to be painted.

C.
Existing Painted Surfaces

1.
Remove deteriorated and chalked existing paint down to sound substrate by scraping and or high pressure spray.  Feather edges of existing paint by sanding to be smooth with adjacent surfaces.

2.
Clean existing sound painted surfaces as well as scraped and sanded existing painted surfaces as recommended by Paint Manufacturer.

3.
Fill cracks with masonry crack filler.

4.
Prime scraped and sanded areas.

5.
Apply finish coat as required for new work.

D.
Existing Unpainted Surfaces

1.
Power wash surfaces to be painted.

2.
Fill cracks with masonry crack filler.

3.
Aply sealer coat.

4.
Apply finish coat as required for new work.


END OF SECTION

ADVANCE \d252
B L A N K   P A G E

20020
3
Section 09914

MeetingHouse
May 22, 2000
Exterior Painted CMU, Concrete, Stucco

