STANDARD
29 Jul 1999
09936

UPDATES  -

15 Mar 99
-
Added ICI LDS 95 and LDS Cherry stain colors

4 Feb 99
-
Added new color scheme information.

Use this Section for new buildings and for existing buildings where ALL of the woodwork is being replaced or refinished.



SECTION  09936


INTERIOR CLEAR FINISHED HARDWOOD

PART 1 GENERAL

 1.1
SUMMARY

A.
Includes But Not Limited To

1.
Preparing and finishing of new interior clear finished hardwood as described in Contract Documents.

B.
Related Sections

1.
Section 09901  -  General Painting Requirements
09901
 1.2
SUBMITTALS

A.
Samples
Samples
1.
Before performing work of this Section, prepare control sample, to match sample available from Architect, to be used as finishing standard for interior clear finished hardwood.  

2.
Finish applicator shall attend progress meeting held before preparation of control sample.  Architect will review requirements to insure that control sample will be prepared using specified products and procedures.

3.
Control sample shall consist of 12 inch square plain sawn solid Red Oak or plain sliced Red Oak veneer plywood.

4.
Architect will inspect control sample at progress meeting following preparation of control sample.  When sample is approved, work of this Section may proceed.

PART 2 PRODUCTS

Edit the list of approved finish manufacturers and their systems to include only those with whom you are familiar and whose products are available in the Project area.  Do not add or approve any other manufacturers or systems except as noted.

 2.1
MATERIALS

Use this Paragraph ‘A’ for Southwest and Classical Style buildings

A.
LDS 95 Oak Stain

1.
Fuller O'Brien  -  Fruitwood No. 640-02 Pen Chrome Stain.

2.
Sherwin-Williams  -  S64XXN0443-4371

3.
ICI  -  Woodpride 1700-6700 Early American

4.
Equal matching Architect's sample as approved by Architect before application.  See Section 01600.

Use this Paragraph ‘A’ for Colonial, New England, and Traditional Style buildings

B.
Clear Finish Coats

1.
Guardsman  -

a.
First Coat  -  14-7074 Pre-Catalyzed Lacquer Sealer

b.
Second And Third Coats  -  14-7075 Pre-Catalyzed Lacquer

2.
ICI Dulux / Trinity  -

a.
First Coat  -  ICE Vinyl Sanding Sealer

b.
Second And Third Coats  -  ICI Pre-Catalyzed Lacquer

3.
Lilly  -

a.
First, Second, And Third Coats  -  20 Sheen Pre-Catalyzed Lacquer 587E208

4.
Pratt & Lambert / M.L.Campbell  -

a.
First Coat  -  C101-83 Vinyl Sealer

b.
Second And Third Coats  -  C112-204 Pre-Catalyzed Lacquer.

5.
Sherwin-Williams  -

a.
First Coat  -  T67F3 Vinyl Sealer

b.
Second And Third Coats  -  T77F38 Sherwood Pre-Catalyzed Lacquer DRE.

Edit the list of approved manufacturers to include only those with whom you are familiar and whose products are available in the Project area.  Edit the product listing in each paint Section to correspond with this list as edited for this Project.  DO NOT ADD OR APPROVE ANY OTHER MANUFACTURERS OR SYSTEMS.  NO OTHER MANUFACTURERS OR PRODUCTS ARE ACCEPTABLE FOR THIS PAINT.

 2.2
APPROVED MANUFACTURERS
Approved Products
A.
Guardsman, Grand Rapids, MI  (616) 452-5181  www.guardsmanwoodpro.com
B.
ICI Dulux Paints, Cleveland, OH  (800) 984-5444  www.icidulux.com
C.
Lilly Industries Inc, Indianapolis, IN  (317) 634-8512  www.lillyindustries.com
D.
Pratt & Lambert, Cleveland, OH  (800) 289-7728

E.
Sherwin-Williams, Cleveland, OH  (800) 321-8194  www.sherwin-williams.com
PART 3 EXECUTION

 3.1
APPLICATION
Installation
A.
See appropriate paragraphs of Section 09901.
09901
B.
Sand entire surface of item to be finished lightly with 120 to 150 non-stearated sandpaper and clean before applying dye or stain.

C.
Apply stain in accordance with Manufacturer's recommendations and as necessary to attain correct color.

D.
Scuff sand with 220 stearated sandpaper between application of application stain and first finish coat.

E. Where backpriming is required, apply one coat of finish material.

END OF SECTION

557-1804 (20020)
2
Section 09936

Orlando Welfare Complex
October 11,2000
Interior Clear Finished Hardwood


