Copyright 2011 AIA
MasterSpec Professional
05/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 061533 - WOOD PATIO DECKING
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Wood decking.

2. Plastic decking.

3. Stairs for elevated decks.

4. Railings for elevated decks.

5. Wood benches for elevated decks.

6. Support framing for elevated decks.

1.2 ACTION SUBMITTALS

A. Product Data: For preservative-treated wood products, plastic decking and metal framing anchors.

1.3 INFORMATIONAL SUBMITTALS

A. Material Certificates:

Delete first subparagraph below if species and grade are indicated for each use.

1. For lumber specified to comply with minimum allowable unit stresses. Indicate species and grade selected for each use and design values approved by ALSC's Board of Review.

2. For preservative-treated wood products. Indicate type of preservative used and net amount of preservative retained.

B. Evaluation Reports: For the following, from ICC-ES:

Revise list below to retain only those products retained in Part 2.

1. Preservative-treated wood products.

2. Plastic decking.

3. Expansion anchors.

4. Metal framing anchors.

5. Decking fasteners.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see SECTION 016000 "Product Requirements."

2.1 LUMBER, GENERAL

A. Comply with DOC PS 20 and with grading rules of lumber grading agencies certified by ALSC's Board of Review as applicable. If no grading agency is indicated, comply with the applicable rules of any rules-writing agency certified by ALSC's Board of Review.

1. Factory mark each item with grade stamp of grading agency.

Retain first option in first subparagraph below if authorities having jurisdiction require grade stamps on all materials.

2. For items that are exposed to view in the completed Work, mark grade stamp on end or back of each piece or omit grade stamp and provide certificates of grade compliance issued by grading agency.

3. Provide dressed lumber, S4S, unless otherwise indicated.

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply. An alternative method of dealing with this credit requirement is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," or Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how this credit requirement will be met.

Retain "Certified Wood" Paragraph below if wood patio decking is required to be certified for LEED. An alternative method of dealing with this credit requirement is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," or Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how the credit requirement will be met. Manufacturers certifying products as "FSC Mixed Credit" do not have to use 100 percent certified wood in the products, but in their total production manufacturers must use an amount equal to or greater than the percentage of their production that is labeled "FSC Mixed Credit."

B. Maximum Moisture Content:

1. Boards: 19 percent.

2. Dimension Lumber: 19 percent.

3. Timber. 19 percent.

2.2 WOOD DECKING AND STAIR TREADS
Retain one of two "Dimension Lumber Decking( and Stair Treads)" paragraphs below for 2-by-4 and 2-by-6 decking.

A. Dimension Lumber Decking and Stair Treads: Construction or No. 2 grade and any of the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Redwood; RIS.

B. Dimension Lumber Decking and Stair Treads: Deck Heart or Construction Heart redwood; RIS.

C. Board Decking and Stair Treads: 1-1/4-inch actual thickness radius-edged decking of any of the following species and grades:

1. Douglas fir-larch or Douglas fir-south, Patio 1; WWPA.

2. Douglas fir-larch, Select Dex; WCLIB.

3. Douglas fir-larch (North), Commercial Patio; NLGA.

4. Hem-fir, Patio 1; WWPA.

5. Hem-fir, Commercial Dex; WCLIB.

6. Hem-fir (North), Commercial Patio; NLGA.

7. Redwood, Heart B or Select Heart; RIS.

8. Southern pine, Premium; SPIB.

9. Western red cedar, Patio 1; WWPA.

10. Western red cedar, Commercial Dex; WCLIB.

11. Western red cedar (North), Commercial Patio; NLGA.

2.3 WOOD RAILINGS

A. Dimension Lumber Railing Members: No. 1 or No. 2 grade and any of the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Redwood; RIS.

5. Spruce-pine-fir or spruce-pine-fir (South); NeLMA, NLGA, WCLIB, or WWPA.

B. Dimension Lumber Railing Members: Heart B or Select Heart redwood; RIS.

C. Railing Boards:  Any of the following species and grades:
1. Douglas fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

2. Hem-fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

3. Redwood, Heart B or Select Heart; RIS.

4. Southern pine, B & B finish; SPIB.

2.4 WOOD BENCHES

A. Dimension Lumber for Benches: Select Structural or No. 1 grade and any of the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Redwood; RIS.

5. Spruce-pine-fir or spruce-pine-fir (South); NeLMA, NLGA, WCLIB, or WWPA.

B. Dimension Lumber for Benches: Heart B or Select Heart redwood; RIS.

C. Boards for Benches: Any of the following species and grades:
1. Douglas fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

2. Hem-fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

3. Redwood, Heart B or Select Heart; RIS.

2.5 DIMENSION LUMBER FRAMING

If retaining first "Deck( and Stair) Framing" Paragraph below, retain one of five options for grade; verify with structural requirements. Generally retain "No. 2" or "Construction or No. 2" option for best economy if grades comply with structural requirements.

A. Deck and Stair Framing: Select Structural, No. 1 or No. 2 grade and any of the following species:

Revise list below; usually retain all species that comply with requirements except those not available in Project's location. Species groups are listed in order of decreasing strength (extreme fiber in bending).

1. Hem-fir (North); NLGA.

2. Southern pine; SPIB.

3. Douglas fir-larch; WCLIB or WWPA.

4. Spruce-pine-fir; NLGA.

5. Douglas fir-south; WWPA.

6. Hem-fir; WCLIB or WWPA.

7. Douglas fir-larch (North); NLGA.

8. Spruce-pine-fir (South); NeLMA, WCLIB, or WWPA.

"Deck( and Stair) Framing" Paragraph below is an example of a performance requirement that can be used instead of paragraph above. If retaining paragraph below, retain options or revise values and insert other properties to suit structural requirements of Project.

B. Deck and Stair Framing: Any species and grade with a modulus of elasticity of at least 1,300,000 psi  and an extreme fiber stress in bending of at least 850 psi for 2-inch nominal  thickness and 12-inch nominal width for single-member use.

2.6 POSTS

Retain "Dimension Lumber Posts" Paragraph below for posts 4 by 4 inches nominal (89 by 89 mm actual). Posts 6 by 6 inches nominal (140 by 140 mm actual) and larger are timber rather than dimension lumber.

A. Dimension Lumber Posts: Construction or No. 2  grade and any of the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Spruce-pine-fir or spruce-pine-fir (South); NeLMA, NLGA, WCLIB, or WWPA.

Species group in first subparagraph below includes hem-fir (North) and spruce-pine-fir.

5. Northern species; NLGA.

Species group in first subparagraph below includes spruce-pine-fir (South).

6. Eastern softwoods; NeLMA.

Species group in subparagraph below includes hem-fir and spruce-pine-fir (South).

7. Western woods; WCLIB or WWPA.

Retain one of three "Timber Posts" paragraphs below for rectangular posts 6 by 6 inches nominal (140 by 140 mm actual) and larger.

B. Timber Posts: Balsam fir, Douglas fir-larch, Douglas fir-larch (North), eastern hemlock tamarack (North), hem-fir, southern pine, western hemlock, or western hemlock (North); No. 2; NeLMA, NLGA, SPIB, WCLIB, or WWPA.

C. Timber Posts: Alaska cedar; No. 2; WCLIB.

D. Timber Posts: Southern pine; No. 2; SPIB.

2.7 PRESERVATIVE TREATMENT

A. Pressure treat boards and dimension lumber with waterborne preservative according to AWPA U1; Use Category UC3b for exterior construction not in contact with the ground, and Use Category UC4a for items in contact with the ground.
B. Pressure treat timber with waterborne preservative according to AWPA U1; Use Category UC4a.

See Evaluations for information about treatment chemicals.

C. Preservative Chemicals: Acceptable to authorities having jurisdiction.

1. Do not use chemicals containing arsenic or chromium, except for timber posts.

Usually retain one of first two paragraphs below.

D. Use process that includes water-repellent treatment.

E. Use process that does not include water repellents or other substances that might interfere with application of indicated finishes.

Revise options in first paragraph below to eliminate items for which treated kiln-dried wood is not required.

F. After treatment, redry board, dimension lumber and timber to 19 percent maximum moisture content.

G. Mark treated wood with treatment quality mark of an inspection agency approved by ALSC's Board of Review.

Retain first option in subparagraph below if authorities having jurisdiction require quality mark on all materials.

1. For items indicated to receive a stained or natural finish, mark each piece on surface that will not be exposed or omit marking and provide certificates of treatment compliance issued by inspection agency.

Retain first option in "Application" Paragraph below and delete subparagraphs if total treatment is required; otherwise, retain second option and applicable subparagraphs.

H. Application: Treat items indicated on Drawings and the following:
1. Framing members.
2. Sills and ledgers.

3. Members in contact with masonry or concrete.

4. Posts.

5. Round wood poles.

6. Decking.

7. Stair treads.

2.8 PLASTIC DECKING

A. Plastic Lumber, General: Products acceptable to authorities having jurisdiction with current model code evaluation reports that show compliance with building code in effect for Project for indicated type of construction.

1. Allowable loads and spans, as documented in evaluation reports or in information referenced in evaluation reports, shall not be less than design loads and spans indicated.

Most plastic decking is a composite product consisting of solid shapes made from recycled polyethylene and cellulose fiber (wood or agricultural waste fiber).

B. Composite Plastic Lumber: Solid or hollow shapes made from a mixture of cellulose fiber and polyethylene or polypropylene.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's name and model number are indicated on Drawings.

a. AZEK Building Products, Inc.

b. CertainTeed Corporation.

c. Crawford Industries, LLC.

d. Deceuninck North America.

e. Fiberon, LLC.

f. GAF Decking Systems, LLC.

g. GAF Materials Corporation.

h. Green Bay Decking.

i. Midwest Manufacturing Extrusion.

j. Millennium Decking Inc.

k. Premium Composites LLC.

l. Rhino Deck.

m. TAMKO Building Products, Inc.

n. Thermal Industries, Inc.

o. TimberTech.

p. Trex Company, Inc.

q. Universal Forest Products, Inc.

r. Weyerhaeuser Company.

2. Decking Standard: ICC-ES AC109 or ICC-ES AC174.

3. Surface Texture: Specified by Architect.

4. Color: As selected by Architect from manufacturer's full range.

2.9 FASTENERS

A. General: Provide fasteners of size and type indicated, acceptable to authorities having jurisdiction, and that comply with requirements specified in this article for material and manufacture. Provide nails or screws, in sufficient length, to penetrate not less than 1-1/2 inches into wood substrate.

1. Use fasteners with hot-dip zinc coating complying with ASTM A 153/A 153M or ASTM F 2329 unless otherwise indicated.

2. For pressure-preservative-treated wood, use stainless-steel fasteners.

3. For wood decking, use stainless-steel fasteners where fasteners are exposed to view.

B. Postinstalled Anchors: Stainless-steel, chemical or torque-controlled expansion anchors with capability to sustain, without failure, a load equal to 6 times the load imposed when installed in unit masonry assemblies and equal to 4 times the load imposed when installed in concrete as determined by testing according to ASTM E 488 conducted by a qualified independent testing and inspecting agency.

1. Stainless-steel bolts and nuts complying with ASTM F 593 and ASTM F 594, Alloy Group 1 or 2.
2.10 METAL FRAMING ANCHORS

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Retain "Basis-of-Design Product" Paragraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's name and model number are indicated on Drawings.

1. Cleveland Steel Specialty Co.

2. KC Metals Products, Inc.

3. Phoenix Metal Products, Inc.

4. R. H. Tamlyn & Sons LP.

5. Simpson Strong-Tie Co., Inc.

6. USP Structural Connectors.

If retaining first option in "Allowable Design Loads" Paragraph below, indicate design loads for metal framing anchors on Drawings.

B. Allowable Design Loads: Provide products with allowable design loads, as published by manufacturer, that meet or exceed those indicated on Drawings. Manufacturer's published values shall be determined from empirical data or by rational engineering analysis and demonstrated by comprehensive testing performed by a qualified independent testing agency.

Retain "Galvanized-Steel Sheet" or "Stainless-Steel Sheet" Paragraph below. For pressure-preservative-treated wood, G185 (Z550) galvanizing or stainless steel is required by the IBC for exterior applications. Type 304 is usually standard for stainless steel; use Type 316 where subject to salt spray or immersion in salt water.

C. Galvanized-Steel Sheet: Hot-dip, zinc-coated steel sheet complying with ASTM A 653/A 653M, G90 coating designation.

D. Stainless-Steel Sheet: ASTM A 666, Type 304.

2.11 CONCEALED DECKING FASTENERS

A. Deck Splines: Corrosion-resistant metal or plastic splines that fit in grooves routed into the sides of decking material and are fastened to deck framing with screws. Splines provide uniform spacing of decking material.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, available products that may be incorporated into the Work include, but are not limited to, the following:

a. Blue Heron Enterprises, LLC; Eb-Ty Hidden Deck-Fastener.

b. Grabber Construction Products; Deck Clip.

c. Ipe Clip Fastener Company Inc. (The); Ipe Clip.

d. KK Mfg. Co., Inc; Lumber Loc Hidden Deck Fasteners.

e. M. M. Products, Inc; Invisi-Fast Biscuit.

f. Titan Metal Werks, Inc; DeckEase Hidden Deck Fasteners.

B. Deck Clips: Black-oxide-coated, stainless-steel clips designed to be fastened to deck framing with screws, and to secure decking material with teeth that also provide uniform spacing of decking material.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, available products that may be incorporated into the Work include, but are not limited to, the following:

a. Tiger Claw Inc; Tiger Claw Hidden Deck Fasteners.

C. Deck Tracks: Formed metal strips designed to be fastened to deck framing and to secure decking material from underside with screws. Made from epoxy-powder-coated, hot-dip galvanized steel or stainless steel.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, available products that may be incorporated into the Work include, but are not limited to, the following:

a. Grabber Deckmaster; Deckmaster.

b. Ty-Lan Enterprises Inc; Shadoe Track.

PART 3 -  EXECUTION

3.1 INSTALLATION, GENERAL

A. Set work to required levels and lines, with members plumb, true to line, cut, and fitted. Fit work to other construction; scribe and cope as needed for accurate fit.

B. Framing Standard: Comply with AF&PA WCD1 unless otherwise indicated.

C. Install wood decking and stair treads with crown up (bark side down).

D. Install plastic lumber to comply with manufacturer's written instructions.

Retain options for acceptable fastening methods in first paragraph below, or delete paragraph to allow Contractor to use any method acceptable to authorities having jurisdiction.

E. Secure decking to framing with deck tracks or screws.

F. Install metal framing anchors to comply with manufacturer's written instructions.

G. Do not splice structural members between supports unless otherwise indicated.

Delete first paragraph below for southern pine.

H. Apply copper naphthenate field treatment to comply with AWPA M4, to cut surfaces of preservative-treated lumber.

I. Securely attach exterior rough carpentry work to substrate by anchoring and fastening as indicated, complying with the following:

If retaining first subparagraph below, verify that evaluation report is acceptable to authorities having jurisdiction.

1. ICC-ES AC70 for power-driven fasteners.

Retain one of two subparagraphs below, with or without subparagraph above.

2. "Fastening Schedule" in ICC's International Building Code.

3. "Fastener Schedule for Structural Members" and "Alternate Attachments" in ICC's International Residential Code for One- and Two-Family Dwellings.

3.2 ELEVATED DECK JOIST FRAMING INSTALLATION

A. General: Install joists with crown edge up and support ends of each member with not less than 2 inches of bearing on wood or metal, or 3 inches on masonry. Attach floor joists where framed into wood supporting members by using wood ledgers as indicated or, if not indicated, by using metal joist hangers. Do not notch joists.

B. Lap members framing from opposite sides of beams or girders not less than 4 inches or securely tie opposing members together.

3.3 STAIR INSTALLATION

First paragraph below is an example only; option is based on NFPA 101 requirement. Revise if more stringent tolerances are required.

A. Provide stair framing with no more than 3/16-inch variation between adjacent treads and risers and no more than 3/8-inch variation between largest and smallest treads and risers within each flight.

B. Treads and Risers: Secure by gluing and screwing to carriages. Countersink fastener heads, fill flush, and sand filler. Extend treads over carriages and finish with bullnose edge.

3.4 RAILING INSTALLATION

Descriptive requirements in this article cover basic railing installation only; supplement with complete details.

A. Balusters: Fit to railings, glue, and screw in place. Countersink fastener heads, fill flush, and sand filler.

B. Newel Posts: Secure to stringers and risers with through bolts.

C. Railings: Secure wall rails with metal brackets. Fasten freestanding railings to newel posts and to trim at walls with countersunk-head wood screws or rail bolts and glue.

END OF SECTION 061533

	WOOD PATIO DECKING
	061533 - 6



