Section 07466 – Page 2
Fiber Cement Siding and Trim
Section 07466 – Page 3
Fiber Cement Siding and Trim  

SECTION 07466 
 FIBER CEMENT SIDING AND TRIM
PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Siding Panels
2. Accessories and Trim

B. Related Sections:

1. Section 06100 – Rough Carpentry
2. Section 07920 – Joint Sealants

3. Section 09910 – Paints and Coatings

1.2 REFERENCES
A. ASTM C 920 – Standard Specification for Elastomeric Joint Sealants; 1998
B. ASTM C 1185 – Standard Test Methods for Sampling and Testing Non – Asbestos Fiber Cement Flat Sheet, Roofing and Siding Shingles, and Clapboards; 1999
C. ASTM C 1186 – Standard Specification for Flat Non – Asbestos Fiber Cement Sheets; 1999

D. ASTM E 72
-
Standard Test Methods of Conducting Strength Tests of Panels for Building Construction; 1998
E. ASTM E 84 – Standard Test Method for Surface Burning Characteristics of Building Materials; 1999

F. ASTM E 96 – Standard Test Method for Water Vapor Transmission of Materials: 1995

G. ASTM E 136 – Standard Test Method for Behavior of Materials in a Vertical Tube Furnace AT 750 Degrees C; 1999

H. ASTM E 228 – Standard Test Method for Linear Thermal Expansion of Solid Materials With a Vitreous Silica Dilatometer; 1995

I. ASTM G 26 – Standard Practice for Operating Light – Exposure Apparatus (Xenon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials; 1996
1.3 SUBMITTALS

A. Product Data:  For each type of product indicated.
1.

Preparation Instructions and recommendations.

2.

Storage and handling requirements and recommendations.

3.

Installation methods, including nailing patterns.

4.
Applicable model code authority evaluation report (ICBO, BOCA, CCMC, etc.)

B. Siding manufacturer’s requirements for vapor retarders, primer, paint, etc., to be installed by others.
C. Samples:  6” x 6” of each type of siding and trim and in each color, texture, and trim pattern required.
D. Maintenance and periodic inspection recommendations.
1.4 WARRANTY

A. Register manufacturer’s warranty, made out in California Department of Parks & Recreation (DPR), with a copy to DPR.
1.   Warranty Period:  30 non-pro-rated years on siding and a 15 non-pro-rated year minimum on all trim material from date of Substantial Completion.

PART 2 -  PRODUCTS

2.1 BASIS OF DESIGN
A. Fiber Cement Siding:  Fiber cement siding and accessories complying with ASTM C1185-96, ASTM E72-95 and ASTM E 84.
1. James Hardie Building Products, Inc.
26300 La Alameda, Suite 400

Mission Viejo, CA 92691

866-274-3464 or 949-367-4980

www.jameshardie.com

2. Color and Texture: Primed ready for paint. Prime all cut edges prior to installation.

3. Interior Pattern:  HardiePanel-Sierra 8”.

4. Exterior Pattern:  HardiePanel-Cedarmill non-grooved.
2.2 ACCESSORIES
A. Batten Material:  “HardieBatten” rustic fiber-cement trim boards; nominal 1x3 (3/4”x2-1/2” actual).
B. Trim:  “Hardie Artisan Accent Trim” rustic fiber-cement trim boards, nominal 2x4 and 2x6 (1-1/2”x3-1/2” and 1-1/2”x5-1/2” actual).
C. Joint Treatment:  Caulk joints per Section 07920.

D. Siding Nails:  Fasteners shall be corrosion resistant, high stainless steel; .092” shank x .225” head x 2” siding nails.
E. Water-Resistive Barrier:  “HardieWrap TM” weather barrier; “HardieWrap TM” flashing; “HardieWrap TM” flex flashing; “HardieWrap TM” seam Tape.

F. Field Finish Paint:  100 percent acrylic latex as specified in Section 09900.
PART 3 -  EXECUTION

3.1 EXAMINATION

A. Prior to commencing installation, verify governing dimensions of building and condition of substrate.
3.2 PREPARATION
A. Examine, clean, and repair as necessary any substrate conditions that would be detrimental to proper installation.
B. Do not begin installation until unacceptable conditions have been corrected.
3.3 INSTALLATION
A. Install in accordance with manufacturer’s instructions and drawing details.
1. Read warranty and comply with all terms necessary to maintain warranty coverage.

2. Use trim details indicated on drawings.

3. Touch up all field cut edges before installing.

4. Pre-drill nail holes if necessary to prevent breakage.
B. Over Plywood Sheathing: Fasten siding through sheathing into studs.

C. Position all ends and edges of all interior and exterior panels over framing members, except when butt joints are at right angles to framing members, as in perpendicular application.  Install double blocking at panel butt joints.
D. To minimize end joints, use panels of maximum practical lengths.

E. Allow space between both ends of siding panels that butt against trim for thermal movement; seal joint between panel and trim with exterior grade sealant.

F. Joints in Vertical Siding: Install Z-flashing in horizontal joints between successive courses of vertical siding.

G. Do not install siding less than 6 inches from surface of ground nor closer than 1 inch to roofs, patios, porches, and other surfaces where water may collect.

H. After installation, seal all joints.  Seal around all penetrations.  Paint all exposed cut edges.

I. Finish Painting: Specified in Section 09900.

J. Finish Painting: Within 24 months after installation.
3.4 CLEANING
A. At completion of work, remove debris caused by siding installation from project site.
B. Touch-up, repair or replace damaged products before Substantial Completion.
END OF SECTION 07466
