STATE OF LOUISIANA

STATE POLICE TROOP L HEADQUARTERS

HVAC SYSTEM REPLACEMENT

MANDEVILLE, LOUISIANA



Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 042000
UNIT MASONRY
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Concrete masonry units (CMU's).

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product indicated.

1.3 INFORMATIONAL SUBMITTALS

Usually retain first paragraph below. Material certificates are required for all masonry constructed under MSJC Code. Retain second option if required by authorities having jurisdiction or if the added assurance of quality that test reports provide is desired.

A. Material Certificates: For each type and size of product indicated. For masonry units include material test reports substantiating compliance with requirements.

B. Mix Designs: For each type of mortar and grout. Include description of type and proportions of ingredients.

1. Include test reports for mortar mixes required to comply with property specification. Test according to ASTM C 109/C 109M for compressive strength, ASTM C 1506 for water retention, and ASTM C 91 for air content.

2. Include test reports, according to ASTM C 1019, for grout mixes required to comply with compressive strength requirement.

1.4 QUALITY ASSURANCE

A. Masonry Standard: Comply with ACI 530.1/ASCE 6/TMS 602 unless modified by requirements in the Contract Documents.

1.5 PROJECT CONDITIONS

A. Cold-Weather Requirements: Do not use frozen materials or materials mixed or coated with ice or frost. Do not build on frozen substrates. Remove and replace unit masonry damaged by frost or by freezing conditions. Comply with cold-weather construction requirements contained in ACI 530.1/ASCE 6/TMS 602.

B. Hot-Weather Requirements: Comply with hot-weather construction requirements contained in ACI 530.1/ASCE 6/TMS 602.

PART 2 -  PRODUCTS

2.1 MASONRY UNITS, GENERAL

A. Defective Units: Referenced masonry unit standards may allow a certain percentage of units to contain chips, cracks, or other defects exceeding limits stated in the standard. Do not use units where such defects will be exposed in the completed Work.

See BIA Technical Notes 16B and NCMA TEK 7-3 for information on determining fire-resistance ratings of masonry walls.

B. Fire-Resistance Ratings: Where indicated, provide units that comply with requirements for fire-resistance ratings indicated as determined by testing according to ASTM E 119, by equivalent masonry thickness, or by other means, as acceptable to authorities having jurisdiction.

2.2 CONCRETE MASONRY UNITS

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply.

A. Shapes: Provide special shapes for lintels, corners, jambs, sashes, movement joints, headers, bonding, and other special conditions.

Retain first paragraph below for increased water resistance of units if required. If retaining, also retain water-repellent mortar admixture.

Copy and revise first paragraph below for non-load-bearing CMUs (changing ASTM C 90 to ASTM C 129) if needed; they are not usually an inventory item and may have to be ordered in large quantities. Indicate load-bearing and non-load-bearing units on Drawings if both are specified.

B. CMUs: ASTM C 90.

Usually retain first subparagraph below only for masonry designed by analytical methods; delete if compressive strength specified in ASTM C 90, which is 1900 psi (13.1 MPa), is acceptable. See Evaluations.

1. Unit Compressive Strength: Provide units with minimum average net-area compressive strength of 1900 psi.
Retain one of three weights in subparagraph below or delete subparagraph for Contractor's option. Retain last option for default requirement if more than one weight is used. See Evaluations.

2. Density Classification: Normal weight unless otherwise indicated.

Concrete building brick in first paragraph below is often used to adjust dimensions in CMU construction.

2.3 MORTAR AND GROUT MATERIALS

Coordinate requirements in this article with those in "Mortar and Grout Mixes" Article.

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply.

Retain one or more of first four paragraphs below. Delete masonry cement if not allowed by "Mortar and Grout Mixes" Article. See Evaluations for discussion of masonry cement.

A. Portland Cement: ASTM C 150, Type I or II, except Type III may be used for cold-weather construction. Provide natural color or white cement as required to produce mortar color indicated.

B. Hydrated Lime: ASTM C 207, Type S.

Mix in first paragraph below allows better control of color than job-mixed, portland cement-lime mortar. If retaining, also retain last two paragraphs above.

C. Portland Cement-Lime Mix: Packaged blend of portland cement and hydrated lime containing no other ingredients.

2.4 REINFORCEMENT

Retain first paragraph below for reinforcing bars in grouted cells. Revise if another grade of steel is required. Revise to specify epoxy-coated, stainless-steel, or galvanized bars if required.

A. Uncoated Steel Reinforcing Bars: ASTM A 615/A 615M or ASTM A 996/A 996M, Grade 60.
Standard in first paragraph below includes requirements for mill-galvanized, carbon steel; hot-dip galvanized, carbon steel; and stainless steel. It is not necessary to specify these materials separately.

PART 3 -  EXECUTION

3.1 INSTALLATION, GENERAL

A. Use full-size units without cutting if possible. If cutting is required to provide a continuous pattern or to fit adjoining construction, cut units with motor-driven saws; provide clean, sharp, unchipped edges. Allow units to dry before laying unless wetting of units is specified. Install cut units with cut surfaces and, where possible, cut edges concealed.

B. Select and arrange units for exposed unit masonry to produce a uniform blend of colors and textures.

Retain paragraph below for high-suction brick. A simple test to determine if wetting is required consists of drawing a circle the size of a quarter on a brick and placing 20 drops of water in the circle; if water is absorbed within 1-1/2 minutes, the brick requires wetting.

3.2 MORTAR BEDDING AND JOINTING

A. Lay hollow CMUs as follows:

1. With face shells fully bedded in mortar and with head joints of depth equal to bed joints.

2. With webs fully bedded in mortar in all courses of piers, columns, and pilasters.

3. With webs fully bedded in mortar in grouted masonry, including starting course on footings.

4. With entire units, including areas under cells, fully bedded in mortar at starting course on footings where cells are not grouted.

B. Lay solid masonry units with completely filled bed and head joints; butter ends with sufficient mortar to fill head joints and shove into place. Do not deeply furrow bed joints or slush head joints.

If another joint profile is used, revise first paragraph below or show on Drawings.

C. Tool exposed joints slightly concave when thumbprint hard, using a jointer larger than joint thickness unless otherwise indicated.

D. Cut joints flush for masonry walls to receive plaster or other direct-applied finishes (other than paint) unless otherwise indicated.

3.3 REPAIRING, POINTING, AND CLEANING

A. In-Progress Cleaning: Clean unit masonry as work progresses by dry brushing to remove mortar fins and smears before tooling joints.

B. Final Cleaning: After mortar is thoroughly set and cured, clean exposed masonry as follows:

1. Test cleaning methods on sample wall panel; leave one-half of panel uncleaned for comparison purposes.

Delete first two subparagraphs below if cleaners are not specified in Part 2 or if cleaners are not allowed.

2. Protect surfaces from contact with cleaner.

3. Wet wall surfaces with water before applying cleaners; remove cleaners promptly by rinsing surfaces thoroughly with clear water.

4. Clean brick by bucket-and-brush hand-cleaning method described in BIA Technical Notes 20.

Retain last subparagraph above or first subparagraph below. Coordinate with products retained in Part 2. If high-pressure water cleaning or other methods are acceptable, delete or revise subparagraph below and insert applicable requirements.

5. Clean masonry with a proprietary acidic cleaner applied according to manufacturer's written instructions.

6. Clean concrete masonry by cleaning method indicated in NCMA TEK 8-2A applicable to type of stain on exposed surfaces.

END OF SECTION 042000

	UNIT MASONRY
	042000 - 1



