SLIDELL MEMORIAL HOSPITAL

WOMEN’S IMAGING CENTER

1495 GAUSE BLVD.

Slidell LA  70458



SECTION 02751
CEMENT CONCRETE PAVEMENT
Copyright 2002, The American Institute of Architects (AIA)

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes exterior cement concrete pavement for the following:

Adjust list below to suit Project.

1. Driveways and roadways.

2. Parking lots.

3. Curbs and gutters.

4. Walkways.

B. Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

1. Division 2 Section "Earthwork" for subgrade preparation, grading, and subbase course.

2. Division 2 Section "Cement Concrete Pavement" for surface-imprinted, stamped finished concrete pavement.

3. Division 3 Section "Cast-in-Place Concrete" for general building applications of concrete.

1.3 DEFINITIONS

Definition below refers to those materials that make up cementitious component of water-cementitious materials ratio.

A. Cementitious Materials:  Portland cement alone or in combination with one or more of blended hydraulic cement, fly ash and other pozzolans, and ground granulated blast-furnace slag.

1.4 SUBMITTALS

A. Product Data:  For each type of manufactured material and product indicated.

B. Design Mixtures:  For each concrete pavement mixture.  Include alternate mixture designs when characteristics of materials, Project conditions, weather, test results, or other circumstances warrant adjustments.

Coordinate paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

C. Qualification Data:  For manufacturer.

Delete paragraph and subparagraph below if material test reports are not required.

D. Material Test Reports:  From a qualified testing agency indicating and interpreting test results for compliance of the following with requirements indicated, based on comprehensive testing of current materials:

Retain option in subparagraph below if retaining service record data with "Normal-Weight Aggregates" Paragraph in Part 2 "Concrete Materials" Article.

1. Aggregates.

Delete paragraph and subparagraphs below if material test reports are not required.

E. Material Certificates:  Signed by manufacturers certifying that each of the following materials complies with requirements:

Edit list below to suit Project.

1. Cementitious materials.

2. Steel reinforcement and reinforcement accessories.

3. Fiber reinforcement.

4. Admixtures.

5. Curing compounds.

6. Applied finish materials.

7. Bonding agent or epoxy adhesive.

8. Joint fillers.

Retain paragraph below if Contractor is responsible for field quality-control testing.

F. Field quality-control test reports.

Delete paragraph below if no preinstallation conference.

G. Minutes of preinstallation conference.

1.5 QUALITY ASSURANCE

A. Manufacturer Qualifications:  Manufacturer of ready-mixed concrete products who complies with ASTM C 94/C 94M requirements for production facilities and equipment.

Delete subparagraph below if not required.

1. Manufacturer certified according to NRMCA's "Certification of Ready Mixed Concrete Production Facilities."

Retain first paragraph below if Contractor or manufacturer selects testing agency.

B. Testing Agency Qualifications:  An independent agency qualified according to ASTM C 1077 and ASTM E 329 for testing indicated, as documented according to ASTM E 548.

Retain subparagraph below, which is required by ACI 301 and ASTM C 31/C 31M, if emphasis is needed.  ASTM C 1077 notes that relevant field or laboratory technician certification by ACI, NRMCA, PCA, or National Institute for Certification in Engineering Technologies may demonstrate evidence of competence.

1. Personnel conducting field tests shall be qualified as ACI Concrete Field Testing Technician, Grade 1, according to ACI CP-01 or an equivalent certification program.

C. ACI Publications:  Comply with ACI 301, "Specification for Structural Concrete," unless modified by requirements in the Contract Documents.

D. Concrete Testing Service:  Engage a qualified independent testing agency to perform material evaluation tests and to design concrete mixtures.

Delete paragraph and subparagraphs below if not required.  If retaining, indicate location, size, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

E. Mockups:  Cast mockups of full-size sections of concrete pavement to demonstrate typical joints, surface finish, texture, color, and standard of workmanship.

1. Build mockups in the location and of the size indicated or, if not indicated, as directed by Architect.

2. Notify Architect seven days in advance of dates and times when mockups will be constructed.

3. Obtain Architect's approval of mockups before starting construction.

4. Maintain approved mockups during construction in an undisturbed condition as a standard for judging the completed pavement.

5. Demolish and remove approved mockups from the site when directed by Architect.

Delete subparagraph above or below.

6. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Preinstallation conference in paragraph below is desirable for major concrete pavement installations because it helps minimize misunderstandings and reviews Project conditions that might lead to significant problems.  Delete paragraph and subparagraphs below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 1.

F. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination."

Retain subparagraph and associated subparagraphs below if warranted by complexity of mixture design and quality control of concrete materials.

1. Before submitting design mixtures, review concrete pavement mixture design and examine procedures for ensuring quality of concrete materials and concrete pavement construction practices.  Require representatives, including the following, of each entity directly concerned with concrete pavement, to attend conference:

a. Contractor's superintendent.

b. Independent testing agency responsible for concrete design mixtures.

c. Ready-mix concrete producer.

d. Concrete pavement subcontractor.

1.6 PROJECT CONDITIONS

Delete this Article if not required.

A. Traffic Control:  Maintain access for vehicular and pedestrian traffic as required for other construction activities.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

Edit this Article with other Part 2 articles in which manufacturers and products, or manufacturers only, are named.  See Division 1 Section "Product Requirements" for an explanation of the terms "Available Products," "Products," "Available Manufacturers," and "Manufacturers" and the effect these terms have on "Comparable Product" and "Product Substitution" requirements.

A. In other Part 2 articles where titles below introduce lists, the following requirements apply to product selection:

1. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, products specified.

2. Products:  Subject to compliance with requirements, provide one of the products specified.

3. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, manufacturers specified.

2.2 FORMS

Delete or revise materials in this Article to suit Project.

A. Form Materials:  Plywood, metal, metal-framed plywood, or other approved panel-type materials to provide full-depth, continuous, straight, smooth exposed surfaces.

1. Use flexible or curved forms for curves with a radius 100 feet or less.

B. Form-Release Agent:  Commercially formulated form-release agent that will not bond with, stain, or adversely affect concrete surfaces and will not impair subsequent treatments of concrete surfaces.

2.3 STEEL REINFORCEMENT

A. Plain-Steel Welded Wire Reinforcement:  ASTM A 185, fabricated from as-drawn steel wire into flat sheets.

B. Deformed-Steel Welded Wire Reinforcement:  ASTM A 497, flat sheet.

C. Epoxy-Coated Welded Wire Fabric:  ASTM A 884/A 884M, Class A, plain steel.

D. Reinforcing Bars:  ASTM A 615/A 615M, Grade 60; deformed.

E. Steel Bar Mats:  ASTM A 184/A 184M; with ASTM A 615/A 615M, Grade 60, deformed bars; assembled with clips.

F. Plain Steel Wire:  ASTM A 82.

G. Deformed-Steel Wire:  ASTM A 496.

Plastic-surfaced or reinforced-paper-covered dowels are available from proprietary sources.

H. Joint Dowel Bars:  Plain steel bars, ASTM A 615/A 615M, Grade 60.  Cut bars true to length with ends square and free of burrs.

I. Tie Bars:  ASTM A 615/A 615M, Grade 60, deformed.

Retain paragraph above or first paragraph below.  Tie bars above or hook bolts below may be used for connection between new and existing pavement and between pavement and gutters.

J. Hook Bolts:  ASTM A 307, Grade A, internally and externally threaded.  Design hook-bolt joint assembly to hold coupling against pavement form and in position during concreting operations, and to permit removal without damage to concrete or hook bolt.

K. Bar Supports:  Bolsters, chairs, spacers, and other devices for spacing, supporting, and fastening reinforcing bars, welded wire reinforcement, and dowels in place.  Manufacture bar supports according to CRSI's "Manual of Standard Practice" from steel wire, plastic, or precast concrete of greater compressive strength than concrete, and as follows:

Delete or revise subparagraphs below to suit Project.

1. Equip wire bar supports with sand plates or horizontal runners where base material will not support chair legs.

L. Zinc Repair Material:  ASTM A 780.

2.4 CONCRETE MATERIALS

Retain option in paragraph below if final choice of cementitious material will be Contractor's option.

A. Cementitious Material:  Use one of the following cementitious materials, of the same type, brand, and source throughout the Project:

1. Portland Cement:  ASTM C 150, Type II gray.   Supplement with the following:

a. Fly Ash:  ASTM C 618, Class C.

b. Ground Granulated Blast-Furnace Slag:  ASTM C 989, Grade 100 or 120.

B. Normal-Weight Aggregates:  ASTM C 33, uniformly graded.  Provide aggregates from a single source.

1. Maximum Coarse-Aggregate Size:  1 inch nominal.

Retain subparagraph below if optional restriction in ASTM C 33 is required.

2. Fine Aggregate:  Free of materials with deleterious reactivity to alkali in cement.

C. Water:  ASTM C 94/C 94M.

D. Air-Entraining Admixture:  ASTM C 260.

E. Chemical Admixtures:  Provide admixtures certified by manufacturer to be compatible with other admixtures and to contain not more than 0.1 percent water-soluble chloride ions by mass of cementitious material.

Select one or more chemical admixtures from six subparagraphs below.

1. Water-Reducing Admixture:  ASTM C 494/C 494M, Type A.

2. Retarding Admixture:  ASTM C 494/C 494M, Type B.

3. Water-Reducing and Retarding Admixture:  ASTM C 494/C 494M, Type D.

4. High-Range, Water-Reducing Admixture:  ASTM C 494/C 494M, Type F.

5. High-Range, Water-Reducing and Retarding Admixture:  ASTM C 494/C 494M, Type G.

6. Plasticizing and Retarding Admixture:  ASTM C 1017/C 1017M, Type II.

2.5 CURING MATERIALS

Select curing aids and materials from this Article.

A. Absorptive Cover:  AASHTO M 182, Class 2, burlap cloth made from jute or kenaf, weighing approximately 9 oz./sq. yd.  dry.

B. Moisture-Retaining Cover:  ASTM C 171, polyethylene film or white burlap-polyethylene sheet.

C. Water:  Potable.

Evaporation retarder in paragraph below temporarily reduces moisture loss from concrete surfaces awaiting finishing in hot, dry, and windy conditions.  Evaporation retarders are neither curing compounds nor chemical surface retarders used to delay concrete setting.

D. Evaporation Retarder:  Waterborne, monomolecular film forming; manufactured for application to fresh concrete.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. Available Products:

a. Axim Concrete Technologies; Cimfilm.

b. Burke by Edeco; BurkeFilm.

c. ChemMasters; Spray-Film.

d. Conspec Marketing & Manufacturing Co., Inc.; Aquafilm.

e. Dayton Superior Corporation; Sure Film.

f. Euclid Chemical Company (The); Eucobar.

g. Kaufman Products, Inc.; Vapor Aid.

h. Lambert Corporation; Lambco Skin.

i. L&M Construction Chemicals, Inc.; E-Con.

j. MBT Protection and Repair, ChemRex Inc.; Confilm.

k. Meadows, W. R., Inc.; Sealtight Evapre.

l. Metalcrete Industries; Waterhold.

m. Nox-Crete Products Group, Kinsman Corporation; Monofilm.

n. Sika Corporation, Inc.; SikaFilm.

o. Symons Corporation; Finishing Aid.

p. Vexcon Chemicals, Inc.; Certi-Vex EnvioAssist.

Retain paragraph below if a dissipating-type waterborne membrane-forming curing compound is required.  While EPA mandates maximum VOC emissions of 350 g/L for this product category, verify that it meets curing compound VOC emission limits of authorities having jurisdiction.  If appearance of pavement is important before breakdown and disappearance of curing membrane, verify rate of dissipation with manufacturers.

E. Clear Waterborne Membrane-Forming Curing Compound:  ASTM C 309, Type 1, Class B.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. Available Products:

a. Anti-Hydro International, Inc.; AH Curing Compound #2 DR WB.

b. Burke by Edoko; Aqua Resin Cure.

c. ChemMasters; Safe-Cure Clear.

d. Conspec Marketing & Manufacturing Co., Inc.; W.B. Resin Cure.

e. Dayton Superior Corporation; Day Chem Rez Cure (J-11-W).

f. Euclid Chemical Company (The); Kurez DR VOX.

g. Kaufman Products, Inc.; Thinfilm 420.

h. Lambert Corporation; Aqua Kure-Clear.

i. L&M Construction Chemicals, Inc.; L&M Cure R.

j. Meadows, W. R., Inc.; 1100 Clear.

k. Nox-Crete Products Group, Kinsman Corporation; Resin Cure E.

l. Symons Corporation; Resi-Chem Clear.

m. Tamms Industries Inc.; Horncure WB 30.

n. Unitex; Hydro Cure 309.

o. Vexcon Chemicals, Inc.; Certi-Vex Enviocure 100.

Retain paragraph below if a white waterborne membrane-forming curing compound is required.  Retain if greater reflectivity is required.  Review product choices because some dissipate and others are abraded by traffic.  While EPA mandates maximum VOC emissions of 350 g/L for this product category, verify that it meets curing compound VOC emission limits of authorities having jurisdiction.

F. White Waterborne Membrane-Forming Curing Compound:  ASTM C 309, Type 2, Class B.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. Available Products:

a. Anti-Hydro International, Inc.; AH Curing Compound #2 WP WB.

b. Burke by Edoco; Resin Emulsion White.

c. ChemMasters; Safe-Cure 2000.

d. Conspec Marketing & Manufacturing Co., Inc.; W.B. Resin Cure.

e. Dayton Superior Corporation; Day-Chem White Pigmented Cure (J-10-W).

f. Euclid Chemical Company (The); Kurez VOX White Pigmented.

g. Kaufman Products, Inc.; Thinfilm 450.

h. Lambert Corporation; Aqua Kure-White.

i. L&M Construction Chemicals, Inc.; L&M Cure R-2.

j. Meadows, W. R., Inc.; 1200-White.

k. Symons Corporation; Resi-Chem White.

l. Tamms Industries, Inc.; Horncure 200-W.

m. Unitex; Hydro White.

n. Vexcon Chemicals, Inc.; Certi-Vex Enviocure White 100.

2.6 RELATED MATERIALS

Select one or all options in paragraph below.

A. Expansion- and Isolation-Joint-Filler Strips:  ASTM D 1751, asphalt-saturated cellulosic fiber or ASTM D 1752, cork or self-expanding cork.

Retain first paragraph below for integrally colored concrete pavement.

B. Color Pigment:  ASTM C 979, synthetic mineral-oxide pigments or colored water-reducing admixtures; color stable, free of carbon black, nonfading, and resistant to lime and other alkalis.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. AvailableManufacturers:

a. Bayer Corporation.

b. ChemMasters.

c. Conspec Marketing & Manufacturing Co., Inc.

d. Davis Colors.

e. Elementis Pigments, Inc.

f. Hoover Color Corporation.

g. Lambert Corporation.

h. Scofield, L. M.Company.

i. Solomon Colors.

Select one of three options in subparagraph below.

2. Color: As selected by Architect from manufacturer's full range.

C. Slip-Resistive Aggregate Finish:  Factory-graded, packaged, rustproof, nonglazing, abrasive aggregate of fused aluminum-oxide granules or crushed emery with emery aggregate containing not less than 50 percent aluminum oxide and not less than 20 percent ferric oxide; unaffected by freezing, moisture, and cleaning materials.

Bonding agents may be used directly from container or as an admixture in cement or sand cement slurry.

D. Bonding Agent:  ASTM C 1059, Type II, non-redispersible, acrylic emulsion or styrene butadiene.

E. Epoxy Bonding Adhesive:  ASTM C 881, two-component epoxy resin, capable of humid curing and bonding to damp surfaces, of class suitable for application temperature and of grade to requirements, and as follows:

Select types from options in subparagraph below based on service loadings.

1. Types I and II, non-load bearing or IV and V, load bearing, for bonding hardened or freshly mixed concrete to hardened concrete.

Retain paragraph below for exposed-aggregate finish requiring surface retarder.  This retarder is not an evaporative retarder.

F. Chemical Surface Retarder:  Water-soluble, liquid-set retarder with color dye, for horizontal concrete surface application, capable of temporarily delaying final hardening of concrete to a depth of 1/8 to 1/4 inch .

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. AvailableProducts:

a. Burke by Edeco; True Etch Surface Retarder.

b. ChemMasters; Exposee.

c. Conspec Marketing & Manufacturing Co., Inc.; Delay S.

d. Euclid Chemical Company (The); Surface Retarder S.

e. Kaufman Products, Inc.; Expose.

f. Metalcrete Industries; Surftard.

g. Nox-Crete Products Group, Kinsman Corporation; Crete-Nox TA.

h. Scofield, L. M. Company; Lithotex.

i. Sika Corporation, Inc.; Rugasol-S.

j. Vexcon Chemicals, Inc.; Certi-Vex Envioset.

G. Pigmented Mineral Dry-Shake Hardener:  Factory-packaged dry combination of portland cement, graded quartz aggregate, color pigments, and plasticizing admixture.  Use color pigments that are finely ground, nonfading mineral oxides interground with cement.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. Available Products:

Pigmented mineral dry-shake hardeners below vary in their resistance to freeze-thaw cycles and deicing salts.  Verify suitability for application with manufacturers because many dry-shake hardeners are intended for floor application and are not recommended for use on concrete in which air content exceeds 3 percent.  Verify color range with manufacturers before selection.

a. Conspec Marketing & Manufacturing Co., Inc.; Conshake 600 Colortone.

b. Dayton Superior Corporation; Quartz Tuff.

c. Euclid Chemical Company (The); Surflex.

d. Lambert Corporation; Colorhard.

e. L&M Construction Chemicals, Inc.; Quartz Plate FF.

f. MBT Protection and Repair, ChemRex Inc.; Mastercron.

g. Metalcrete Industries; Floor Quartz.

h. Scofield, L. M. Company; Lithochrome Color Hardener.

i. Symons Corporation; Hard Top.

Select one of three options in subparagraph below.

2. Color:  As selected by Architect from manufacturer's full range.

Retain paragraph below if rock-salt finish is required.

H. Rock Salt:  Sodium chloride crystals, kiln dried, coarse gradation with 100 percent passing 3/8-inch sieve and 85 percent retained on a No. 8 sieve.

2.7 PAVEMENT MARKINGS

Some formulations of waterborne emulsions are very quick drying, others less so; see manufacturer's literature.

A. Pavement-Marking Paint:  Latex, waterborne emulsion, lead and chromate free, ready mixed, complying with FS TT-P-1952, with drying time of less than 45 minutes.

Select colors from options in subparagraph below; show locations on Drawings if more than one color is required.

1. Color: As required by local authorities.

Add product requirements here for permanent-marking tapes or thermoplastic paints if required.  See Evaluations.

2.8 WHEEL STOPS

Retain paragraph and subparagraph below if precast concrete wheel stops are required.  Revise concrete strength or dimensions if required.

A. Wheel Stops:  Precast, air-entrained concrete, 2500-psi minimum compressive strength, 4-1/2 inches high by 9 inches wide by 72 inches  long.  Provide chamfered corners and drainage slots on underside and holes for anchoring to substrate.

1. Dowels:  Galvanized steel, 3/4-inch  diameter, 10-inch  minimum length.

2.9 CONCRETE MIXTURES

A. Prepare design mixtures, proportioned according to ACI 301, for each type and strength of normal-weight concrete determined by either laboratory trial mixes or field experience.

1. Use a qualified independent testing agency for preparing and reporting proposed concrete mixture designs for the trial batch method.

B. Proportion mixtures to provide normal-weight concrete with the following properties:

Select strength from options in subparagraph below or revise to suit Project.  Add flexural strength if required.

1. Compressive Strength (28 Days):  See Plans.

Select water-cementitious materials ratio from options in subparagraph below or revise to suit Project.  Select first option for concrete exposed to deicers or subject to freezing and thawing while moist.  Select second for concrete required to have low water permeability.

2. Maximum Water-Cementitious Materials Ratio at Point of Placement:  0.50.

Select slump limit from options in subparagraph below or revise to suit Project.

3. Slump Limit: 5 inches, plus or minus 1 inch .

Delete paragraph and subparagraphs below if concrete pavement will not be exposed to freeze-thaw cycling or deicing chemicals and if the beneficial effects of air entrainment, such as workability or cohesion of concrete mixture, are not required.

C. Add air-entraining admixture at manufacturer's prescribed rate to result in normal-weight concrete at point of placement having an air content as follows:

Percentages in options in three subparagraphs below are based on ACI 301 for exposure severity and aggregate size. Retain first option for severe exposure, second for moderate exposure, and third for mild exposure.  See Evaluations for exposure definitions.

1. Air Content:  5-1/2 percent plus or minus 1.5 percent for 1-1/2-inch  nominal maximum aggregate size.

Retain first option in first paragraph below if concrete pavement will be exposed to chlorides in service; retain second for concrete pavement that will not be dry or protected from moisture in service.  Percentages are derived from ACI 301.

D. Limit water-soluble, chloride-ion content in hardened concrete to 0.15 or 0.30 percent by weight of cement.

E. Chemical Admixtures:  Use admixtures according to manufacturer's written instructions.

Delete or revise subparagraphs below to suit Project.

1. Use water-reducing admixture in concrete, as required, for placement and workability.

2. Use water-reducing and retarding admixture when required by high temperatures, low humidity, or other adverse placement conditions.

Retain paragraph and subparagraphs below if applicable.  ACI 301 sets no limits on amounts of cementitious or mineral admixtures that can replace portland cement unless concrete is exposed to deicing chemicals.

F. Cementitious Materials:  Limit percentage, by weight, of cementitious materials other than portland cement according to ACI 301 requirements as follows:

Revise percentages in three subparagraphs below to suit Project.  Percentages are ACI 301 limits for concrete exposed to deicing chemicals.  Retain first subparagraph if either fly ash or blended hydraulic cement, pozzolan Type IP or I (PM), is specified.  Retain second if either ground granulated blast-furnace slag or blended hydraulic cement, Type IS or I (SM), is specified.  Retain third if fly ash or pozzolan-type blended hydraulic cement is specified with ground granulated blast-furnace slag.

1. Fly Ash or Pozzolan:  25 percent.

2. Ground Granulated Blast-Furnace Slag:  50 percent.

3. Combined Fly Ash or Pozzolan, and Ground Granulated Blast-Furnace Slag:  50 percent, with fly ash or pozzolan not exceeding 25 percent.

G. Color Pigment:  Add color pigment to concrete mixture according to manufacturer's written instructions and to result in hardened concrete color consistent with approved mockup.

2.10 CONCRETE MIXING

Retain option in paragraph below if synthetic fibers are required.

A. Ready-Mixed Concrete:  Measure, batch, and mix concrete materials and concrete according to ASTM C 94/C 94M and ASTM C 1116.  Furnish batch certificates for each batch discharged and used in the Work.

1. When air temperature is between 85 deg F  and 90 deg F , reduce mixing and delivery time from 1-1/2 hours to 75 minutes; when air temperature is above 90 deg F , reduce mixing and delivery time to 60 minutes.

Delete Project-site mixing below if not permitted.  ACI 301 applies requirements in ASTM C 94/C 94M to site-produced concrete.

B. Project-Site Mixing:  Measure, batch, and mix concrete materials and concrete according to ASTM C 94/C 94M.  Mix concrete materials in appropriate drum-type batch machine mixer.

1. For concrete mixes of 1 cu. yd. or smaller, continue mixing at least 1-1/2 minutes, but not more than 5 minutes after ingredients are in mixer, before any part of batch is released.

2. For concrete mixes larger than 1 cu. yd., increase mixing time by 15 seconds for each additional 1 cu. yd.

3. Provide batch ticket for each batch discharged and used in the Work, indicating Project identification name and number, date, mixture type, mixing time, quantity, and amount of water added.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine exposed subgrades and subbase surfaces for compliance with requirements for dimensional, grading, and elevation tolerances.

Revise requirements in first paragraph and subparagraphs below if concrete walkways or similar lightly loaded pavements do not require this degree of proof-rolling.

B. Proof-roll prepared subbase surface below concrete pavements with heavy pneumatic-tired equipment to identify soft pockets and areas of excess yielding.

1. Completely proof-roll subbase in one direction and repeat in perpendicular direction.  Limit vehicle speed to 3 mph.

Revise minimum weight or type of vehicle in first subparagraph below if required.

2. Proof-roll with a loaded 10-wheel tandem-axle dump truck weighing not less than 15 tons.

3. Subbase with soft spots and areas of pumping or rutting exceeding depth of 1/2 inch require correction according to requirements in Division 2 Section "Earthwork."

C. Proceed with concrete pavement operations only after nonconforming conditions have been corrected and subgrade is ready to receive pavement.

3.2 PREPARATION

A. Remove loose material from compacted subbase surface immediately before placing concrete.

3.3 EDGE FORMS AND SCREED CONSTRUCTION

A. Set, brace, and secure edge forms, bulkheads, and intermediate screed guides for pavement to required lines, grades, and elevations.  Install forms to allow continuous progress of work and so forms can remain in place at least 24 hours after concrete placement.

B. Clean forms after each use and coat with form-release agent to ensure separation from concrete without damage.

3.4 STEEL REINFORCEMENT

A. General:  Comply with CRSI's "Manual of Standard Practice" for fabricating, placing, and supporting reinforcement.

B. Clean reinforcement of loose rust and mill scale, earth, ice, or other bond-reducing materials.

C. Arrange, space, and securely tie bars and bar supports to hold reinforcement in position during concrete placement.  Maintain minimum cover to reinforcement.

D. Install welded wire reinforcement in lengths as long as practicable.  Lap adjoining pieces at least one full mesh, and lace splices with wire.  Offset laps of adjoining widths to prevent continuous laps in either direction.

Retain paragraph below if using zinc-coated reinforcement.

E. Zinc-Coated Reinforcement:  Use galvanized steel wire ties to fasten zinc-coated reinforcement.  Repair cut and damaged zinc coatings with zinc repair material.

Retain first paragraph below if using epoxy-coated reinforcement.

F. Epoxy-Coated Reinforcement:  Use epoxy-coated steel wire ties to fasten epoxy-coated reinforcement.  Repair cut and damaged epoxy coatings with epoxy repair coating according to ASTM D 3963/D 3963M.

G. Install fabricated bar mats in lengths as long as practicable.  Handle units to keep them flat and free of distortions.  Straighten bends, kinks, and other irregularities, or replace units as required before placement.  Set mats for a minimum 2-inch overlap of adjacent mats.

3.5 JOINTS

Coordinate joint types, descriptions, and locations with Drawings.  Three types of joints and tool edgings have been consolidated in this Article for consistency rather than for strict sequence of installation.

A. General:  Form construction, isolation, and contraction joints and tool edgings true to line with faces perpendicular to surface plane of concrete.  Construct transverse joints at right angles to centerline, unless otherwise indicated.

1. When joining existing pavement, place transverse joints to align with previously placed joints, unless otherwise indicated.

B. Construction Joints:  Set construction joints at side and end terminations of pavement and at locations where pavement operations are stopped for more than one-half hour unless pavement terminates at isolation joints.

1. Continue steel reinforcement across construction joints, unless otherwise indicated.  Do not continue reinforcement through sides of pavement strips, unless otherwise indicated.

2. Provide tie bars at sides of pavement strips where indicated.

Retain one or more of three subparagraphs below.  Consider butt joints for joints not subject to traffic.

3. Butt Joints:  Use bonding agent at joint locations where fresh concrete is placed against hardened or partially hardened concrete surfaces.

Retain subparagraph below for low-traffic areas if applicable.  Keyed joints are not capable of significant load transfer at joint and are not recommended by ACI 302.1R for concrete less than 6 inches (150 mm) thick.

4. Keyed Joints:  Provide preformed keyway-section forms or bulkhead forms with keys, unless otherwise indicated.  Embed keys at least 1-1/2 inches into concrete.

Retain subparagraph below for load-transfer doweled joints.  Revise if precoated dowels are required.

5. Doweled Joints:  Install dowel bars and support assemblies at joints where indicated.  Lubricate or asphalt-coat one-half of dowel length to prevent concrete bonding to one side of joint.

C. Isolation Joints:  Form isolation joints of preformed joint-filler strips abutting concrete curbs, catch basins, manholes, inlets, structures, walks, other fixed objects, and where indicated.

Expansion joints are types of isolation joints.  Revise spacing in first subparagraph below to suit Project or delete if not required.

1. Locate expansion joints at intervals of 30 feet, unless otherwise indicated.

2. Extend joint fillers full width and depth of joint.

3. Terminate joint filler not less than 1/2 inch  or more than 1 inch below finished surface if joint sealant is indicated.

4. Place top of joint filler flush with finished concrete surface if joint sealant is not indicated.

5. Furnish joint fillers in one-piece lengths.  Where more than one length is required, lace or clip joint-filler sections together.

6. Protect top edge of joint filler during concrete placement with metal, plastic, or other temporary preformed cap.  Remove protective cap after concrete has been placed on both sides of joint.

Terms "contraction joint" and "control joint" have been used interchangeably in the past.  Recent ACI documents use the term "contraction joint."  Revise description in paragraph below if the term "control joint" is preferred.

D. Contraction Joints:  Form weakened-plane contraction joints, sectioning concrete into areas as indicated.  Construct contraction joints for a depth equal to at least one-fourth of the concrete thickness, as follows:

Select type of joint-forming method required from first two subparagraphs below, or retain both at Contractor's option.  Add spacing of joints if not indicated on Drawings.

1. Grooved Joints:  Form contraction joints after initial floating by grooving and finishing each edge of joint with grooving tool to a 1/4-inch radius.  Repeat grooving of contraction joints after applying surface finishes.  Eliminate groover marks on concrete surfaces.

Delete subparagraph below if saw cutting is not permitted.  Timing is critical to sawed joints.  Widen top portion of sawed joint if joint sealants are required.  Description below allows conventional wet- and dry-cut saws and, if required depth of cut can be achieved, early entry dry-cut saws.

2. Sawed Joints:  Form contraction joints with power saws equipped with shatterproof abrasive or diamond-rimmed blades.  Cut 1/8-inch- wide joints into concrete when cutting action will not tear, abrade, or otherwise damage surface and before developing random contraction cracks.

Delete subparagraph below if no doweled contraction or expansion joints; revise if precoated dowels are required.

3. Doweled Contraction Joints:  Install dowel bars and support assemblies at joints where indicated.  See plan details to prevent concrete bonding to one side of joint.

Edging is included in this Article for its similarity to jointing.  Timing of edging after initial floating is critical.

E. Edging:  Tool edges of pavement, gutters, curbs, and joints in concrete after initial floating with an edging tool to a 1/4-inch radius.  Repeat tooling of edges after applying surface finishes.  Eliminate tool marks on concrete surfaces.

3.6 CONCRETE PLACEMENT

A. Inspection:  Before placing concrete, inspect and complete formwork installation, steel reinforcement, and items to be embedded or cast in.  Notify other trades to permit installation of their work.

B. Remove snow, ice, or frost from subbase surface and reinforcement before placing concrete.  Do not place concrete on frozen surfaces.

C. Moisten subbase to provide a uniform dampened condition at time concrete is placed.  Do not place concrete around manholes or other structures until they are at required finish elevation and alignment.

D. Comply with ACI 301 requirements for measuring, mixing, transporting, and placing concrete.

Delete first paragraph below if adding water after batch mixing is permitted.  ACI 301 and ASTM C 94/C 94M permit water to be added to concrete mix on-site to adjust slump, up to amount allowed in design mix, with some limitations.

E. Do not add water to concrete during delivery or at Project site.

F. Do not add water to fresh concrete after testing.

G. Deposit and spread concrete in a continuous operation between transverse joints.  Do not push or drag concrete into place or use vibrators to move concrete into place.

H. Consolidate concrete according to ACI 301 by mechanical vibrating equipment supplemented by hand spading, rodding, or tamping.

1. Consolidate concrete along face of forms and adjacent to transverse joints with an internal vibrator.  Keep vibrator away from joint assemblies, reinforcement, or side forms.  Use only square-faced shovels for hand spreading and consolidation.  Consolidate with care to prevent dislocating reinforcement, dowels, and joint devices.

Delete first paragraph and subparagraph below if reinforcement is set before concrete is placed.

I. Place concrete in two operations; strike off initial pour for entire width of placement and to the required depth below finish surface.  Lay welded wire fabric or fabricated bar mats immediately in final position.  Place top layer of concrete, strike off, and screed.

1. Remove and replace concrete that has been placed for more than 15 minutes without being covered by top layer, or use bonding agent if approved by Architect.

J. Screed pavement surfaces with a straightedge and strike off.

Initial floating stage between screeding and final floating finish is included here rather than in "Concrete Protection and Curing" Article.

K. Commence initial floating using bull floats or darbies to impart an open textured and uniform surface plane before excess moisture or bleed water appears on the surface.  Do not further disturb concrete surfaces before beginning finishing operations or spreading surface treatments.

Delete paragraph below if machine-placed curbs and gutters are not permitted.

L. Curbs and Gutters:  When automatic machine placement is used for curb and gutter placement, submit revised mix design and laboratory test results that meet or exceed requirements.  Produce curbs and gutters to required cross section, lines, grades, finish, and jointing as specified for formed concrete.  If results are not approved, remove and replace with formed concrete.

Delete paragraph and subparagraph below if machine-placed pavement is not acceptable.

M. Slip-Form Pavers:  When automatic machine placement is used for pavement, submit revised mix design and laboratory test results that meet or exceed requirements.  Produce pavement to required thickness, lines, grades, finish, and jointing as required for formed pavement.

1. Compact subbase and prepare subgrade of sufficient width to prevent displacement of paver machine during operations.

Delete first paragraph below if not required.

N. When adjoining pavement lanes are placed in separate pours, do not operate equipment on concrete until pavement has attained 85 percent of its 28-day compressive strength.

O. Cold-Weather Placement:  Comply with ACI 306.1 and as follows.  Protect concrete work from physical damage or reduced strength that could be caused by frost, freezing actions, or low temperatures.

1. When air temperature has fallen to or is expected to fall below 40 deg F , uniformly heat water and aggregates before mixing to obtain a concrete mixture temperature of not less than 50 deg F  and not more than 80 deg F at point of placement.

2. Do not use frozen materials or materials containing ice or snow.

3. Do not use calcium chloride, salt, or other materials containing antifreeze agents or chemical accelerators unless otherwise specified and approved in mix designs.

P. Hot-Weather Placement:  Comply with ACI 301 and as follows when hot-weather conditions exist:

1. Cool ingredients before mixing to maintain concrete temperature below 90 deg F  at time of placement.  Chilled mixing water or chopped ice may be used to control temperature, provided water equivalent of ice is calculated to total amount of mixing water.  Using liquid nitrogen to cool concrete is Contractor's option.

2. Cover steel reinforcement with water-soaked burlap so steel temperature will not exceed ambient air temperature immediately before embedding in concrete.

3. Fog-spray forms, steel reinforcement, and subgrade just before placing concrete.  Keep subgrade moisture uniform without standing water, soft spots, or dry areas.

3.7 FLOAT FINISHING

Retain first paragraph below.  Some floating and troweling machines have watering attachments.  Adding water weakens the concrete surface and can cause dusting and scaling.

A. General:  Do not add water to concrete surfaces during finishing operations.

Initial floating operation is included in "Concrete Placement" Article.

B. Float Finish:  Begin the second floating operation when bleed-water sheen has disappeared and concrete surface has stiffened sufficiently to permit operations.  Float surface with power-driven floats, or by hand floating if area is small or inaccessible to power units.  Finish surfaces to true planes.  Cut down high spots and fill low spots.  Refloat surface immediately to uniform granular texture.

Select finishes from three subparagraphs below or revise to suit Project.

1. Burlap Finish:  Drag a seamless strip of damp burlap across float-finished concrete, perpendicular to line of traffic, to provide a uniform, gritty texture.

2. Medium-to-Fine-Textured Broom Finish:  Draw a soft bristle broom across float-finished concrete surface perpendicular to line of traffic to provide a uniform, fine-line texture.

3. Medium-to-Coarse-Textured Broom Finish:  Provide a coarse finish by striating float-finished concrete surface 1/16 to 1/8 inch deep with a stiff-bristled broom, perpendicular to line of traffic.

3.8 CONCRETE PROTECTION AND CURING

A. General:  Protect freshly placed concrete from premature drying and excessive cold or hot temperatures.

B. Comply with ACI 306.1 for cold-weather protection.

If evaporation rate in first paragraph below is exceeded, ACI 305R states that plastic shrinkage cracking is probable.  See manufacturers' literature or ACI 305R for estimated moisture-loss chart relating relative humidity, air and concrete temperature, and wind velocity to rate of evaporation.

C. Evaporation Retarder:  Apply evaporation retarder to concrete surfaces if hot, dry, or windy conditions cause moisture loss approaching 0.2 lb/sq. ft. x h before and during finishing operations.  Apply according to manufacturer's written instructions after placing, screeding, and bull floating or darbying concrete, but before float finishing.

D. Begin curing after finishing concrete but not before free water has disappeared from concrete surface.

Select curing method from paragraph and subparagraphs below.

E. Curing Methods:  Cure concrete by moisture curing, moisture-retaining-cover curing, curing compound, or a combination of these as follows:

1. Moist Curing:  Keep surfaces continuously moist for not less than seven days with the following materials:

Retain first three subparagraphs below as Contractor's options unless not suited for Project.

a. Water.

b. Continuous water-fog spray.

c. Absorptive cover, water saturated and kept continuously wet.  Cover concrete surfaces and edges with 12-inch lap over adjacent absorptive covers.

2. Moisture-Retaining-Cover Curing:  Cover concrete surfaces with moisture-retaining cover for curing concrete, placed in widest practicable width, with sides and ends lapped at least 12 inches, and sealed by waterproof tape or adhesive.  Immediately repair any holes or tears during curing period using cover material and waterproof tape.

3. Curing Compound:  Apply uniformly in continuous operation by power spray or roller according to manufacturer's written instructions.  Recoat areas subjected to heavy rainfall within three hours after initial application.  Maintain continuity of coating and repair damage during curing period.

3.9 PAVEMENT TOLERANCES

A. Comply with tolerances of ACI 117 and as follows:

ACI 117 establishes few pavement tolerances; those in subparagraphs below are based on ACI 330.1.

1. Elevation:  1/4 inch.

2. Thickness:  Plus 3/8 inch, minus 1/4 inch.

3. Surface:  Gap below 10-foot- long, unleveled straightedge not to exceed 1/4 inch.

4. Lateral Alignment and Spacing of Tie Bars and Dowels:  1 inch.

5. Vertical Alignment of Tie Bars and Dowels:  1/4 inch.

6. Alignment of Tie-Bar End Relative to Line Perpendicular to Pavement Edge:  1/2 inch.

7. Alignment of Dowel-Bar End Relative to Line Perpendicular to Pavement Edge:  Length of dowel 1/4 inch per 12 inches.

8. Joint Spacing:  3 inches.

9. Contraction Joint Depth:  Plus 1/4 inch, no minus.

10. Joint Width:  Plus 1/8 inch, no minus.

3.10 PAVEMENT MARKING

Delete this Article if no pavement marking.

A. Do not apply pavement-marking paint until layout, colors, and placement have been verified with Architect.

B. Allow concrete pavement to cure for 28 days and be dry before starting pavement marking.

C. Sweep and clean surface to eliminate loose material and dust.

D. Apply paint with mechanical equipment to produce pavement markings of dimensions indicated with uniform, straight edges.  Apply at manufacturer's recommended rates to provide a minimum wet film thickness of 15 mils.

3.11 WHEEL STOPS

Delete this Article if no wheel stops.

A. Securely attach wheel stops into pavement with not less than two galvanized steel dowels embedded in holes drilled or cast into wheel stops at one-quarter to one-third points.  Firmly bond each dowel to wheel stop and to pavement.  Securely install dowels into pavement and bond to wheel stop.  Recess head of dowel beneath top of wheel stop.

3.12 FIELD QUALITY CONTROL

Retain first option in paragraph below if Owner engages agency; retain second option if Contractor engages agency.  If retaining second option, retain requirement for field quality-control test reports in Part 1 "Submittals" Article.

A. Testing Agency:  Owner will engage a qualified independent testing and inspecting agency to perform field tests and inspections and prepare test reports.

Revise field quality-control testing in first paragraph and subparagraphs below to suit Project, or delete if not required for smaller work.

B. Testing Services:  Testing of composite samples of fresh concrete obtained according to ASTM C 172 shall be performed according to the following requirements:

Revise frequency of testing in subparagraph below to suit Project.  First option is based on ACI 301, second on ACI 318 (ACI 318M) for slabs.

1. Testing Frequency:  Obtain at least 1 composite sample for each 100 cu. yd.

Retain first subparagraph below with either option in subparagraph above.

a. When frequency of testing will provide fewer than five compressive-strength tests for each concrete mixture, testing shall be conducted from at least five randomly selected batches or from each batch if fewer than five are used.

2. Slump:  ASTM C 143/C 143M; one test at point of placement for each composite sample, but not less than one test for each day's pour of each concrete mix.  Perform additional tests when concrete consistency appears to change.

3. Air Content:  ASTM C 231, pressure method; one test for each composite sample, but not less than one test for each day's pour of each concrete mix.

4. Concrete Temperature:  ASTM C 1064; one test hourly when air temperature is 40 deg F  and below and when 80 deg F and above, and one test for each composite sample.

Revise number of laboratory- or field-cured test specimens below if required.

5. Compression Test Specimens:  ASTM C 31/C 31M; cast and laboratory cure one set of three standard cylinder specimens for each composite sample.

Coordinate number of compression test specimens in subparagraph above with number of compressive-strength tests in subparagraph and associated subparagraph below.

6. Compressive-Strength Tests:  ASTM C 39/C 39M; test 1 specimen at 7 days and 2 specimens at 28 days.

a. A compressive-strength test shall be the average compressive strength from 2 specimens obtained from same composite sample and tested at 28 days.

C. Strength of each concrete mix will be satisfactory if average of any 3 consecutive compressive-strength tests equals or exceeds specified compressive strength and no compressive-strength test value falls below specified compressive strength by more than 500 psi.

D. Test results shall be reported in writing to Architect, concrete manufacturer, and Contractor within 48 hours of testing.  Reports of compressive-strength tests shall contain Project identification name and number, date of concrete placement, name of concrete testing and inspecting agency, location of concrete batch in Work, design compressive strength at 28 days, concrete mixture proportions and materials, compressive breaking strength, and type of break for both 7- and 28-day tests.

E. Nondestructive Testing:  Impact hammer, sonoscope, or other nondestructive device may be permitted by Architect but will not be used as sole basis for approval or rejection of concrete.

F. Additional Tests:  Testing and inspecting agency shall make additional tests of concrete when test results indicate that slump, air entrainment, compressive strengths, or other requirements have not been met, as directed by Architect.

G. Remove and replace concrete pavement where test results indicate that it does not comply with specified requirements.

H. Additional testing and inspecting, at Contractor's expense, will be performed to determine compliance of replaced or additional work with specified requirements.

3.13 REPAIRS AND PROTECTION

A. Remove and replace concrete pavement that is broken, damaged, or defective or that does not comply with requirements in this Section.

B. Drill test cores, where directed by Architect, when necessary to determine magnitude of cracks or defective areas.  Fill drilled core holes in satisfactory pavement areas with portland cement concrete bonded to pavement with epoxy adhesive.

C. Protect concrete from damage.  Exclude traffic from pavement for at least 14 days after placement.  When construction traffic is permitted, maintain pavement as clean as possible by removing surface stains and spillage of materials as they occur.

D. Maintain concrete pavement free of stains, discoloration, dirt, and other foreign material.  Sweep concrete pavement not more than two days before date scheduled for Substantial Completion inspections.

END OF DOCUMENT
CEMENT CONCRETE PAVEMENT

02751 - 3

