LQ


SECTION 04800 

MASONRY ASSEMBLIES

PART 1 GENERAL

1.1 SUMMARY

A. Provide unit masonry construction:

Freestanding site masonry walls.

PART 2 PRODUCTS

2.1 MATERIALS

A. Concrete Masonry Units:

Concrete Masonry Units:  ASTM C 90, 1500 f'm compressive strength:

a. Light weight.

2. Size:  Face dimension of 7-5/8 inches high by 15-5/8 inches long by width required for application.

3. Bond Pattern:  Running Bond.

B. Mortar and Grout for Brick and Concrete Masonry Unit Assemblies:

Mortar Mix:  ASTM C 270, Type S, for reinforced masonry, masonry below grade and masonry in contact with earth and ASTM C 270, Type N, for above-grade loadbearing and nonloadbearing walls and parapet walls and for interior loadbearing and nonloadbearing partitions.

1. Color:  Natural color.

C. Reinforcing Steel:

Reinforcing Bars:  ASTM A 615, Grade 60.

D. Reinforcing:  Welded wire with deformed side rods.

Steel Wire:  9 gauge (.1875 inch) galvanized steel.

1. Type:  Ladder type.

E. Ties and Anchors:

Anchor Bolts:  ASTM A 307, Grade A, galvanized.

1. Post-installed Anchors:  Chemical or expansion anchors.

F. Masonry Accessories:

Preformed control joint gaskets.

1. Bond breaker strips.

2. Cotton sash cord for weeps.

END OF SECTION

MASONRY ASSEMBLIES


04800-1

