
SECTION 05120

STRUCTURAL STEEL

PART 1 GENERAL

1.1 SUMMARY

A. Provide structural steel for building construction including sub-framing units which are part of the general framing system.  Include related anchors, fasteners, and connectors.

PART 2 PRODUCTS

2.1 MATERIALS

A. Steel Materials:

Structural Steel Shapes, Plates, and Bars:  ASTM A 572.

1. Cold-Formed Steel Tubing:  ASTM A 500, Grade B.

2. Hot-Formed Steel Tubing:  ASTM A 501.

3. Anchor Bolts:  ASTM A 307, nonheaded type.

4. Unfinished Threaded Fasteners:  ASTM A 307, Grade A.

5. High-Strength Threaded Fasteners:  ASTM A 325 or ASTM A 490, as applicable.

B. Auxiliary Materials:

Direct Tension Indicators:  ASTM A 959.

1. Electrodes for Welding:  AWS Code.

2. Structural Steel Primer Paint:  SSPC - Paint 13, compatible with topcoats.

3. Cement Grout:  Portland cement, sand.

END OF SECTION


STRUCTURAL STEEL


05120-1

