LQ


SECTION 05510

METAL STAIRS 

PART 1 GENERAL

1.1 SUMMARY

A. Provide steel-framed stairs and handrails.  Steel stairs shall consist of steel channel stringers with steel risers and concrete filled steel pan treads.  Handrails shall be 1-1/4 inch steel pipe handrails and 1/2” vertical pickets at 4 1/2” on center.

PART 2 PRODUCTS

2.1 MATERIALS

A. Materials:

Steel Plates, Shapes, and Bars:  ASTM A 36.

1. Cold-Formed Steel Tubing:  ASTM A 500.

2. Hot-Formed Steel Tubing:  ASTM A 501.

3. Steel Pipe:  ASTM A 53, standard weight (Schedule 40).

4. Rolled Steel Floor Plate:  ASTM A 786.

5. Cold-Rolled Structural Steel Sheet:  ASTM A 611, Grade A.

6. Fasteners:  Plated fasteners, ASTM B 633, zinc-coated.

B. Grout:  Factory-packaged, nonshrink, nonmetallic, ASTM C 1107.  

END OF SECTION


METAL STAIRS 


05510-1

