LQ


SECTION 05720

ORNAMENTAL HANDRAILS AND RAILINGS

PART 1 GENERAL

1.1 SUMMARY

A. Provide ornamental handrails and railings:

Aluminum or stell ornamental handrails and railing systems.

PART 2 PRODUCTS

2.1 MATERIALS

A. Manufacturers: Ametco Manufacturing, Arden Architectural Specialties, Julius Blum & Co., Blumcraft of Pittsburgh, Livers Bronze, Milgo/Bufkin, Zephyr Metals or approved equal.

B. Provide the following:  ornamental handrails shown on design drawings.

C. Aluminum:

Extruded Bar and Tube:  ASTM B 221, alloy 6063 T5/T52.

1. Drawn Seamless Tube:  ASTM B 483, alloy 6063 T832.

2. Castings:  ASTM B 26, alloy A356 T6.

3. Finish:  Baked enamel.

D. Auxiliary Materials:

Welding Electrodes and Filler Metal:  AWS specifications.

1. Fasteners, Anchors, and Inserts:  Non-corrosive.

2. Exterior/Interior Anchoring Cement:  Erosion-resistant hydraulic expansion cement.

END OF SECTION


ORNAMENTAL HANDRAILS AND RAILINGS


05720-1

