

SECTION 09900PRIVATE 


PAINTING

Provisions of the contract including General and Supplementary General Conditions and the General Requirements apply to the work of this section.

1 PART 1 GENERAL


.1

SECTION INCLUDES



A.
Surface preparation and field application of paints and coatings.

 
.2

seq level2 \h \r0 

RELATED SECTIONS




Not used


.3
seq level2 \h \r0 
REFERENCES



A.
ASTM D16 ‑ Definitions of Terms Relating to Paint, Varnish, Lacquer, and Related Products.



B.
NPCA (National Paint and Coatings Association) ‑ Guide to U.S. Government Paint Specifications.



C.
PDCA (Painting and Decorating Contractors of America) -Painting ‑ Architectural Specifications Manual.



D.
Reference to General Conditions.


.4

seq level2 \h \r0 

DEFINITIONS



A.
Conform to ASTM D16 for interpretation of terms used in this Section.


.5

seq level2 \h \r0 

SUBMITTALS



A.
Submit under provisions of Section 01300.



B.
Product Data:  Provide data on all finishing products.



C.
Samples:
Provide samples of each color and materials to be applied with texture to simulate actual conditions on representative samples of the actual substrate. Provide samples defining each separate coat including fillers and primers, use representative colors when preparing for review.



D.
Manufacturer's Instructions:
Indicate special surface preparation procedures, substrate conditions requiring special attention.


.6

seq level2 \h \r0 

QUALIFICATIONS



A.
Manufacturer:  Company specializing in manufacturing the Products specified in this section with minimum three years documented experience.



B.
Applicator:  Company specializing in performing the work of this section with minimum 3 years-documented experience.


.7

seq level2 \h \r0 
 
REGULATORY REQUIREMENTS



A.
Conform to applicable code for flame and smoke rating requirements for finishes.


.8

seq level2 \h \r0 

FIELD SAMPLES



A.
Accepted sample may not remain as part of the Work.


.9

seq level2 \h \r0 

DELIVERY, STORAGE, AND HANDLING





A.
Deliver products to site in sealed and labeled containers; inspect to verify acceptability.



A.
Container label to include manufacturer's name, type of paint, brand name, lot number, brand code, coverage, surface preparation, drying time, cleanup requirements, color designation, and instructions for mixing and reducing.



B.
Store paint materials at minimum ambient temperature of 45 degrees F (7 degrees C) and a maximum of 90 degrees F (32 degrees C), in ventilated area, and as required by manufacturer's instructions.


.10

seq level2 \h \r0 
ENVIRONMENTAL REQUIREMENTS



A.
Do not apply materials when surface and ambient temperatures are outside the temperature ranges required by the paint product manufacturer.




B.
Minimum Application Temperatures for Latex Paints:  45 degrees F for interiors; 50 degrees F for exterior; unless required otherwise by manufacturer's instructions.



B.
Provide lighting level of 80-ft candles measured mid‑height at substrate surface.


.11

seq level2 \h \r0 
EXTRA MATERIALS






Not Used

2

seq level1 \h \r0 

seq level2 \h \r0  PART 2 PRODUCTS


.1

MANUFACTURERS



A.
Manufacturers ‑ Paint




1.
[ Sherwin Williams] 




2.
[ Devo            ] 




3.
[ Benjamin Moore  ] 


.2

seq level2 \h \r0 

MATERIALS



A.
Primers: Latex based interior white primer used on interior gypsum drywall under a flat latex paint.



B.
Coatings:  Ready mixed latex based paint for use as a flat finish over prime coated gypsum drywall. Process pigments to a soft paste consistency, capable of being readily and uniformly dispersed to a homogeneous coating; good flow and brushing properties; capable of drying or curing free of streaks or sags.



C.
Accessory Materials:
Linseed oil, shellac, turpentine, paint thinners and other materials not specifically indicated but required to achieve the finishes specified, of commercial quality.



D.
Patching Materials:  Latex filler.



E.
Fastener Head Cover Materials:
Latex filler.


.3

seq level2 \h \r0 

FINISHES



A.
Refer to schedule at end of section for surface finish and color schedule.

3

seq level1 \h \r0 

seq level2 \h \r0  PART 3 EXECUTION


.1

EXAMINATION



A.
Verify site conditions.



B.
Verify that surfaces are ready to receive work as instructed by the product manufacturer.



C.
Examine surfaces scheduled to be finished prior to commencement of work.  Report any condition that may potentially affect proper application.



D.
Measure moisture content of surfaces using an electronic moisture meter.  Do not apply finishes unless moisture content of surfaces are below the following maximums:




4.
Plaster and Gypsum Wallboard:  12 percent.




5.
Masonry, Concrete, and Concrete Unit Masonry:  [12] percent.




6.
Interior Wood:  15 percent, measured in accordance with ASTM D2016.




7.
Exterior Wood:  15 percent, measured in accordance with ASTM D2016.




8.
Concrete Floors:  8 percent.


.2

seq level2 \h \r0 

seq level3 \h \r0 

PREPARATION



A.
Remove or mask electrical plates, hardware, light fixture trim, escutcheons, and fittings prior to preparing surfaces or finishing.



B.
Correct defects and clean surfaces which affect work of this section.  Remove existing coatings that exhibit loose surface defects.



C.
Seal with shellac and seal marks which may bleed through surface finishes.



D.
Impervious Surfaces:
Remove mildew by scrubbing with solution of tri‑sodium phosphate and bleach.  Rinse with clean water and allow surface to dry.



E.
Gypsum Board Surfaces:  Fill minor defects with filler compound.  Spot prime defects after repair.



F.
Plaster Surfaces:  Fill hairline cracks, small holes, and imperfections with latex patching plaster.  Make smooth and flush with adjacent surfaces.  Wash and neutralize high alkali surfaces.


.3

seq level2 \h \r0 

APPLICATION



A.
Apply products in accordance with manufacturer's instructions.



B.
Do not apply finishes to surfaces that are not dry or over dirt grease, scuffed surfaces or conditions detrimental to formation of a durable paint film.



C.
Apply each coat to uniform finish.



D.
Vacuum clean surfaces free of loose particles.  Use tack cloth just prior to applying next coat.



E.
Allow applied coat to dry before next coat is applied.


.4

seq level2 \h \r0 

FINISHING MECHANICAL AND ELECTRICAL EQUIPMENT



A.
Reinstall electrical cover plates, hardware, light fixture trim, escutcheons, and fittings removed prior to finishing.


.5
seq level2 \h \r0 
FIELD QUALITY CONTROL



A.
Field inspection and testing will be performed under provisions of Section 01400.



B.
Test questionable coated areas.


.6

seq level2 \h \r0 

CLEANING



A.
Clean work thoroughly.



B.
Collect waste material, which may constitute a fire hazard, place in closed metal containers and remove daily from site.


.7

seq level2 \h \r0 

SCHEDULE ‑ SHOP PRIMED ITEMS FOR SITE FINISHING




Not Used


.8

seq level2 \h \r0 

SCHEDULE ‑ EXTERIOR SURFACES




Not Used


seq level3 \h \r0 

seq level3 \h \r0 



.9

seq level2 \h \r0 

seq level3 \h \r0 

SCHEDULE ‑ INTERIOR SURFACES

A. Gypsum Drywall System 




Flat Emulsion Finish 2 coats





Primer Latex Based Interior White Primer





Final Coat: Latex Based Interior Paint 



.10

seq level2 \h \r0 

seq level3 \h \r0 
SCHEDULE ‑ COLORS



A.
Match existing colors for all new surfaces and with touch up.

B. Match existing colors from existing walls.  Assure that patching or existing plaster, etc. has been accomplished prior to painting.


END OF SECTION


09900
PAGE  
Section 09900 Page 5 of 5

