554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

Fax: 985-641-5950

dammonengineering.com

dammoneng@bellsouth.net

# Structural Inspection

March 5, 2015

For: 	Josh Gardner

Branch Manger

Power Mortgage

1349 Corporate Square Blvd.

Suite 2

Slidell, LA. 70458

Ref:     109 Millbrook Lane

Carriere, MS.

Construction:

Single-story, wood frame with brick/vinyl veneer and composition shingle roof on a conventional foundation

Scope:

This inspection is limited to a visual inspection of the exterior foundation of the residence.  No inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers Standards and Practices for Residential and Small Building Property Condition Surveys.  This report is not an explanation of cause, effect, or engineering.

History:

Josh Gardner with Power Mortgage contacted Dammon Engineering requesting a structural inspection of the referenced home. An appraisal inspection report noted cracks in the foundation.

Findings:

There is one surface crack in the foundation on the front left side of the exterior of the home.  These types of surface cracks are from when the form boards are removed improperly. The addition in the rear of the home you can see was added onto existing foundations to create one and the seams were noted.

Conclusion:

The surface crack in the foundation does not appear to have compromised the structural integrity of the home; there are no visible mortar cracks or cracked bricks that were noted. It is my opinion that the structural integrity of this home is currently sound.

The rebar should be cut back and the surface crack of the foundation on the left front side of the home should be filled. The joints of the foundation addition in the rear of the home should be sealed with a non-shrinking grout to prevent insects from entering the home.

Sincerely,

Brian A. Mistich, P.E.

PE:20971