554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

November 19, 2020

For: 	Ricky Smith

53021 Hwy 433

Slidell La. 70461

Construction:

Raised on pilings, one-story, wood frame, Vinyl veneer, ceramic and wood flooring with a composition shingle roof. Home is approximately 13 years old.

Scope:

This inspection is limited to a visual inspection of the shell of the home, including the interior and exterior foundation of the home. No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to request a structural inspection from the purchaser to inspect the pilings and wood decks prior to purchasing.

Findings:

An overall visual inspection at the base of the pilings appears to be solid. The base of the pilings are wrapped in felt and enclosed in a concrete slab, over time the concrete has cracked and are exposing the pilings base to the elements.

An overall inspection of the front porch noted some rotten wood on the 2x8 floor joist, deterioration of handrails and the 6x6 support post are warping.  The rear deck/porch handrails are loose and showing signs of deterioration with the deck losing its torch down roofing. The pilings supporting it are overall good except one is rotting from the inside out from rainwater.

Recommendation:

It is my opinion that the structural integrity of this home is currently sound, but will deteriorate if not addressed as noted below.

Items to be addressed are as follows:

1)  Replace the concrete slab to create a level surface for walking and seal around the pilings to keep water from intruding.

2)   Replace all the rotten wood on the front porch and replace 6x6 supports and secure the handrails to the home.

3)  Cap and seal the tops of all the pilings on the rear decking and replace the roof covering to make a   complete sealed system.

Sincerely,

Brian Mistich, P.E.