
SECTION 06112PRIVATE 


REPAIRS TO EXTERIOR WALLS

1 PART 1 GENERAL


.1
SECTION INCLUDES



A.
WALL REPAIRS

In addition to work of installing vinyl siding, the following work to repair the substrate shall be accomplished.




1.01
SCOPE

Provide all labor, material and equipment to repair areas of rot or other damage listed by square footages later in this section.


.2
PRODUCTS FURNISHED BUT NOT INSTALLED UNDER THIS SECTION


.
Not Used


.3
RELATED SECTIONS



Not Used


.4
REFERENCES



A.
ALSC - American Lumber Standards Committee:  Softwood Lumber Standards.



B.
ANSI A208.1 – Mat-Formed Wood Particleboard.



C.
AWPA (American Wood Preservers Association) C1 - All Timber Products Preservative Treatment by Pressure Process.



D.
AWPA (American Wood Preservers Association) C20 -Structural Lumber Fire Retardant Treatment by Pressure Process.



E.
NFPA:  National Forest Products Association.



F.
RIS:  Redwood Inspection Service.



G.
SPIB:  Southern Pine Inspection Bureau.


.5
SUBMITTALS



Not Used


.6
QUALITY ASSURANCE



Not Used


.7
DELIVERY, STORAGE, AND HANDLING



A.
Deliver, store, protect, and handle products to site under provisions of Section 01600.



B.
Protect site framed structural site fabricated trusses from warping or other distortion by stacking in vertical position, braced to resist movement.

2 PART 2 PRODUCTS


.1
LUMBER MATERIALS

A. Material shall be new and unused.

B. All lumber surfaces exposed to the weather shall be treated.

C. Studs and other framing shall be Construction Grade Southern Yellow Pine.

D. Sheathing shall be ½” OSB, or ½” Plywood Sheathing, exterior grade, or replace with siding of existing type and size.

E. Vapor barrier shall be .005 PVC.

(Note that use of sheathing must not change the appearance of the new vinyl siding being installed.)

F. Lumber Grading Rules: SPIB.

G. Joist Framing: 19 percent maximum moisture content.
H. Non-structural Light Framing: SYP species, 19 percent maximum moisture content.
I. Studding:  Stress Group SYP species, 19 percent maximum moisture content.
J. Framing in contact with foundation: Pressure treated SYP.
A. Miscellaneous Framing: SYP species, 19 percent maximum moisture content.

.2
SHEATHING MATERIALS

B. 

Not Used


.3
UNDERLAYMENT MATERIALS
C. 

Not Used


.4
ACCESSORIES

D. 

A.
Moisture barrier (.005” PVC)

3 PART 3 EXECUTION


.1
FRAMING

E. Remove all damaged siding, or remove siding as required to reach areas that require repairs.  Siding that is not damaged beyond use may be reused.

F. Where studs are partially rotted, remove area of rot.  Install full height stud on side of existing stud (scab) and nail (stagger 12D common nails at 12” o.c. minimum.).

G. Where damage is greater than the square footage estimates shown in this specification, notify owner for determination.  (See Proposal Document for price per square foot of wall repair beyond the square footages listed in this specification (base bid).

H. Place horizontal members flat, crown side up.
I. Double members at openings over [24] inches wide.  Space short studs over and under opening to stud spacing.
J. Construct double joist headers at floor and ceiling openings and under wall stud partitions that are parallel to floor joists.  Frame rigidly into joists.

.2
SHEATHING



A.
Secure sheathing perpendicular to framing members with ends staggered and sheet ends over firm bearing.  Use sheathing clips between sheets between roof framing members.



B.
Secure wall sheathing with long dimension perpendicular to wall studs, with ends over firm bearing and staggered.



C.
Place building paper horizontally over wall sheathing, weather lap edges and ends.


.3
SITE APPLIED WOOD TREATMENT



Not Used


.4
TOLERANCES



Not Used

END OF SECTION

PAGE  
Section 06112 Page 2 of 3
Error! Main Document Only.

