ST. TAMMANY FIRE PROTECTION DISTRICT NO. 1

FIRE STATION #19

57047 ALLEN ROAD

SLIDELL LA  70461


Copyright 2003 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 079200
JOINT SEALANTS
GLASS UNIT MASONRY ASSEMBLIES This Section uses the term "Architect."  Change this term as necessary to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

Copyright 2003 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

Copyright 2001 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

Retain second option in paragraph below if other Sections refer to this Section for sealant-related requirements.

A. This Section includes joint sealants for the following applications, including those specified by reference to this Section:

Adjust list below to suit Project or delete if retaining the Joint-Sealant Schedule at the end of Part 3.  List summarizes typical sealant joints; if retained, complement with schedules, details, and designations on Drawings indicating exactly what products are required and where.

1. Exterior joints in the following vertical surfaces and horizontal nontraffic surfaces:

a. Construction joints in cast-in-place concrete.

b. Joints in glass unit masonry assemblies.

c. Joints between metal panels.

d. Joints between different materials listed above.

e. Perimeter joints between materials listed above and frames of doors, windows and louvers.

f. Control and expansion joints.

g. Other joints as indicated.

Joints in first subparagraph and associated subparagraphs below cover traffic surfaces that are part of a building and not those in roads, sidewalks, and parking lots, which should be specified in Division 2 Section "Pavement Joint Sealants."

2. Exterior joints in the following horizontal traffic surfaces:

a. Isolation and contraction joints in cast-in-place concrete slabs.

b. Tile control and expansion joints.

c. Joints between different materials listed above.

d. Other joints as indicated.

3. Interior joints in the following vertical surfaces and horizontal nontraffic surfaces:

a. Control and expansion joints on exposed interior surfaces of exterior walls.

b. Perimeter joints of exterior openings where indicated.

c. Tile control and expansion joints.

d. Vertical joints on exposed surfaces of walls and partitions.

e. Perimeter joints between interior wall surfaces and frames of interior doors, windows.

f. Joints between plumbing fixtures and adjoining walls, floors, and counters.

g. Other joints as indicated.

4. Interior joints in the following horizontal traffic surfaces:

a. Isolation joints in cast-in-place concrete slabs.

b. Control and expansion joints in tile flooring.

c. Other joints as indicated.

1.3 PERFORMANCE REQUIREMENTS

A. Provide elastomeric joint sealants that establish and maintain watertight and airtight continuous joint seals without staining or deteriorating joint substrates.

Delete paragraph above or below if not applicable.  Revise wording to reflect performance required for both interior and exterior joints.  Add specific applications where watertight or water-resistant performance may not be required or attainable with products selected.

B. Provide joint sealants for interior applications that establish and maintain airtight and water-resistant continuous joint seals without staining or deteriorating joint substrates.

1.4 SUBMITTALS

A. Product Data:  For each joint-sealant product indicated.

B. Samples for Initial Selection:  Manufacturer's color charts consisting of strips of cured sealants showing the full range of colors available for each product exposed to view.

Delete paragraph above if colors are preselected and specified or scheduled.  Retain first paragraph below with or without above.

C. Samples for Verification:  For each type and color of joint sealant required, provide Samples with joint sealants in 1/2-inch- wide joints formed between two 6-inch- long strips of material matching the appearance of exposed surfaces adjacent to joint sealants.

D. Product Certificates:  For each type of joint sealant and accessory, signed by product manufacturer.

Delete paragraph below if subparagraph requiring testing to obtain SWRI validation is not retained in "Quality Assurance" Article.

E. SWRI Validation Certificate:  For each elastomeric sealant specified to be validated by SWRI's Sealant Validation Program.

Correlate test reports below with testing requirements in "Quality Assurance" Article, or delete if no test reports are required for Project.

F. Preconstruction Field Test Reports:  Indicate which sealants and joint preparation methods resulted in optimum adhesion to joint substrates based on preconstruction testing specified in "Quality Assurance" Article.

Delete paragraph above and first paragraph and subparagraphs below if testing described is not required elsewhere in this Section.

G. Compatibility and Adhesion Test Reports:  From sealant manufacturer, indicating the following:

1. Materials forming joint substrates and joint-sealant backings have been tested for compatibility and adhesion with joint sealants.

2. Interpretation of test results and written recommendations for primers and substrate preparation needed for adhesion.

H. Field Test Report Log:  For each elastomeric sealant application.

I. Product Test Reports:  Based on comprehensive testing of product formulations performed by a qualified testing agency, indicating that sealants comply with requirements.

J. Warranties:  Special warranties specified in this Section.

1.5 QUALITY ASSURANCE

If a manufacturer's warranty is specified requiring manufacturer's approval or licensing of Installer, retain first paragraph below.

A. Installer Qualifications:  Manufacturer's authorized Installer who is approved or licensed for installation of elastomeric sealants required for this Project.

B. Source Limitations:  Obtain each type of joint sealant through one source from a single manufacturer.

C. Preconstruction Compatibility and Adhesion Testing:  Submit to joint-sealant manufacturers, for testing indicated below, samples of materials that will contact or affect joint sealants.

1. Use ASTM C 1087 or manufacturer's standard test method to determine whether priming and other specific joint preparation techniques are required to obtain rapid, optimum adhesion of joint sealants to joint substrates.

2. Submit pieces of each type of material, including joint substrates, shims, joint-sealant backings, secondary seals, and miscellaneous materials.

3. Schedule sufficient time for testing and analyzing results to prevent delaying the Work.

4. For materials failing tests, obtain joint-sealant manufacturer's written instructions for corrective measures including use of specially formulated primers.

Retain subparagraph below only if sealant installation is not critical.

5. Testing will not be required if joint-sealant manufacturers submit joint preparation data that are based on previous testing of current sealant products for adhesion to, and compatibility with, joint substrates and other materials matching those submitted.

D. Product Testing:  Obtain test results for "Product Test Reports" Paragraph in "Submittals" Article from a qualified testing agency based on testing current sealant formulations within a 36-month period preceding the commencement of the Work.

1. Testing Agency Qualifications:  An independent testing agency qualified according to ASTM C 1021 to conduct the testing indicated, as documented according to ASTM E 548.

If retaining subparagraph below, also retain "Product Test Reports" Paragraph in "Submittals" Article.

2. Test elastomeric joint sealants for compliance with requirements specified by reference to ASTM C 920, and where applicable, to other standard test methods.

If retaining subparagraph below, also retain "SWRI Validation Certificate" Paragraph in "Submittals" Article.  Verify availability of SWRI sealant validation for products selected.

3. Test elastomeric joint sealants according to SWRI's Sealant Validation Program for compliance with requirements specified by reference to ASTM C 920 for adhesion and cohesion under cyclic movement, adhesion-in-peel, and indentation hardness.

Retain subparagraph below for nonelastomeric sealants.

4. Test other joint sealants for compliance with requirements indicated by referencing standard specifications and test methods.

E. Preconstruction Field-Adhesion Testing:  Before installing elastomeric sealants, field test their adhesion to Project joint substrates as follows:

1. Locate test joints where indicated on Project or, if not indicated, as directed by Architect.

2. Conduct field tests for each application indicated below:

Revise list below to suit Project.

a. Each type of elastomeric sealant and joint substrate indicated.

b. Each type of nonelastomeric sealant and joint substrate indicated.

3. Notify Architect seven days in advance of dates and times when test joints will be erected.

Delete subparagraph below if not required.  Before retaining, determine availability of manufacturer's representative.

4. Arrange for tests to take place with joint-sealant manufacturer's technical representative present.

Method below is the first of four test methods recommended in Appendix X1.1 in ASTM C 1193.  Revise if one of the other three test methods is more appropriate for Project joint conditions.

a. Test Method:  Test joint sealants according to Method A, Field-Applied Sealant Joint Hand Pull Tab, in Appendix X1 in ASTM C 1193.

1) For joints with dissimilar substrates, verify adhesion to each substrate separately; extend cut along one side, verifying adhesion to opposite side.  Repeat procedure for opposite side.

5. Report whether sealant in joint connected to pulled-out portion failed to adhere to joint substrates or tore cohesively.  Include data on pull distance used to test each type of product and joint substrate.  For sealants that fail adhesively, retest until satisfactory adhesion is obtained.

6. Evaluation of Preconstruction Field-Adhesion-Test Results:  Sealants not evidencing adhesive failure from testing, in absence of other indications of noncompliance with requirements, will be considered satisfactory.  Do not use sealants that fail to adhere to joint substrates during testing.

Delete paragraph and subparagraph below if not required.  Coordinate with panel mockups specified in other Sections that include sealant joints.  If retaining, indicate location, size, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

F. Mockups:  Build mockups incorporating sealant joints, as follows, to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution:

Revise subparagraph below to suit Project.

1. Joints in mockups of assemblies specified in other Sections that are indicated to receive elastomeric joint sealants, which are specified by reference to this Section.

Delete below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 1.

G. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination."

1.6 PROJECT CONDITIONS

A. Do not proceed with installation of joint sealants under the following conditions:

1. When ambient and substrate temperature conditions are outside limits permitted by joint-sealant manufacturer or are below 40 deg F.

2. When joint substrates are wet.

3. Where joint widths are less than those allowed by joint-sealant manufacturer for applications indicated.

4. Contaminants capable of interfering with adhesion have not yet been removed from joint substrates.

1.7 WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this Article are not less than remedies available to Owner under prevailing local laws.  Coordinate with Division 1 Section "Product Requirements."

A. Special Installer's Warranty:  Installer's standard form in which Installer agrees to repair or replace elastomeric joint sealants that do not comply with performance and other requirements specified in this Section within specified warranty period.

Verify available warranties and insert number below.

1. Warranty Period:  Two years from date of Substantial Completion.

B. Special Manufacturer's Warranty:  Manufacturer's standard form in which elastomeric sealant manufacturer agrees to furnish elastomeric joint sealants to repair or replace those that do not comply with performance and other requirements specified in this Section within specified warranty period.

Verify available warranties and insert number below.

1. Warranty Period:  Two years from date of Substantial Completion.

C. Special warranties specified in this Article exclude deterioration or failure of elastomeric joint sealants from the following:

1. Movement of the structure resulting in stresses on the sealant exceeding sealant manufacturer's written specifications for sealant elongation and compression caused by structural settlement or errors attributable to design or construction.

2. Disintegration of joint substrates from natural causes exceeding design specifications.

3. Mechanical damage caused by individuals, tools, or other outside agents.

4. Changes in sealant appearance caused by accumulation of dirt or other atmospheric contaminants.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

See Editing Instructions No. 1 and No. 2 in the Evaluations for cautions about naming manufacturers and products and in coordinating requirements in this Section with other Part 2 articles.

A. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, products listed in other Part 2 articles.

2.2 MATERIALS, GENERAL

A. Compatibility:  Provide joint sealants, backings, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by sealant manufacturer, based on testing and field experience.

Retain paragraph and subparagraphs below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  Coordinate product selection in other Part 2 articles to be sure that products selected comply.

B. VOC Content of Interior Sealants:  Provide sealants and sealant primers for use inside the weatherproofing system that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

1. Architectural Sealants:  250 g/L.

2. Nonmembrane Roof Sealants:  300 g/L.

3. Single-Ply Roof Membrane Sealants:  450 g/L.

4. Sealant Primers for Nonporous Substrates:  250 g/L.

5. Sealant Primers for Porous Substrates:  775 g/L.

6. Modified Bituminous Sealant Primers:  500 g/L.

Delete below if sealant colors are specified in the Joint-Sealant Schedule at the end of Part 3 or on Drawings.

C. Colors of Exposed Joint Sealants: As selected by Architect from manufacturer's full range.

2.3 ELASTOMERIC JOINT SEALANTS

Retain paragraph below with entries in remainder of this Article.  See Editing Instruction No. 2 in the Evaluations.

A. Elastomeric Sealants:  Comply with ASTM C 920 and other requirements indicated for each liquid-applied chemically curing sealant specified, including those referencing ASTM C 920 classifications for type, grade, class, and uses related to exposure and joint substrates.

Generally retain paragraph below with silicones applied to porous substrates such as marble, limestone, granite, and sandstone.

B. Stain-Test-Response Characteristics:  Where elastomeric sealants are specified to be nonstaining to porous substrates, provide products that have undergone testing according to ASTM C 1248 and have not stained porous joint substrates indicated for Project.

Delete paragraph below if no sealants are indicated for Use I.  Revise if a liquid other than water is used in testing.

C. Suitability for Immersion in Liquids.  Where elastomeric sealants are indicated for Use I for joints that will be continuously immersed in liquids, provide products that have undergone testing according to ASTM C 1247 and qualify for the length of exposure indicated by reference to ASTM C 920 for Class 1 or 2.  Liquid used for testing sealants is deionized water, unless otherwise indicated.

Delete paragraph below if no sealants are indicated for applications where sealants will come in contact with food.  Indicate on Drawings or by inserts which products must comply with this requirement.

D. Suitability for Contact with Food:  Where elastomeric sealants are indicated for joints that will come in repeated contact with food, provide products that comply with 21 CFR 177.2600.

E. Preformed Foam Sealant:  Manufacturer's standard preformed, precompressed, open-cell foam sealant that is manufactured from high-density urethane foam impregnated with a nondrying, water-repellent agent; is factory produced in precompressed sizes in roll or stick form to fit joint widths indicated; is coated on one side with a pressure-sensitive adhesive and covered with protective wrapping; develops a watertight and airtight seal when compressed to the degree specified by manufacturer; and complies with the following:

1. Available Products:

a. EMSEAL Joint Systems, Ltd.; Emseal 25V.

b. illbruck Sealant Systems, Inc.; Wilseal 600.

c. Polytite Manufacturing Corporation; Polytite B.

"Polytite B" above differs from "Polytite Standard" below by having a coating on one face that acts as a bond breaker for sealant.

d. Polytite Manufacturing Corporation; Polytite Standard.

e. Sandell Manufacturing Co., Inc.; Polyseal.

2. Properties:  Permanently elastic, mildew resistant, nonmigratory, nonstaining, and compatible with joint substrates and other joint sealants.

2.4 PREFORMED TAPE SEALANTS

Preformed tape sealants in this Article are intended primarily for glazing of vision lites and spandrel panels and are also covered in Division 8 Section "Glazing."

A. Back-Bedding Mastic Tape Sealant:  Preformed, butyl-based elastomeric tape sealant with a solids content of 100 percent; nonstaining and nonmigrating in contact with nonporous surfaces; with or without spacer rod as recommended in writing by tape manufacturers for application indicated; packaged on rolls with a release paper backing; and complying with ASTM C 1281 and AAMA 800 for products indicated below:

Retain one or more of three back-bedding tapes below, which are primarily intended for glazing applications.  AAMA 804.3 tape is for less-severe applications.  AAMA 806.3 tape is for high-performance commercial applications involving continuous pressure.  AAMA 807.3 tape is for commercial applications not involving continuous pressure from gaskets and stop designs.

1. AAMA 804.3 tape, where indicated.

2. AAMA 806.3 tape, for applications in which tape is subject to continuous pressure.

3. AAMA 807.3 tape, for applications in which tape is not subject to continuous pressure.

B. Expanded Cellular Tape Sealant:  Closed-cell, PVC foam tape sealant; factory coated with adhesive on both surfaces; packaged on rolls with release liner protecting adhesive; and complying with AAMA 800 for the following types:

1. Type 1, for applications in which tape acts as the primary sealant.

2. Type 2, for applications in which tape is used in combination with a full bead of liquid sealant.

2.5 JOINT-SEALANT BACKING

A. General:  Provide sealant backings of material and type that are nonstaining; are compatible with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by sealant manufacturer based on field experience and laboratory testing.

Retain one of three types in paragraph below; if retaining more than one, also retain fourth option.  Type B products are "Sof Rod" by Nomaco and "Soft Backer Rod" by Sonneborn.  Verify with joint-sealant manufacturers the suitability of each material for sealants selected.  Type O sealant backings, which are open-cell urethane foams, are unsuitable for horizontal surfaces.  See Evaluations.

B. Cylindrical Sealant Backings:  ASTM C 1330, Type C (closed-cell material with a surface skin) or any of the preceding types, as approved in writing by joint-sealant manufacturer for joint application indicated, and of size and density to control sealant depth and otherwise contribute to producing optimum sealant performance:

Retain first paragraph below or revise to suit Project.  Tubing is sometimes used as a temporary seal and secondary water barrier.  Verify with joint-sealant manufacturers the suitability of tubing for sealants selected.  See Evaluations.

C. Elastomeric Tubing Sealant Backings:  Neoprene, butyl, EPDM, or silicone tubing complying with ASTM D 1056, nonabsorbent to water and gas, and capable of remaining resilient at temperatures down to minus 26 deg F.  Provide products with low compression set and of size and shape to provide a secondary seal, to control sealant depth, and to otherwise contribute to optimum sealant performance.

D. Bond-Breaker Tape:  Polyethylene tape or other plastic tape recommended by sealant manufacturer for preventing sealant from adhering to rigid, inflexible joint-filler materials or joint surfaces at back of joint where such adhesion would result in sealant failure.  Provide self-adhesive tape where applicable.

2.6 MISCELLANEOUS MATERIALS

Generally retain first paragraph below unless it is known that priming of substrates is not required with sealants specified.  Purpose of primers is to improve adhesion of sealant to substrate.

A. Primer:  Material recommended by joint-sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from preconstruction joint-sealant-substrate tests and field tests.

B. Cleaners for Nonporous Surfaces:  Chemical cleaners acceptable to manufacturers of sealants and sealant backing materials, free of oily residues or other substances capable of staining or harming joint substrates and adjacent nonporous surfaces in any way, and formulated to promote optimum adhesion of sealants to joint substrates.

C. Masking Tape:  Nonstaining, nonabsorbent material compatible with joint sealants and surfaces adjacent to joints.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine joints indicated to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint-sealant performance.

B. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. Surface Cleaning of Joints:  Clean out joints immediately before installing joint sealants to comply with joint-sealant manufacturer's written instructions and the following requirements:

1. Remove all foreign material from joint substrates that could interfere with adhesion of joint sealant, including dust, paints (except for permanent, protective coatings tested and approved for sealant adhesion and compatibility by sealant manufacturer), old joint sealants, oil, grease, waterproofing, water repellents, water, surface dirt, and frost.

2. Clean porous joint substrate surfaces by brushing, grinding, blast cleaning, mechanical abrading, or a combination of these methods to produce a clean, sound substrate capable of developing optimum bond with joint sealants.  Remove loose particles remaining after cleaning operations above by vacuuming or blowing out joints with oil-free compressed air.  Porous joint substrates include the following:

Delete porous substrates below if not applicable.  Insert additional items to suit Project.

a. Concrete.

b. Masonry.

c. Unglazed surfaces of ceramic tile.

3. Remove laitance and form-release agents from concrete.

4. Clean nonporous surfaces with chemical cleaners or other means that do not stain, harm substrates, or leave residues capable of interfering with adhesion of joint sealants.  Nonporous joint substrates include the following:

Delete nonporous substrates below if not applicable.  Insert additional items to suit Project.

a. Metal.

b. Glass.

c. Porcelain enamel.

d. Glazed surfaces of ceramic tile.

As previously noted in "Miscellaneous Materials" Article, purpose of primers is to improve adhesion of sealant to substrate.

B. Joint Priming:  Prime joint substrates , where recommended in writing by joint-sealant manufacturer, based on preconstruction joint-sealant-substrate tests or prior experience.  Apply primer to comply with joint-sealant manufacturer's written instructions.  Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

Delete below if not required.

C. Masking Tape:  Use masking tape where required to prevent contact of sealant with adjoining surfaces that otherwise would be permanently stained or damaged by such contact or by cleaning methods required to remove sealant smears.  Remove tape immediately after tooling without disturbing joint seal.

3.3 INSTALLATION OF JOINT SEALANTS

A. General:  Comply with joint-sealant manufacturer's written installation instructions for products and applications indicated, unless more stringent requirements apply.

B. Sealant Installation Standard:  Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

Delete first paragraph below only if use of acoustical sealants is specified in other Sections without reference to this Section.

C. Acoustical Sealant Application Standard:  Comply with recommendations in ASTM C 919 for use of joint sealants in acoustical applications as applicable to materials, applications, and conditions indicated.

D. Install sealant backings of type indicated to support sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

1. Do not leave gaps between ends of sealant backings.

2. Do not stretch, twist, puncture, or tear sealant backings.

3. Remove absorbent sealant backings that have become wet before sealant application and replace them with dry materials.

Retain first paragraph below for sealants installed in moving joints without sealant backings.

E. Install bond-breaker tape behind sealants where sealant backings are not used between sealants and backs of joints.

F. Install sealants using proven techniques that comply with the following and at the same time backings are installed:

1. Place sealants so they directly contact and fully wet joint substrates.

2. Completely fill recesses in each joint configuration.

3. Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

G. Tooling of Nonsag Sealants:  Immediately after sealant application and before skinning or curing begins, tool sealants according to requirements specified below to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint.

1. Remove excess sealant from surfaces adjacent to joints.

2. Use tooling agents that are approved in writing by sealant manufacturer and that do not discolor sealants or adjacent surfaces.

Retain one or more of three subparagraphs and associated subparagraph below to suit joint configurations required for Project.  First subparagraph makes concave configuration the default requirement; second and third subparagraphs and associated subparagraph require that other configurations be indicated on Drawings.  Revise if one of the latter two configurations needs to become the default requirement.

3. Provide concave joint configuration per Figure 5A in ASTM C 1193, unless otherwise indicated.

4. Provide flush joint configuration where indicated per Figure 5B in ASTM C 1193.

5. Provide recessed joint configuration of recess depth and at locations indicated per Figure 5C in ASTM C 1193.

a. Use masking tape to protect surfaces adjacent to recessed tooled joints.

H. Installation of Preformed Tapes:  Install according to manufacturer's written instructions.

I. Installation of Preformed Silicone-Sealant System:  Comply with the following requirements:

1. Apply masking tape to each side of joint, outside of area to be covered by sealant system.

2. Apply silicone sealant to each side of joint to produce a bead of size complying with preformed silicone-sealant system manufacturer's written instructions and covering a bonding area of not less than 3/8 inch.  Hold edge of sealant bead 1/4 inch inside masking tape.

3. Within 10 minutes of sealant application, press silicone extrusion into sealant to wet extrusion and substrate.  Use a roller to apply consistent pressure and ensure uniform contact between sealant and both extrusion and substrate.

4. Complete installation of sealant system in horizontal joints before installing in vertical joints.  Lap vertical joints over horizontal joints.  At ends of joints, cut silicone extrusion with a razor knife.

J. Installation of Preformed Foam Sealants:  Install each length of sealant immediately after removing protective wrapping, taking care not to pull or stretch material, producing seal continuity at ends, turns, and intersections of joints.  For applications at low ambient temperatures where expansion of sealant requires acceleration to produce seal, apply heat to sealant in compliance with sealant manufacturer's written instructions.

3.4 FIELD QUALITY CONTROL

Revise first paragraph and associated subparagraphs below if Owner engages an independent testing agency to perform tests.  Testing described below is generally required by sealant manufacturer if warranty is required.

A. Field-Adhesion Testing:  Field test joint-sealant adhesion to joint substrates as follows:

1. Extent of Testing:  Test completed elastomeric sealant joints as follows:

a. Perform 1 test for each 1000 feet of joint length thereafter or 1 test per each floor per elevation.

Method A below is the first of four test methods recommended in Appendix X1.1 in ASTM C 1193.  Retain one or more of the other three test methods if more appropriate for Project joint conditions, and include optional text ", as appropriate for type of joint-sealant application indicated."

2. Test Method:  Test joint sealants according to as appropriate for type of joint-sealant application indicated.

a. For joints with dissimilar substrates, verify adhesion to each substrate separately; do this by extending cut along one side, verifying adhesion to opposite side.  Repeat procedure for opposite side.

3. Inspect joints for complete fill, for absence of voids, and for joint configuration complying with specified requirements.  Record results in a field-adhesion-test log.

4. Inspect tested joints and report on the following:

a. Whether sealants in joints connected to pulled-out portion failed to adhere to joint substrates or tore cohesively.  Include data on pull distance used to test each type of product and joint substrate.  Compare these results to determine if adhesion passes sealant manufacturer's field-adhesion hand-pull test criteria.

b. Whether sealants filled joint cavities and are free of voids.

c. Whether sealant dimensions and configurations comply with specified requirements.

5. Record test results in a field-adhesion-test log.  Include dates when sealants were installed, names of persons who installed sealants, test dates, test locations, whether joints were primed, adhesion results and percent elongations, sealant fill, sealant configuration, and sealant dimensions.

6. Repair sealants pulled from test area by applying new sealants following same procedures used originally to seal joints.  Ensure that original sealant surfaces are clean and that new sealant contacts original sealant.

B. Evaluation of Field Test Results:  Sealants not evidencing adhesive failure from testing or noncompliance with other indicated requirements will be considered satisfactory.  Remove sealants that fail to adhere to joint substrates during testing or to comply with other requirements.  Retest failed applications until test results prove sealants comply with indicated requirements.

3.5 CLEANING

A. Clean off excess sealant or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved in writing by manufacturers of joint sealants and of products in which joints occur.

3.6 PROTECTION

A. Protect joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion.  If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately so installations with repaired areas are indistinguishable from original work.

END OF SECTION 079200
JOINT SEALANTS

079200 - 1

