
SECTION 02300

EARTHWORK

PART 1 - GENERAL

1.01 SUMMARY

A. Perform complete geotechnical investigation and comply with recommendations of investigation report.

B. Perform excavation, filling, compacting and grading operations both inside and outside building limits as required for below-grade improvements and to achieve grades and elevations indicated.  Provide trenching and backfill for mechanical and electrical work and utilities.

C. Provide subbase materials, drainage fill, common fill, and structural fill materials for slabs, pavements, and improvements.

D. Provide suitable fill from off-site if on-site quantities are insufficient or unacceptable, and legally dispose of excess fill off-site.

E. Provide rock excavation without blasting unless blasting is specifically authorized.

1.02 SUBMITTALS

A. Product Data:  Submit manufacturer's product data and installation instructions for each material and product used. 

B. Test Reports:  Submit for approval test reports, list of materials and gradations proposed for use.

1.03 QUALITY ASSURANCE

A. Compaction:

1. Under structures, building slabs, steps, pavements, and walkways, as required by geotechnical report.

2. Under lawns or unpaved areas, as required by geotechnical report.

B. Grading Tolerances Outside Building Lines:

1. Lawns, unpaved areas, and walks, plus or minus 1 inch.

2. Pavements, plus or minus 1/2 inch.

C. Grading Tolerance for Fill Under Building Slabs:  Plus or minus 1/2 inch measured with 10 foot straightedge.

PART 2 - PRODUCTS

2.01 MATERIALS

A. Subbase material (as required by geotechnical investigation and design engineer):  Gravel or crushed stone graded for intended use as subbase for paving materials specified.

B. Drainage fill (as required by geotechnical investigation and design engineer):  Washed gravel or crushed stone, 1/4" to 3/4" size; ASTM C 33, Size 67.

C. Common fill (as required by geotechnical investigation and design engineer):  Mineral soil substantially free from organic and unsuitable materials, and free from rock or gravel larger than 2" in diameter; 80 percent passing No. 40 sieve and not more than 50 percent passing No. 200 sieve.

D. Structural fill (as required by geotechnical investigation and design engineer):  Gravel or sandy gravel free of organic and unsuitable materials and within the following gradation limits:  4" sieve, 100 percent finer by weight; 1" sieve, 60 to 100 percent; No. 4 sieve, 25 to 85 percent; No. 20 sieve, 10 to 60 percent; No. 50 sieve, 4 to 35 percent; No. 200 sieve, 0 to 5 percent.

PART 3 - EXECUTION

3.01 INSTALLATION

A. Comply with requirements of geotechnical investigation report.

B. Excavation is unclassified and includes excavation to subgrade regardless of materials encountered.  Repair excavations beyond elevations and dimensions indicated as follows:

1. At Structure:  Concrete or compacted structural fill.

2. Elsewhere:  Backfill and compact as directed.

C. Maintain stability of excavations; coordinate shoring and bracing as required by authorities having jurisdiction.  Prevent surface and subsurface water from accumulating in excavations.  Stockpile satisfactory materials for reuse, allow for proper drainage and do not stockpile materials within drip line of trees to remain.

D. Compact materials at the optimum moisture content as determined by ASTM D 1557 by aeration or wetting to the percentages of maximum dry density: required by the geotechnical investigation recommendations and design engineer.

E. Place acceptable materials in layers not more than 8" loose depth for materials compacted by heavy equipment and not more than 4" loose depth for materials compacted by hand equipment to subgrades indicated as follows:

1. Structural Fill:  Use under foundations, slabs on grade in layers as indicated.

2. Drainage Fill:  Use under designated building slabs, at foundation drainage and elsewhere as indicated.

3. Common Fill:  Use under unpaved areas.

4. Subbase Material:  Use under pavement, walks, steps, piping and conduit.

F. Grade to within 1/2" above or below required subgrade and within a tolerance of 1/2" in 10'.

G. Protect newly graded areas from traffic and erosion.  Recompact and regrade settled,  disturbed and damaged areas as necessary to restore quality, appearance, and condition of work.

H. Control erosion to prevent runoff into sewers or damage to sloped or surfaced areas.  

I. Control dust to prevent hazards to adjacent properties and vehicles.  Immediately repair or remedy damage caused by dust including air filters in equipment and vehicles.  Clean soiled surfaces.

J. Dispose of waste and unsuitable materials off-site in a legal manner.

END OF SECTION


EARTHWORK


02300-2

