
SECTION 02780

UNIT PAVERS

PART 1 - GENERAL

1.01 SUMMARY

A. Provide unit pavers over cast-in-place concrete sub-base.

1.02 SUBMITTALS

A. Product Data:  Submit manufacturer's product data and installation instructions for each material and product used. 

B. Samples:  Submit two representative samples of each material specified indicating visual characteristics and finish.  Include range samples if variation of finish is anticipated.

1.03 QUALITY ASSURANCE

A. Comply with governing codes and regulations.  Provide products of acceptable manufacturers which have been in satisfactory use in similar service for three years.  Use experienced installers.  Deliver, handle, and store materials in accordance with manufacturer's instructions.

B. Construction Tolerance:  Unit-to-unit offset tolerance of 1/32 inch from flush and 1/8 inch in 10 feet from level or required slope.

C. Mock-Ups:  Provide mock-up as required to demonstrate quality of workmanship.

PART 2 - PRODUCTS

2.01 PRODUCTS

A. Precast Concrete Pavers:  Solid concrete units as manufactured by Pavestone.  Color to match patterned concrete.

B. Mortar and Grout:

1. Mortar:  Portland cement and lime setting-bed mortar, ASTM C 270, Type M.

2. Integral Color:  Pigment additive.

C. Setting Bed:  

1. Mortar over concrete slab.

D. Joint Treatment:  

1. Joint Treatment:  Latex-Modified Portland cement grout, 3/8 inch wide.

2. Expansion joints:  Elastomeric joint filler with horizontal sealant.

PART 3 - EXECUTION

3.01 INSTALLATION

A. Install materials in accordance with manufacturer's instructions and approved submittals.  Install materials in proper relation with adjacent construction and with uniform appearance.  Coordinate with work of other sections.

B. Restore damaged pavers.  Clean and protect work from damage.

END OF SECTION


UNIT PAVERS


02780-1

