

MASTER SHORT FORM SPECIFICATIONS



( 2000 KALIN ASSOCIATES INC.


SECTION 06100

ROUGH CARPENTRY

PART 1 - GENERAL

1.01 SUMMARY

A. Provide rough carpentry:

1. Framing with dimension lumber.

2. Framing with engineered wood products.

3. Rooftop equipment bases and support curbs.

4. Wood grounds, nailers, and blocking.

5. Wood furring.

6. Backing panels.

7. Sheathing.

8. Subflooring.

9. Underlayment.

10. Air infiltration barrier.

1.02 SUBMITTALS

A. Product Data:  Submit manufacturer's product data and installation instructions for each material and product used. 

1.03 QUALITY ASSURANCE

A. Comply with governing codes and regulations.  Provide products of acceptable manufacturers which have been in satisfactory use in similar service for three years.  Use experienced installers.  Deliver, handle, and store materials in accordance with manufacturer's instructions.

B. Lumber Standards and Grade Stamps:  U.S. Product Standard PS 20, American Softwood Lumber Standard and inspection agency grade stamps.

C. Construction Panel Standards:  PS 1, U.S. Product Standard for Construction and Industrial Plywood; APA PRP-108.

D. Preservative Treatment:  AWPA C2 for lumber and AWPA C9 for plywood; waterborne pressure treatment.  Provide for wood in contact with soil, concrete, masonry, roofing, flashing,  dampproofing and waterproofing.

E. Fire-Retardant Treatment:  AWPA C20 for lumber and AWPA C27 for plywood; noncorrosive type.  Provide at building interior where required by code.

PART 2 - PRODUCTS

2.01 MATERIALS

A. Dimension Lumber:

1. Light Framing:  Stud, No. 3 or Standard grade.

2. Structural Framing:  Select structural grade.

3. Species:  Any species of grade indicated.

4. Exposed Framing:  Appearance grade.

B. Boards:

1. Exposed Boards:  19 percent moisture content.

2. Concealed Boards:  19 percent moisture content.

C. Miscellaneous Lumber:

1. Moisture Content:  19 percent.

2. Grade:  Standard grade light framing.

D. Engineered Wood Products:

1. Prefabricated Wood I Joists:  Stress-graded lumber bonded to APA performance rated panel with exterior type adhesive; design stresses for use intended.

2. Composite Joists and Headers:  Laminated lumber veneers; design stresses for use intended.

E. Construction Panels:

1. Combination Subfloor-Underlayment:  APA Sturd-I-Floor, Exterior.

2. Combination Subfloor-Underlayment:  APA Sturd-I-Floor, Exposure 1.

3. Subflooring:  APA Sheathing, Exterior.

4. Subflooring:  APA Sheathing, Exposure 1.

5. Roof Sheathing:  APA Sheathing, Exterior.

6. Plywood Backing Panels:  APA C-D Plugged Exposure 1 with exterior glue, fire-retardant treated.

7. Plywood Underlayment for Resilient Flooring:  APA Underlayment Exterior.

8. Construction Panel Underlayment for Resilient Flooring:  APA Sturd-I-Floor, Exterior.

9. Construction Panel Underlayment for Ceramic Tile:  APA Sturd-I-Floor, Exposure 1.

10. Plywood Underlayment for Carpet:  APA Underlayment Exposure 1.

F. Gypsum Sheathing:

1. Material:  Glass-fiber-surfaced gypsum sheathing board.

2. Type:  Type X fire-resistant ASTM C 79.

G. Auxiliary Materials:

1. Air Infiltration Barrier:  High density polyethylene.

2. Sill Sealer Gaskets:  Glass fiber strip resilient insulation.

3. Framing Anchors and Fasteners:  Non-corrosive, suitable for load and exposure.  Drywall screws are not acceptable.

PART 3 - EXECUTION

3.01 INSTALLATION

A. Wood framing:  Comply with recommendations of NFPA Recommended Nailing Schedule, and NFPA National Design Specifications for Wood Construction.

B. Plywood:  Comply with recommendations of APA Design and Construction Guide - Residential and Commercial.

C. Provide nailers, blocking and grounds where required.  Set work plumb, level and accurately cut.

D. Install materials and systems in accordance with manufacturer's instructions and approved submittals.  Install materials and systems in proper relation with adjacent construction.  Coordinate with other work.

E. Comply with manufacturer's requirements for cutting, handling, fastening and working treated materials.

F. Restore damaged components.  Protect work from damage.

END OF SECTION


ROUGH CARPENTRY


06100-2

