STRUCTURAL INSPECTION

Date:
December 1, 2005

Type:
Primary residence

RE:
Post Hurricane Katrina Structural Inspection

Structure:
Wood frame on post tension slab/brick veneer/seal tab composition shingle roof

Owner(s): 
Sally and David Ducombs

Care of:
Welbilt Custom Homes

Property: 
124 Anna St.





33045 Bayou Paquet Rd.



Slidell, La 70458




Slidell, La 70460



847-2275





Fax # 985-847-2359

History:

Mrs. Tammy Lassere contacted Dammon Engineering to perform a structural inspection on the referenced residence.  She was concerned about the fractures in the foundation.

Findings:

A visual inspection of the residence revealed the following:

1. Entering the front door of the home, a fracture (approximately 1/32 inch wide) in the concrete slab runs north to south in front of the fireplace to the rear door.

2. There is a hairline crack in the concrete slab running from the fireplace to the kitchen.

3. There is a hairline crack in the concrete slab in the dining room running north and south.

4. There is a hairline crack in the concrete slab in the study running north and south.

5. There is a hairline crack in the concrete slab in the master bedroom running east and west from the fireplace

6. There is a second hairline crack in the concrete slab in the master bedroom running from the toilet of the master bathroom to the center of the room.

7. There is a hairline crack in the concrete slab in the rear bedroom running in a wide sweep north to west

Analysis:

It is not known how long these cracks have existed in the slab, but probably go back to the curing cycle and may have been caused by temperature or other weather related problems.  This is not an uncommon finding in this area.  None of these cracks were found to go through the footings.  Fortunately, this is a post tensioned cable slab and tends to hold the unit together, even when there are small cracks.  The foundation is level and no changes in elevation have occurred.  It is recommended that the fractures be treated for termites for the protection of the home.

Conclusion:

It is my professional opinion that the dwelling is structurally sound.

Sincerely,

Emmett G. (Pete) Dammon, P.E.

Louisiana License No. 8796

This inspection is limited to the apparent visual conditions of the structural components of this building.  It does not cover, nor attempts to cover, any components, items, and/or conditions which, by their nature or location, are concealed or are difficult or hazardous to inspect, or which require the moving of furniture, flooring materials, rugs, fixtures, appliances, or any component-part nailed, bolted, or screwed down or shut.  No opinions are expressed regarding conditions which could be discovered only by the disassembly of any component parts, special testing, or removal of any concealing objects.

Inspections are made under normal weather conditions, and are not opinions of the conditions of the property and/or structure which may exist under unusual weather conditions, such as, but not limited to floods, heavy rains or snows, high winds, temperature extremes, or any act of God.  Specific hazardous wastes, toxic substances, toxic mold, air and water quality, communicable diseases, asbestos, soil, environmental, radon, carbon monoxide, formaldehyde, building code and termite conditions are not included in this report unless otherwise stipulated.

This report is not a warranty or guarantee of the property inspected, but it is our opinion of its condition at the time inspected.  Our liability shall be limited to reimbursement of the total cost of inspection.


