554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

February 16, 2018

For: 	Joe Harvin

221 Jacqueline Drive

Slidell, La. 70458

Construction:

One-story raised on pilings, wood frame, with a composition shingle roof.

Scope:

This inspection is limited to a visual inspection of the pilings under the home. No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to perform an inspection of the referenced home due to an inspection of the pilings that were noted to have some rot at the base.

Findings:

Upon inspection, it was visibly noted that five of the pilings that support the front part of the home are rotten at the base, this was further confirmed by tapping on it and listening for a solid sound that the pilings in question are rotten at the base. Two of the pilings in question under the front porch are exposed at the top and not covered by the house.

Conclusion:

The pilings in question have deteriorated over time at the base due to water intrusion. This is typical when the bases of the pilings are not sealed airtight.

Recommendation:

- Secure the existing pilings with a concrete wrap as noted in the attached dwg.

- Seal the top of the two pilings that are exposed under the front porch.

Sincerely,

Brian Mistich, P.E.