554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

February 05 2019

For: Helen Adams 
	         Property Manager

Commodore Apartments

4456 Pontchartrain Drive

Slidell, La. 70458

Two-story, wood frame, brick and vinyl veneer, with a composition shingle roof on a concrete foundation.

History:

Dammon Engineering was contacted and requested to do a structural inspection due to elevation differences noted in the flooring on a second floor apartment located above the foyer entrance to the apartments.

Findings:

An overall visual inspection of the interior of apartment unit 819 was conducted and several items were noted;  the flooring around the kitchen and bathroom have settled leaving gaps between the base boards and flooring, the sheetrock walls have cracked in these areas also.

An inspection of the exterior of the building for unit 819 was conducted and several items were noted. The left stairwell railing on the second floor has a gap between railing and the concrete walkway and the beam under that area is sagging. The beams that support unit 819 are sagging also along with the floor joist.

Some of the vinyl soffit was removed from around the beams and bottom of the floor joist and it was noted to be inundated with termite damage causing major structural weakness to the supporting beams. Additional vinyl was removed revealing extensive damage to main beams and cross members.  An exposed termite nest appeared to be of substantial size; however no active termites were noted at the time of inspection.

Recommendation:

Due to the extent of the damage it is recommend that:

- A thorough termite inspection and preventative treatment program for the entire structure should be preformed.

- An inspection of the entire structure to determine if additional areas of the building have been or are being compromised.

- Replace main beams and floor joist members affected by termite damage.

- An inspection for any leaks or water sources that may leak or be leaking into the sub-flooring or into the walls.

- Lifting the sagging second floor back into place.

Once completed, reinstall vinyl to seal as best as possible the newly installed wood members.  Please see the attached pictures for reference.

Sincerely,

Brian Mistich, P.E.

Pictures attached: