GL-4  1/4”  CLEAR TEMP – 1/2” MILL AIRSPACE – ( ¼” CLEAR TEMP / 0.09 PVB /  ¼” CLEAR TEMP)

ASTM E 1300 GLASS LOAD RESISTANCE REPORT

JOB DETAILS:

Project Name:   Algiers Pediatric 003     -          MARK B – 20.25 x 12 (Inner  & Outer Panes)

WINDOW GLASS DETAILS:                         1-1/4”  Insulated Window

Lite Designation                             QTY 2  Window

Rectangular Dimensions:	Long:    20.25”            : Short:   12”

Window Construction:     	 Insulated

¼” Glass / ½” Air Space/  (¼”  TEMP / 0.09 PVB /  ¼”  TEMP)

Window Orientation:		Sloped at 0° from Horizontal

Outer Lite

Product                                            1/2“ Tempered

Glass Type:			Laminated  & Tempered

Construction:			Monolithic

Nominal Thickness:		Plate thicknesses   --  .509”

InnerLite

____________________________________________________________________________

Glass Type:                                      ¼ “ Tempered

Construction:		  	Monolithic

Nominal Thickness:	 	Plate thicknesses   --  1/4”

Laminate Construction:	               n/a

SHORT DURATION LOAD, RESISTANCE AND DEFLECTION DATA:

Load (<=60 sec.)    		                                            :       45 psf

Load Deflection (Inner  Lite):				:    < 0.001     in

Load Deflection (Outer  Lite):				:    < 0.001     in

Maximum Allowable Glass Deflection:	:        L/175

CONCLUSION:

This glass configuration is below the maximum L/175 deflection for the specified loading.

STATEMENT OF COMPLIANCE:

Procedures followed in determining the resistance of this window glass configuration are in accordance with ASTM E 1300-97.

Disclaimer:

The load resistance of specified glass types exposed to uniform lateral loads of short or long duration subject to the following conditions:

- The glass is free of edge and surface damage and has been properly glazed in the opening in conformance with the manufacturers recommendations.

- The glass is supported on all sides by a framing system sufficiently stiff to limit lateral deflection of the glass edge (not center-of-glass) less than to 1/175 of the glass edge length; Center of glass deflection in excess of 19-mm (0.75-in.) is a design issue and does not affect glass strength;

- The laminated glass factors for short term loads are representative of roof temperature data to which the glass is exposed.

For other limiting conditions that may apply, refer to Section 5 of ASTM E1300 and local building codes.

Prepared by : 	__________________________	Date:_______6/19/2016_____