Dimensions

| Actual inside diameter (in.) | 1.61 | Product Height (in.) | 1.5 |
| --- | --- | --- | --- |
| Actual outside diameter (in.) | 1.71 | Product Length (ft.) | 300 ft |
| Pipe Size | 1-1/2" | Product Width (in.) | 1.5 |
| Product Depth (in.) | 1.5 |  |  |

Details

| Coiled | Yes | Pipe or Fitting Product Type | Pipe & Tubing |
| --- | --- | --- | --- |
| Material | Polyethylene | Product Weight (lb.) | 387 lb |
| Maximum Working Temperature (F) | 80 | Rating | DWV |
| Maximum working pressure (psi) | 100 | Recommended function | Water Supply |
| Minimum working temperature (F) | 0 | Returnable | 90-Day |
| Pipe & Tubing Product Type | Polyethylene | Wrapped | No |

# 1-1/2 in. x 300 ft. IPS 100 psi NSF Poly Pipe