
SECTION 07600

FLASHING AND SHEET METAL

PART 1 GENERAL

1.1 SUMMARY

A. Provide flashing and sheet metal.

PART 2 PRODUCTS

2.1 MATERIALS

A. Applications:

Metal counterflashing and base flashing.

1. Exterior wall flashing and expansion joints.

2. Built-in metal valleys, gutters, and scuppers.

3. Gutters and downspouts.

4. Exposed metal trim and fascia units.

5. Sheet metal accessories.

6. Ridge and soffit vents.

B. Sheet Metal Flashing and Trim:

Zinc-Coated Steel:  ASTM A 653, G90 hot-dip galvanized, 20 gauge (.0359 inch).

1. Sheet Aluminum:  ASTM B 209, alloy 3003, clear anodized, 20 gauge (.0359 inch).

C. Flexible Sheet Membrane Flashing:  Nonreinforced flexible black elastic sheet, 50 to 65 mils thick, neoprene synthetic rubber.

D. Fabricated Units:  Compliance with SMACNA  Sheet Metal Manual.

E. Elastic Expansion Joints:  Factory-fabricated metal-flanged edges to fit curbs and curb substrate.

F. Ridge and Soffit Vents:

Continuous aluminum strip soffit vents

1. Baffled ridge vent suitable for direct application of shingles.

G. Auxiliary Materials:

Solder compatible with metal.

1. Bituminous isolation coating.

2. Mastic and elastomeric sealants.

3. Epoxy seam sealer.

4. Rosin-sized building paper slip sheet.

5. Reglets and metal accessories.

6. Gutter and conductor head guards.

END OF SECTION


FLASHING AND SHEET METAL


07600-1

