554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

Fax: 985-641-5950

dammonengineering.com

dammoneng@bellsouth.net

# Structural Inspection

September 10, 2014

For: 	Luke M. Calamari

Gardner Realtors

1300 Gause Blvd.

Suite C-1

Slidell, LA. 70458

Ref:     2804 Carey St.

Slidell, LA 70458

Construction:

Two-story, wood frame with vinyl veneer and composition shingle/metal roof on a raised pier foundation. This house was built in 1902.

Scope:

This inspection is limited to a visual inspection of the shell of the home, including the interior and exterior foundation of the residence.  No inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers Standards and Practices for Residential and Small Building Property Condition Surveys.  This report is not an explanation of cause, effect, or engineering.

History:

Luke Calamari with Gardner Realtors contacted Dammon Engineering requesting a structural inspection of the referenced home due to a home inspection report that noted the piers in the rear of the home to be settling from improper installation.

Findings:

All the original pier supports for this home are of stacked bricks that have settled over the lifetime of this home. As you can tell from the attached pictures a lot of the piers have been shimmed up to level that pier out but have since shifted. Since hurricane Katrina it suffered more settling in the front of the home and it was leveled to bring it back to original floor height within limits.

Some of the new cinder blocks used as piers for leveling are not installed properly; they are laid sideways and have also settled.   It also appears that that some of the ledger boards are rotten and sagging in the left rear of the home. No termite shields are installed on any of the existing and new piers.

Analysis:

There appear to be low areas under the home with lots of debris ranging from old piers that were replaced and a stump with large roots spreading throughout.  These areas can trap rain water and prevent it from draining away from the foundation therefore causing the piers to settle.

Conclusion:

House foundations all settle.  Usually everything settles together, and the fastest rate of settlement occurs in the first year after construction.  By the fifth or sixth year the settlement has exponentially slowed to where there is little danger that something will happen unless caused by improperly installed piers, weather, expansion & contraction, tree roots, improper drainage, etc.

When this house was built in 1902 there were no codes for installing brick piers. The new building codes for new construction require that a concrete footing be installed around the exterior of the house and all load bearing walls with proper strapping through the concrete footing and the pier be attached to the house. If one or two piers are only repaired then the new bldg code does not apply.

Recommendation:

- Remove stump & all roots under house, back fill with structural fill.

- Remove all debris under house.

- Repair & level all piers that have settled into a leaning position.

- Repair & level all cinder blocks that are installed incorrectly.

- When doing any repairs to the piers, install termite shields.

It is my opinion that the structural integrity of this home can be repaired and secured from future settling.

Sincerely,

Brian Mistich

PE:30187