554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

September 18, 2018

For: Parkview Condo HOA

103 Parkview Blvd.

Mandeville, La. 70471

Attn: Jan Mullen

Construction:

Two-story, wood frame, vinyl veneer, with a composition shingle roof on a post tension foundation.

History:

Dammon Engineering was contacted to request a structural inspection due to termite damage noted on the stairwell of building #300. The manger noted dirt falling out the siding and determined to investigate further.

Findings:

An overall visual inspection of the exterior of the building was conducted and several items were noted. The stairwell for building #300 has been inundated with termites causing major structural damage to the supporting beams. The termites don’t appear to be active at this time.

The stairwell consists of wood stringers with wood risers and treads, both landing and porches are supported by wood joist, decked over with plywood and a lightweight concrete on top. These stairs and landings are connected to horizontal wood beams that are attached to the exterior 2x4 walls. This whole stairwell is structurally damaged by the termites.

This stairwell also serves two units and each have a rear porch. These porches are constructed out of wood also and have signs of major termite damage on the supporting beams.

Recommendation:

Due to the extent of the damage it is recommend that the whole stairwell and porch’s be removed and replaced with new treated wood and new lightweight concrete to allow for a complete sealed system. Please see the attached pictures for reference.

The roof and vinyl siding should be inspected for leaks and sealed as necessary.

Sincerely,

Brian Mistich, P.E.