554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

November 10, 2017

For: 	Stacey Pereira

Ref:     1706 Dunkirk

Slidell, La. 70458

Construction:

One-story, wood frame, brick veneer, carpet and wood flooring with a composition shingle roof on a conventional foundation.  Home is approximately 35 years old.

Scope:

This inspection is limited to a visual inspection of the shell of the home, including the interior and exterior foundation of the home. No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to request a structural inspection of the referenced home due to a home inspection that noted some cracks in the brick veneer and a crack in the foundation.

Findings:

Upon inspection, a zip level was used to verify the floor height conditions.  The level was set up at the front door. The elevation ranges in the house from 0.0” to -0.5” The area in question, master bathroom appears to be level with the front door elevation.  An overall visual inspection of the interior sheet rock and flooring especially in the master bathroom does not appear to show any cracks.

An overall visual inspection of the exterior of the home was conducted and few items were noted. There is a crack in the foundation on the left side of the home; the fill was removed in this area for observation. It appears to start at the top of the foundation and go down approximately 5” and stops before going into the bottom of the footing.

There are a couple of cracks in the brick veneer here and there.  There appears to be more cracks in the mortar around the house than the brick veneer.

It was also noted that there are no gutters or down spouts on the home. The front left corner of the home near the entrance of the garage, the earth is eroding around the foundation due to the water runoff of the roof.  In the front of the home near the entrance, earth is eroding around the foundation due to water runoff of the roof.

Conclusion:

It is important to note that all foundations settle.  Usually, everything settles together and the fastest rate of settlement occurs in the first year after construction.  By the fifth or sixth year the settlement has exponentially slowed to where there is little danger that something will happen unless caused by weather, expansion & contraction, tree roots, improper drainage, etc.  The yard appears to be level and does not allow rain water to flow to the street to keep the foundation dry.

Recommendation:

Due to the fact that there are no visible signs of distress in the sheet rock walls, ceilings or wood/ceramic flooring in the house at the time of this inspection, it is likely that settlement has subsided. Cracks may propagate in the future; however, at this time it appears stable and does not appear to compromise the integrity of the house.

It is recommended when there is more than a 3” elevation difference (tripping hazard) to have the home stabilized with screw pilings; this home only has a ½” in elevation change.

Items to be addressed are as follows:

1)  Seal cracks in the brick veneer, mortar with a non-shrinking grout, to prevent insects from entering the home.

2) The yard should also be re-graded to allow for proper drainage of rainwater away from the foundation and add gutters and down spouts to carry the rain water to the street.

Sincerely,

Brian Mistich, P.E.