554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

January 10-2022

For: 	Jennifer Bondio

215 North Blvd

Slidell, La. 70458

Construction:

One-story, wood frame, brick veneer, ceramic and wood flooring with a composition shingle roof on a conventional foundation.

Scope:

This inspection is limited to a visual inspection of the shell of the home, including the interior and exterior foundation of the home. No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to request a structural inspection of the referenced home due to a home inspection that noted some cracks in the brick veneer.

Findings:

An overall visual inspection of the exterior of the home was conducted and several items were noted.

There are some bricks that have lost mortar around them; the cracks in the brick veneer do not show up in the foundation.

There is a stump on the left side of the home near the foundation that is deteriorating.

Conclusion:

It is important to note that all foundations settle.  Usually, everything settles together and the fastest rate of settlement occurs in the first year after construction.  By the fifth or sixth year the settlement has exponentially slowed to where there is little danger that something will happen unless caused by weather, expansion & contraction, tree roots, improper drainage, etc.

Recommendation:

The cracks in the brick veneer do not appear to have compromised the structural integrity of the home.  It is my opinion that the structural integrity of this home is currently sound, but the foundation will expand and contract with the ground movement and any standing water.  It is recommended when there is more than a 3” elevation difference (tripping hazard) to have the home stabilized with screw pilings.

Items to be addressed are as follows:

- Seal the cracks in the brick veneer with a non-shrinking grout, to prevent insects from entering the home.

- Remove stump.

Sincerely,

Brian Mistich, P.E.

Pictures attached