554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

July 27, 2020

For: 	Jason Doyle

John Welch

337 Carr Drive

Slidell La. 70458

Construction:

One-story raised on CMU blocks, wood frame, vinyl siding, wood flooring/carpet with a composition shingle roof.  The home is approximately 15 years old.

Scope:

This inspection is limited to a visual inspection of the shell of the home, including the interior and exterior foundation of the home. No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to request a structural inspection of the referenced home prior to purchasing it. It was reported that this home did not suffer any structural damage or flooding from Hurricane Katrina.

Findings:

Upon inspection some of the CMU columns on the ground floor were noted to have some surface abrasions. The exterior of the foundation noted some areas in the foundation where the steel is exposed.

At the time of this inspection the interior of the home did not reveal any cracks in the sheetrock ceilings or walls.

Conclusion:

The surface abrasions in the CMU columns and exposed steel in the foundation do not appear to have compromised the structural integrity of the home.  It is my opinion that the structural integrity of this home is currently sound.

Recommendation:

Items to be addressed are as follows:

- Resurface the abrasions in the CMU Columns for a smooth finish

- Resurface the exposed steel in the foundation.

Sincerely,

Brian Mistich, P.E.