554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

October 15, 2021

For: 	Distinctive Real Estate, Inc.

1501 Gause Blvd. Ste. 1

Slidell, La. 70458

Ref:     Bayou Mason

4800 Pontchartrain Drive

Slidell. La. 70458

Construction:

Two-story, wood frame, brick/vinyl veneer with a metal roof on a conventional piling foundation.

Scope:

This inspection is limited to a visual inspection of the shell of the building, including the interior and exterior foundation of the home. No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to request a structural inspection of the referenced two story apartments due to some cracks noted in the concrete walkways and the bulkhead.

Findings:

Upon inspection, an overall visual inspection of the interior courtyard was conducted and several items were noted.

The right side staircase is in need of repair. Where the steel staircase attaches to the building itself it has deteriorated the horizontal wood support. The horizontal wood supports are sagging with the weight of the concrete walkways on top of it and stressing the concrete, therefore cracking it.

The left side staircase is in need of repair. Where the steel staircase attaches to the building itself it has deteriorated the horizontal wood support. The horizontal wood supports are sagging with the weight of the concrete walkways on top of it and stressing the concrete, therefore cracking it.

All the wood base columns supporting the walkways have connectors (ground floor and second floor) that have rusted away and provide no structural support. There are multiple areas that have cracked concrete walkways and are allowing water intrusion and rusting away all connections for the walkway.

Upon inspection of the bulkhead, it was noted that the original concrete bulkhead is in place with an added PVC bulkhead on the outside of it, both bulkheads have failed.  The PVC bulkhead appears to only have one horizontal batter board attached to it and no fill was brought in between the two bulkheads. It also appears that the original concrete bulkhead is still falling outward onto the PVC bulkhead causing damage.

Some drainage concerns where noted also. The property on north side (left rear) of the building is draining into and under the foundation, bulkhead and dock area and causing erosion of the soil as it doesn’t drain into the waterway.

Recommendation:

Items to be addressed are as follows:

- Remove and replace all wood connectors for the columns (ground floor and second floor)

- Remove and replace all horizontal walkway wood supports that are rotten

- Remove and replace all cracked concrete walkways that have more than 1” separation or jack up back in place

- Remove and reinstall steel staircase

- Seal all concrete walkways

- Remove  bulkhead and install new bulkhead

Sincerely,

Brian Mistich, P.E.

Pictures attached