554 Old Spanish Trail

Slidell, LA 70458

Phone: 985-649-5832

dammonengineering.com

info@dammonengineering.com

# Structural Inspection

November 23, 2020

For: 	Heather M. Laughlin

Century 21 Action Reality

4736 West Napoleon Ave, Suite 100

Metairie, La. 70001

Ref:     6627 W Laverne St.

New Orleans, La. 70126

Construction:

One-story, wood frame, brick and vinyl veneer, ceramic flooring with a composition shingle roof on a conventional foundation.

Scope:

This inspection is limited to a visual inspection of the shell of the home, including the interior and exterior foundation of the home. No Inspection of the mechanical or electrical systems was performed.  This report is as outlined by the National Academy of Building Inspection Engineers and is not an explanation of cause, effect, or engineering.

History:

Dammon Engineering was contacted to request a structural inspection of the referenced home due to termites noted.

Findings:

An overall visual inspection of the exterior of the home was conducted and a few items were noted. The rear entrance door is not latching properly due to rotten framing wood, termite infestation and water intrusion due to improper roof drainage. The exterior windows lower framing are rotten and allowing water to intrude into the home where there is no overhang.

The interior of the home was noted to have severally damaged walls and ceilings in many of the rooms. Where these damages occur it is noted to have major termite infestation. Evidentially this home was in a fire at one time due the roof rafters being painted white. Some of the interior walls that fall on the exterior of the home have termite damage all the way to the exterior sheathing.

It was also noted that some areas of the foundation are not level; this is typical for this area.

Conclusion:

Due to the fact that this home has been neglected over the years has allowed water infiltration through the roof and exterior walls, the termites have damaged a major part of the integral structural framing. Upon entering the home the smell of mold and mildew is prevalent and that is a sign of termite infestation.

This home is more than 50% structurally damaged.  It is recommended this home be totally demolished as the structural integrity has been compromised.

Sincerely,

Brian Mistich, P.E.