Site Preparation for Standard Materials New Facility

Project  #1906

Prior to installing any fill, completely remove all surface vegetation, debris, organic matter, muck, and old man-made fill deposits. Digging test pits in various structural areas is recommended to determine the extent of deleterious materials.

Slope excavation to one corner to facilitate removal of any water.

Proof roll stripped areas with observation by a geotechnical engineer prior to installing structural fill.

Provide a minimum depth of two feet of structural fill for all footprints, including five feet outside the footprint. Structural fill to be as follows:

a. Percent Passing U.S. Sieve #200: 50%.

b. Liquid Limit: 40 Max.

c. Plasticity index: 15 Max.

d. Inert material (Non-Expansive).

e. Free of Organics.

f. Maximum Particle Size: 2”.

Install fill in max. eight inch loose lifts and compact to 98% of the maximum dry density by ASTM D-698, Standard Procter.

